## Slide 1
Aerogels
Background Information

## Slide 2: Overview
The following slides present background information on aerogel and its role in nanotechnology. They may be presented as part of a lecture introducing the Aerogel activity.

## Slide 3: Aerogel’s nickname: “Solid blue smoke”
Aerogel resembles a hologram.
Is it there or not?
Aerogel is a highly porous,
solid material.
Aerogel has the lowest density
of any solid known to man.
It is one thousand times less
dense than glass.
NASA Jet Propulsion Laboratory, California Institute of Technology, Pasadena, California

## Slide 4: Aerogel is a Product of Nanotechnology
Aerogels are made of 10nm
silica spheres.
They weigh only slightly
more than air. In fact,
one form is 99.8% air.
About 8,000 of these air bubbles would fit across a single human hair
Scanning electron microscope image of aerogel

## Slide 5: Why is Aerogel Blue?
The size of the air bubbles is similar in size to the
molecules in air and the air pockets in glaciers.
They all scatter blue light more than red, making them look blue.
NASA Jet Propulsion Laboratory, California Institute of Technology, Pasadena, California
Gray Glacier, Torres del Paine National Park Chile

## Slide 6: How is Aerogel Made?
Labs make aerogels by suspending silicon dioxide in alcohol and water to form a gel.
The liquid is removed with carbon dioxide under high pressure and temperature.
Aerogels are expensive to make.

## Slide 7: Extreme Physical Properties of Aerogel
Property | Silica Aerogel | Silica Glass
Density (kgm3) | 5-200 | 2300
Specific Surface area (m2/g) | 500-800 | 0.1
Optical Transmission at 632.8nm | 90% | 99%
Thermal conductivity (1/C at 20-80 deg C) | 0.016-0.03 | 1.2
Acoustic Impedance (kg/m2/s) | 104 | 107
Refractive Index at 632.8 nm | 1.002-1.046 | 1.514-1.644
NASA Jet Propulsion Laboratory, California Institute of Technology, Pasadena, Californisa

## Slide 8: Aerogel is Extremely Strong for its Weight
A 2.5 kg brick
supported on top of
a piece of aerogel
weighing only 2 grams-
over 1000 times
lighter!
NASA Jet Propulsion Laboratory, California Institute of Technology, Pasadena, California

## Slide 9: Why is Aerogel So Strong?
Aerogel has a high surface area to volume ratio.
All of the tiny spheres that make up aerogel provide more structural support than regular glass that has less surface area per volume.
Aerogel structure
German Aerospace Center (DLR)

## Slide 10: Aerogel is an Extreme Insulator
All those tiny glass bubbles
filled with air make
aerogel an amazing
insulator.
40 times better than
fiberglass
NASA Jet Propulsion Laboratory, California Institute of Technology, Pasadena, California

## Slide 11: Aerogel is Transparent
Aerogel panels are used for daylighting. Buildings are
designed to save money by using natural light and thus
reducing lighting costs.
Aerogel is
transparent
and allows light in
through panels
Keeps building warm

## Slide 12: Aerogel is Extremely Lightweight
Aerogel has extremely low density
NASA uses aerogel because it is so lightweight which makes rocket payloads less expensive to send into space.
Was used on the Mars Pathfinder rover and on the Stardust probe
NASA Jet Propulsion Laboratory, California Institute of Technology, Pasadena, California

## Slide 13: Catching Comet Dust
The challenge of the Stardust mission was to gather dust from comet Wild 2. The problem was how to slow down the comet particles from their high velocity without changing their shape and chemical composition.
These particles were travelling six times faster than a rifle bullet but were stopped by a block of aerogel.

## Slide 14: Catching Comet Dust
When a particle hits the
aerogel, it buries itself in
the material, creating a
carrot shaped track up to
200 times its own length.
Since aerogel is mostly
transparent, scientists
can use the tracks to find
the tiny (10 micron) particles.
NASA Jet Propulsion Laboratory, California Institute of Technology, Pasadena, California

## Slide 15: Citizen Science
You can help look for comet dust!
(Computers can’t tell the difference between cracks in the aerogel and tracks made by comet particles; humans can)
http://stardustathome.ssl.berkeley.edu/

## Slide 16: Photo Credits and References
"Aerogels: Their History, Structure, and Applications." The Frontier -. N.p., n.d. Web. 22 Aug. 2015. <http://geobeck.tripod.com/frontier/aerogels.html>.
"Bristolite Daylighting Systems." Bristolite Daylighting Systems. N.p., n.d. Web. 22 Aug. 2015. <http://www.bristolite.com/interfaces/productsummary.aspx?M=4&V=1>.
DeForrest. "Aerogel Uses: Current and Future." Untitled. Western Oregon University, n.d. Web. 22 Aug. 2015. <https://www.wou.edu/las/physci/ch350/Projects_2006/DeForrest/Aerogel%20Project/Uses-Current%20and%20Future.html>.
Liljeholm, Anders. "Aerogel." Nanoscale Informal Science Education. Oregon Museum of Science and Industry, n.d. Web. <http://www.nisenet.org/>.
United States. NASA. Jet Propulsion Laboratory. Aerogel Mystifying Blue Smoke. N.p.: n.p., n.d. Print.
United States. NASA. Jet Propulsion Laboratory. Stardust NASA's Comet Sample Return Mission. N.p.: n.p., n.d. Print.