## Slide 1: Nanotechnology Characterization

## Slide 2: Characterization Techniques
Two types of nanomaterial characterization:
Spectroscopic methods
    i.e. UV-VIS, DLS
  Imaging methods
    i.e. TEM, SEM, AFM
Source: NSC students
Source: NSC students
Notes: Substitute SEM image, and get name of sample
DLS sample?
AFM sample?

## Slide 3: 0-D Nanoparticles
Color of a nanoparticle solution is dependent on nanoparticle size.

## Slide 4: UV-Vis Absorption
Gives quantitative measure of color.
What wavelengths are absorbed?
What wavelengths are transmitted?
Source: Cytodiagnostics
Notes: Gold Nanoparticles (left) A = sphereical, B = urchin shaped
UV-Vis spectrum (right) red solution absorbs green light and allows red light to be transmitted to our eyes while blue solution absorbs red light and allows the blue end of the spectrum to be transmitted to our eyes.

## Slide 5: UV-Vis Spectrometer
Source: Vernier
Notes: The Vernier SpectraVis Plus uses a Diode array for a more compact spectrometer (upper right diagram) Larger benchtop intstrumetns use a monochrometer (dispersion device, exit slit) as diagramed in the bottom center.

## Slide 6: Dynamic Light Scattering (DLS)
DLS measures the Brownian motion of the nanoparticles and correlates this to particle size
Notes: DLS tell you about the size of the particles as well as the distribution of particles within a sample (i.e. the homogeneity of nanoparticles in a sample). Brownian motion of small particles is faster than that of large particles so the position of small particles lose correlation faster.

## Slide 7: Dynamic Light Scattering (DLS)
Source: NSC Students
DLS instrument
Source: www.Malvern.com

## Slide 8: Imaging Methods
Light (Optical) Microscopy
Electron Microscopy
TEM
SEM
Scanning Probe Microscopy
STM
AFM
Profilometry
SEM micrograph
Source: NSC Students
Notes: Need more images

## Slide 9: Resolution Limit
Light microscopes
  500 X to 1500 X magnification
  Resolution of ~0.2 µm
  Limits reached by early 1930’s
Resolution dependent on:
  wavelength of illumination ()
  Numerical Aperture (NA) of lens system
Notes: The lowest wavelength of visible light is around 400 nm which gives the optical limit of about 0.2 microns

## Slide 10: Electron Microscopes
Wavelength of the electron dependent on:
    Electron mass (m)
    Electron charge (q)
    Potential difference to accelerate electrons (V)
Notes: Potential difference is a way to express the momentum of electrons. This equation is related to the deBroglie equation for the wavelength of objects. Electrons can achieve much smaller wavelengths than visible light

## Slide 11: Transmission Electron Microscope
Transmission Electron Microscope (TEM)
e-beam strikes sample and is transmitted through the sample
Scattering occurs
Un-scattered electrons pass through sample and are detected

## Slide 12: Transmission Electron Microscope
Copper Grid Sample Holder
TEM
Notes: Conductive copper grid helps electrons to be transmitted through the sample. Sample must be very thin

## Slide 13: TEM Images
Organic Material
Inorganic Material
Notes: Both biological and inorganic samples can be imaged using a TEM. In the silica nanoparticle on the right the rows of individual atoms can be seen as the white spots in the image.

## Slide 14: Scanning Electron Microscope
Scanning Electron Microscope (SEM)
e- beam strikes sample and electron penetrate surface
Interactions occur between electrons and sample
Electrons and photons emitted from sample
Emitted e- or photons detected
Notes: A helpful animation which shows SEM operation http://virtual.itg.uiuc.edu/training/EM_tutorial/

## Slide 15: Scanning Electron Microscope (SEM)
Conidia of Aspergillus
SEM
Aspex Explorer located at NSC
Notes: Picture of NSC Instrument.

## Slide 16: Scanning Electron Microscope (SEM)
Source: NSC Students
Source: NSC students
A succulent plant
SiO2 spheres

## Slide 17: Scanning Electron Microscope (SEM)
Source: NSC Students
Source: NSC students
A hair “split end”
A “bug” eye

## Slide 18: Scanning Probe Microscopy
Measure feedback from atomically defined tip
Many types of feedback (dependent on tip)
AFM – Forces between sample and tip
STM – Tunneling current between sample and tip

## Slide 19: Scanning Tunneling Microscope
Tip scans just above surface of stage
Electrons have a small probability of escaping material to tip creating tunneling current
Tunneling current is depends on distance between tip and sample

## Slide 20: STM Images
“See” individual atoms
Must have high vacuum , low temp (4 K)
Pt and Ni atoms on an alloy surface
STM at University of Wisconsin – Eau Claire
Notes: STM is actually measuring electrons. Pt which has more electrons than Ni appears darker in the STM image

## Slide 21: Atomic Force Microscope (AFM)
Tip scans across surface
Laser reflects off of cantilever to a photodetector
Feedback loop changes tip to sample distance
Height changes recorded
Notes: A good animated tutorial on AFM: http://virtual.itg.uiuc.edu/training/AFM_tutorial/

## Slide 22: Atomic Force Microscopy (AFM)
AFM Cantilevers and tips
Source: NSC Students
Source: NSC Students
Source: NSC Students

## Slide 23: Atomic Force Microscopy (AFM)
Source: SHINE
Nanosurf EasyScan 2
Source: NSC Students
Butterfly Wing

## Slide 24: Profilometery
Typical profilometer scan
Bruker Dektak XT profilometer
Source: NSC students
Source: NSC students
0.5 nm resolution in the Z-direction
Notes: Stylus is in contact with the sample. Used in semiconductor metrology. X, Y resolution is less. On this instrument is a couple of microns.

## Slide 25: 3-D Profilometery
2-D profilometer scan
Source: NSC students
3-D profilometer scan
Source: NSC students
Notes: A series of 2D scans can be stitched together into a 3-D image.

## Slide 26: Image References
Slide 3 | Adv. Mater. 2006., 18, 2529 - 2534
Slide 4 | Gold nanoparticle shape dependent LSPR. Cytodiagnostics. [Online Image]. 8 May 2016. <http://www.cytodiagnostics.com/store/pc/Introduction-to-Gold-Nanoparticle-Characterization-d3.htm>
Slide 5 | SpectraVis Plus Spectrophotometer. Vernier. [Online Image]. 8 May 2016. <http://www.vernier.com/products/sensors/spectrometers/visible-range/svis-pl/> Spectrometer Diagrams. Adapted from Hewlett-Packard's "Fundamentals of Modern UV-Visible Spectroscopy" publication number 12-5965-512E, 1996. [Online Image]. 8 May 2016 <http://www.the-scientist.com/?articles.view/articleNo/18797/title/Across-the-Spectrum--Instrumentation-for-UV-Vis-Spectrophotometry/>
Slide 6 | Dynamic Light Scattering. Jones, Mike. [Online Image]. 21 June 2016. <https://commons.wikimedia.org/wiki/File:DLS.svg>

## Slide 27: Image References
Slide 6 | Intensity Fluctuations and Brownian Motion. AZO Materials. [Online Image] 10 May 2016. <http://www.azom.com/article.aspx?ArticleID=12255> Weighted Distributions. Yilun LiAndrew R. Barron, Dynamic Light Scattering. OpenStax CNX. ‎May‎ ‎7‎, ‎2014 http://cnx.org/contents/3fc98dad-934d-45e6-a19f-c0a1cf440d43@1.>
Slide 7 | Microscope. [Online Image] 10 May 2016. <http://mssmith.wicomico.wikispaces.net/Tools+Scientists+Use>
Slide 11 | Transmission Electron Microscope. Wikimedia Commons. [Online Image]. 10 May 2016 <https://commons.wikimedia.org/wiki/File:Electron_Microscope.png>

## Slide 28: Image References
Slide 12 | TEM. Boundless. “Electron Microscopy.” Boundless Microbiology. Boundless, 13 Apr. 2016. Retrieved 10 May. 2016 from <https://www.boundless.com/microbiology/textbooks/boundless-microbiology-textbook/microscopy-3/other-types-of-microscopy-30/electron-microscopy-249-1065/> 3 mm copper grid. Lilly_M. Wikimedia Commons. [Online Image]. 17 May 2016. <https://commons.wikimedia.org/wiki/File:3_mm_copper_grid_electron_microscopy_for_sample-04.jpg>
Slide 13 | Golgi Apparatus. [Online Image]. 17 May 2016. <https://courses.candelalearning.com/biology11xmaster/chapter/eukaryotic-cells/> Mesoporous silica nanoparticle. [Online Image]. 21 May 2016. <https://en.wikipedia.org/wiki/File:Mesopourus_silica_closeup.jpg>
Slide 14 | SEM Image. MyScope. [Online Image]. 21 May 2016. <http://li155-94.members.linode.com/myscope/sem/practice/principles/layout.php>

## Slide 29: Image References
Slide 15 | Conidium. Gans, Murray. [Online Image]. 21 May 2016. <http://murry-gans.blogspot.com/2013_04_01_archive.html>
Slide 19 | Scanning Tunneling Microscope. [Online Image]. 22 May 2016. <https://en.wikipedia.org/wiki/Scanning_tunneling_microscope#/media/File:ScanningTunnelingMicroscope_schematic.png>
Slide 20 | Pt and Ni. Richmond, Michael. [Online Image]. 22 May 2016. <http://spiff.rit.edu/classes/phys314/lectures/stm/stm.html> STM. [Online Image]. 22 May 2016. <http://www.uwec.edu/Matsci/center/instrumentation/>
Slide 21 | AFM. Hansma, Helen. [Online Image]. 22 May 2016. <http://web.physics.ucsb.edu/~hhansma/biomolecules.htm>

## Slide 30: Image References
Slide 22 | Butterfly Wing. NanoSurf. [Online Image]. 22 May 2016. <https://www.nanosurf.com/en/application/70-butterfly-wings-a-fragile-biological-nanostructure>