## Slide 1: Nanotechnology Fabrication

## Slide 2: Nanomaterial Fabrication
A nanomaterial is a structure which is smaller than 100 nm in at least one dimension.
0-D Nanoparticles
1-D Nanowires or nanotubes
2-D Thin films
3-D Porous structures
Notes: The number of dimension corresponds to the dimensions that are NOT in the nanoscale

## Slide 3: Types of fabrication
Top Down
Bottom Up
Chemistry!
Crystal Growth
0-D particles
1-D particles
2-D films
Milling
Large size distribution
No control of shape
Impurities
Lithography
Notes: Bottom up = starting with atomic/molecular precursors, combining to form nanomaterial
Top Down = starting with bulk material and removing material until a nanomaterial is obtained

## Slide 4: Nucleation and growth
NP’s from homogenous solution
Source: Nanostructures & Nanomaterials, Cao, G. Fig. 3.2
As r  Esurface 
Esurface α r2
As r  Evolume 
Esurface α r3
r* = critical nucleus size

## Slide 5: 0-D Nanoparticle Synthesis
Example: Reduction of chlorauric acid (HAuCl4) with sodium citrate  Gold NPs

## Slide 6: 1-D Nanostructures
Nanowhiskers and fibers
Nanorods and nanobelts
Nanowires
Carbon Nanotubes
4 : 1
6 : 1
12 : 1
36 : 1
Aspect ratio = length ÷ diameter
Notes: 1D nanostructures are loosely differentiated by aspect ratio. Smaller aspect ratio = nanorod , larger aspect ratio = nanofiber or nanowire

## Slide 7: 1-D Nanostructures
Bottom up:
Anisotropic spontaneous growth
Template directed
Top Down:
Laser ablation synthesis of carbon nanotubes (CNTs)
Notes: Anisotropic: growth must be faster in one direction than in others for spontaneous growth to result in a 1D structure. (isotropic growth would lead to 0D structures)

## Slide 8: Anisotropic Growth
Surfactants can bind to certain facets of a crystal and encourage anisotropic growth

## Slide 9: Template Based Synthesis
Cross section of nanowires in template
Notes: Template can be removed by selective etching and nanowires can be isolated

## Slide 10: Synthesis of Carbon Nanotubes
Laser ablation (vaporizing graphite with a laser)
Plasma arcing of graphite or coal
Combustion synthesis
  Burn hydrocarbon at low pressure
Notes: Top down synthesis is imprecise, fullerenes and graphene are also produced.
Diagram shows Plasma Arcing Method

## Slide 11: 2D Nanostructures
Thin films – Thickness less than 100 nm
Vapor Deposition
  Thermal Evaporation
  Sputtering
  Chemical Vapor Deposition (CVD)
Solution Deposition
  Self-assembly
  Electroplating
  Spin Coating

## Slide 12: Thermal Evaporation
Vacuum (10-4 – 10-8 Torr)
Source material is heated and evaporates
Source material deposits on substrate
  Control concentration of growth species in vapor
  Thickness measured in situ
  Angstroms to 100’s nm thick layers

## Slide 13: Sputtering
Rough Vacuum (10’s of mTorr) with a constant stream of gas
High voltage forms plasma ex: Ar gas  Ar+ + e-
Plasma (Ar+) accelerated towards target
Ar+ hits target, neutral target atoms (Au) are ejected
Ejected atoms (Au) deposit on substrate

## Slide 14: Chemical Vapor Deposition (CVD)
Rough Vacuum (10’s of mTorr)
Reactive gas added
Chemical reaction in gas phase or on surface
Notes: CVD of indium phosphide (InP) is depicted. InP grown in this in manner may be used to make active material for a laser diode.

## Slide 15: Image References
Slide 4 | Guoshong, Cao. "Nanostructures and nanomaterials." (2004). Fig. 3.2
Slide 5 | Gold Nanoparticle Synthesis. UWMRSEC. [Online Image] 22 May, 2016. <http://education.mrsec.wisc.edu/277.htm>
Slide 8 | Gold Nanoparticle Growth. Chalmers Research Group. [Online Image] 29 May, 2016. <http://www.materialsmodeling.com/index.php/component/content/category/17-positions>
Slide 9 | Artin Petrossians, John J. Whalen III, James D. Weiland and Florian Mansfeld (2013). Nanotechnology for Packaging, Advances in Micro/Nano Electromechanical Systems and Fabrication Technologies, Assistant Professor Kenichi Takahata (Ed.), InTech, DOI: 10.5772/55033. Available from: <http://www.intechopen.com/books/advances-in-micro-nano-electromechanical-systems-and-fabrication-technologies/nanotechnology-for-packaging>

## Slide 16: Image References
Slide 10 | Carbon Nanotube. UC Davis ChemWiki. [Online Image]. 29 May 2016. <http://chemwiki.ucdavis.edu/Wikitexts/New_York_University/CHEM-UA_127%3A_Advanced_General_Chemistry_I/17%3A_Introduction_to_Organic_Chemistry> Arc Discharge. Somnath2. [Online Image] 29 May 2016. <https://commons.wikimedia.org/wiki/File:Arc_discharge_nanotube.png>
Slide 12 | Thermal Evaporation. [Online Image] 29 May 2016. <http://hist-materialer-og-energi.wikispaces.com/Physical+Vapour+Deposition>
Slide 13 | Sputtering. Physics StackExchange. [Online Image] 29 May 2016. <http://physics.stackexchange.com/questions/54936/what-favors-island-growth-of-a-sputtered-material>
Slide 14 | MOCVD. Crystalgrower. [Oniline Image] 29 May 2016. <https://commons.wikimedia.org/wiki/File:MOCVDprocess.jpg>

## Slide 17: Additional Resources