## Slide 1: Nanoengineering Cellulose for Environmental & Biomedical Applications
Assistant Professor
Chemical Engineering
Biomedical Engineering (Courtesy)
The Pennsylvania State University
sheikhi@psu.edu
Bio-Soft Materials Laboratory (B-SMaL): www.sheikhilab.com
Amir Sheikhi, Ph.D.
NACK Network and NCI-SW
Pennsylvania State University
University Park, PA, USA, April 16, 2020

## Slide 2: This Webinar Is Hosted By
ATE Central acts as an information Hub for the National Science Foundation ATE Grantee Community
atecentral.net/webinars

## Slide 3: This Webinar Is Brought To You By

## Slide 4
Mike
Lesiecki, host
Robert Ehrmann
NACK Network
Introductions
Trevor Thornton Professor
Notes: I’m Mike Lesiecki, with Luka Partners. I’ll be the moderator for the webinar today and I also serve on EvaluATE’s community college liaison panel. Lori Wingate will is the main presenter for the webinar. She is director of EvaluATE, which is located at The Evaluation Center at Western Michigan University.

## Slide 5: Introductions
Presenter
Amir Sheikhi
Assistant Professor
Chemical Engineering

## Slide 6
Amir Sheikhi
EDUCATION
-I was born in Tehran, the capital city of Iran.
-When I was a kid, I really wanted to become an astronaut! I was kind of addicted to collecting space-related magazines that my parents got worried about me!
-DID YOU KNOW: During the launch phase, an astronaut has to endure a force of up to four times their own body weight. Ill-fitting dental fillings could become loose or fall out  So, I took a good care of my teeth and never had any problem with them…but never became an astronaut!!
Many years later, I became a Chemical Engineering faculty!!
-Hobbies (Swimming), favorite food (Barberry rice w/ saffron chicken)
FUN FACT(S) about ME
BS: University of Tehran, Chemical Engineering
MS: University of Tehran, Chemical Engineering
PhD: McGill University, Chemical Engineering
PDF: McGill University, Chemistry
PDF: Harvard-MIT Health Sciences and Technologies, Engineering in Medicine
PDF: UCLA, Bioengineering
Research Keywords
Experimental Soft Materials
Biomaterials
Living Materials
Environment
Tissue Engineering and Regeneration
Bioseparation
Me!

## Slide 10
More than 38% of men and women
will be diagnosed with cancer at some point during their lifetimes (American Cancer Society, 2013-2015)
Every 20 seconds, a child dies…
from not having access to clean water
Chart: 
| 1st Qtr | 2nd Qtr | 3rd Qtr | 4th Qtr
Sales | 67 | 10 | 9 | 14
0
1-3
4-5
>6
side effects
14%

## Slide 11
The most abundant…
…biopolymer
in the world
…protein
in the body
…mineral
in the soil
Cellulose
Collagen
Silicon (Si)
Hairy Nanocelluloses
Layered Minerals
Beaded Gelatin Hydrogels
Micro-/Nanoengineered
Soft Materials
Notes: What if we could use natural materials to overcome the biggest challenges in environment and medicine?
These materials are the most abundant
They are, biodegrdable, and they are always renewed by nature (there for us),
Outline in the left

## Slide 12: Outline
Part IV:
Water remediation
Part I:
Scale inhibition
Hairy nanocelluloses
Part III:
Scale-resistant interfaces
Part II: Biomimetic mineralization
Part V: Other applications
Nanocomposites
Bactericides
Humidity switches
Rheology modifiers
Notes: Remove the materials (images of NCC etc)
Highlight the keywords

## Slide 13: Conventional nanocelluloses
1 µm
200 nm
Kontturi et al., Advanced Materials (2018)
Dufresene, Materials Today (2017)
Habibi et al., Journal of Materials Chemistry (2008)
Malainine et al., Carbohydrate Polymers (2003)
Late 1970s ITT Rayonier labs
Whippany, NJ
CNC
MFC/NFC
Biorenewable
Biodegradable
Cost effective
Environmentally friendly
Large surface area (>100 m2/g)

## Slide 14: Introduction to conventional nanocelluloses
Conventional nanocelluloses
Anselme Payen
1795-1871
Applications
Bengt Rånby
1920-2000
Nanocomposites (1100 articles)
Films (500)
Hydrogels (240)
Rheology (190)
Coating (160)
Aerogels (145)
Fillers (145)
Optical (140)
Self-assembly (120)

## Slide 15
Conventional nanocelluloses
Applications
Tan et al., Science of The Total Environment (2019)
Introduction to conventional nanocelluloses

## Slide 16
Conventional nanocelluloses
Introduction to conventional nanocelluloses

## Slide 17
Conventional nanocelluloses
Applications
Introduction to conventional nanocelluloses

## Slide 18: Introduction to Hairy Nanocelluloses
Conventional nanocelluloses
Hairy nanocelluloses
Unique properties
Colloidal structure
Functional groups
Charge density
Colloidal stability
Facile production
Biodegradation/ hemocompatibility
Cellulose Nanotechnology
Research Consortium

## Slide 19: Part I: Scale inhibition
Sparingly soluble salts
  Anions: CO32-, SO42-, …
  Cations: Ca2+, Mg2+, Ba2+, …
Examples of affected operating units
  Cooling towers, digesters, evaporators, and heaters
Problems: Fluid mechanics, heat and mass transfer
Inhibition methods
  Acid treatment, ion exchange, macromolecular additives

## Slide 20
Most of the antiscalants are not biodegradable
Their backbone is toxic
They comprise phosphorus and nitrogen
Their functional groups result in eutrophication
Canadian Water Quality Guidelines for the Protection of Aquatic Life, Canadian Council of Ministers of the Environment, 2004.
Drawbacks of current macromolecular antiscalants
= 0.1 ppm

## Slide 21
Simulated industrial scale formation
No additive
Chronoamperometry
Ca2+, Cl-
Na+, HCO3-
Industrial antiscalant
concentration = 10 ppm
Ideal scale inhibition!
Clean
electrode
Scaled
electrode
Highly phosphonated
Flexible
Sheikhi et al., Environmental Science: Water Research & Technology (2015)

## Slide 22: Nanocelluloses as antiscalants
CNC (66.6 ppm)
TEMPO-CNC (66.6 ppm)
NFC (66.6 ppm)
https://www.tomorrowsuccess.com/dare-dont-fear.html, Accessed on Jan 11, 2019
Sheikhi et al., Materials Horizons (2018)
CMC (16.6 ppm)
CMC (166 ppm)
COOH = 4.6 mmol g-1
Not enough charge content
Not enough flexibility

## Slide 23: Hairy nanocelluloses
van de Ven and Sheikhi, Nanoscale (2017)

## Slide 24: Hairy nanocelluloses
Sheikhi and van de Ven, Current Opinion in Colloid & Interface Science (2017)
Sheikhi et al., Journal of Visualized Experiments: JoVE (2016)
Yang et al., Langmuir (2012)
COOH concentration = 0.01195 (VNaOH) × 10 mM (NaOH concentration) / 0.02 g (initial ENCC) ~ 5.98 mmol/g

## Slide 25
Hairy nanocellulose synthesis
Preparing partially oxidized fibers
Preparing electrosterically stabilized nanocrystalline celluloses (ENCC)
1
2
3
4
5
6
11
10
9
8
7

## Slide 26: NCC versus ENCC
[KCl] (mM)
[KCl] (mM)
Hydrodynamic d (µm)
ζ (mV)
Sheikhi et al., Journal of Colloid and Interface Science (2014)
NCC
ENCC
Notes: Write in color for CNC and HCNC

## Slide 27: ENCC assembly
Yang et al., Biomacromolecules (2016)
Notes: Write in color for CNC and HCNC

## Slide 28: ENCC assembly
Tavakolian et al., Journal of Colloid and Interface Science (2019)
Notes: Write in color for CNC and HCNC

## Slide 29: Hairy nanocelluloses as antiscalants
Sheikhi et al., Materials Horizons (2018)
High functional group density
Structural flexibility

## Slide 30
ENCC (8.3 ppm)
ENCC (16.6 ppm)
Additive | C (ppm) | COO-/Ca2+ (mol/mol)
ENCC | 12.5 | 0.037
DCC | 8.3 | 0.026
Sheikhi et al., Materials Horizons (2018)
Hairy nanocelluloses as antiscalants
Notes: Legend for half scale

## Slide 31
Hairy nanocelluloses as an antiscalant
Sheikhi et al., Materials Horizons (2018)

## Slide 33
http://biologyencore.tumblr.com/
Accessed on 12/08/2015
http://www.snail-world.com
Accessed on 12/08/2015
http://www.toonpool.com
Accessed on 12/08/2015
http://www.123rf.com
Accessed on 12/08/2015
Part II: Biomimetic mineralization

## Slide 34: Biomimetic mineralization of CaCO3 using ENCC
Anionic hairy nanocelluloses (ENCC)
Sheikhi et al., Crystal Growth & Design (2016)

## Slide 35
2 μm
2 μm
30 μm
50 μm
Biomimetic mineralization of CaCO3 using ENCC

## Slide 36
50 μm
10 μm
Sheikhi et al., Crystal Growth & Design (2016)
Biomimetic mineralization of CaCO3 using ENCC

## Slide 37: Part III: Scale-resistant interfaces
Sheikhi et al., ACS Applied Materials & Interfaces (2018)
Sheikhi et al., Journal of Materials Chemistry A (2018)
Uncoated
ENCC coated

## Slide 38: Part IV: Water remediation
Additive | qe (mg/g)
ENCC | 185
CM-BNCC | 9.7
Activated C | 4.4
Lead
Copper
Mercury
Cadmium
Arsenic
Sheikhi et al., ACS Applied Materials & Interfaces (2015)
O (1 µm)
O (100 nm)

## Slide 39: Dye removal using hairy nanocellulose-based foams
Yang et al., Langmuir (2016)

## Slide 40: Part V: Reinforcing papers
Sheikhi et al., ACS Applied Nano Materials (2018)

## Slide 41: Part V: Antibacterial nanocrystalline cellulose
Tavakolian et al., ACS Applied Materials & Interfaces (2018)

## Slide 42: Part V: Nanocellulose-based humidity switch
Safari et al., ACS Applied Materials & Interfaces (2016)

## Slide 43: Part V: Colloidal nano-toolbox for molecularly regulated polymerization
Sheikhi et al., Materials Horizons (2017)

## Slide 44: Concluding remarks
Hairy nanocelluloses (HNCs)
Nanoengineering cellulose fibers via facile chemistry yields HNCs.
HNCs overcome the structural limitations of conventional nanocelluloses.
HNCs can provide reliable, green scale inhibitors.
Cellulose-based scale-resistant membranes are now feasible.
HNCs are promising candidates for water remediation, reinforced nanocomposites, bactericides, humidity switches, and rheology modifiers.
Chart: 
| colored | blank
% | 40 | 60

## Slide 45: Acknowledgments
2
Prof. Theo van de Ven
Prof. Ali Khademhosseini
Prof. Dino Di Carlo
Prof. Ashok Kakkar
Prof. Pierre Carreau
Prof. Samanvaya Srivastava
Dr. Rahmi Oklu
Dr. Han Yang
Dr. Salman Safari
Dr. Na Li
Dr. Søren Leth Mejlsøe
Dr. Md. Nur Alam
Dr. Reihaneh Haghniaz
Ms. Nicole Kuntjoro
Mr. Joseph de Rutte
Mr. Enzo Bomal
Mr. Outman Akouissi
Mr. Alireza Sohrabi

## Slide 46: Funding sources
Notes: Group and PI with the flight at the corner

## Slide 48: Join Us
Webinar on May 14, 2020
1 PM Eastern
Luminescent Nanoparticles of Metal Oxides
Yuanbing Mao, PhD
Professor and Chair
Department of Chemistry
Illinois Tech