## Slide 1: Basic Nanotechnology Processes E SC 212
Notes: <number>

## Slide 2
Unit 2 An Introduction to Uses of Plasma in Processing
Plasma Basics
Lecture 1

## Slide 3: Outline
What is a plasma?
How are they made?
Why are they useful in processing?
Additive Plasma Processes
Subtractive Plasma Processes
Notes: <number>

## Slide 4: Basic Definition of a Plasma
An (almost) neutral “soup” of electrons and positively charged ions

## Slide 5: How is it made?
By using some energy source to tear the electrons off of atoms (ionize the atoms) resulting in energetic electrons and ions
Examples: lighting discharge, fluorescent light, sodium vapor lamps, flames
Each plasma has a specific color determined by its composition (the gas(es) used) due to quantum mechanical energy levels

## Slide 6: Common Plasma--Lightning

## Slide 7: Common Plasma--Fluorescent Lights
A good example of a “plasma system” that you are familiar with is the fluorescent lights.
What do you know about the fluorescent lights?
  Use electrical energy to ionize atoms.
  Under vacuum to prevent chemical reactions with air and to allow atoms and materials sufficient mean free path to allow for electron dissociation (i.e., ionization).
  Emissions from ionized Hg gas (plasma) plus impact of coating on inside of tube plus causing fluorescence gives light at many wavelenghts = (almost) white light. Different gases can change the color of the fluorescent light.
Notes: <number>

## Slide 8
Man-made Plasmas for Processing

## Slide 9: How are the Plasmas Used in Processing Created?
DC bias (like a lightning storm).
AC bias (like a fluorescent bulb).
  There are two basic types of AC plasmas:
    capacitively coupled
    inductively coupled plasmas
Notes: <number>

## Slide 10: General Set-up
Cathode
Anode
Plasma
Vacuum Chamber Walls
Public Domain: Image Generated by CNEU Staff for free use
Notes: <number>

## Slide 11: Man-made Plasmas for Processing
Vacuum = Clean and completely controlled
Environment is completely defined by user so full control of possible chemical reactions and of collisions between molecules, atoms, etc.
Control space between the gas, molecules, ions and electrons thereby controlling collisions and possibility of ionization
Why is spacing important?
    The space allows for collisions of the material to provide dissociation.
    Spacing between the gas atoms or molecules is called Mean Free Path (MFP). Plasma glows a specific color depending on its constituents.
Notes: <number>

## Slide 12: Plasma Overview
MFP allows energy to be transferred to the gas.
Electric fields in a plasma can cause accelerated collisions, dissociation, and/or ionization.
Dissociation is the splitting of molecules into parts of molecules. Often these parts are radicals (unpaired electrons) which are very chemically active.
Ionization is stripping electrons from atoms or molecules.
Notes: <number>

## Slide 13: Why are Plasmas Useful in Processing?
Energetic ions can be used to bombard surfaces thereby driving chemical reactions giving etching or deposition.
Plasmas can be used to split apart precursor gas atoms or molecules in the plasma. The fragments can recombine to produce unique materials that deposit as films.
Energy is not supplied in the form of heat but as electrical energy through current and voltage. Generally this allows a relatively lower temperature process.
Plasmas have dissociated atoms, molecules, and radicals, and can also have chemical reactions, occurring in the plasma and/or at the surface.
Plasmas have physical processes too: ion bombardment.
Notes: <number>

## Slide 14: Controlling Factors in Man-made Plasmas
Pressure
Energy input
Flow rate
Voltage developed between the plasma and substrate
Chamber condition

## Slide 15: DC Plasma
DC Power Source
Cathode
Anode
Vacuum Chamber Walls
Plasma
Public Domain: Image Generated by CNEU Staff for free use
Notes: <number>

## Slide 16: DC Plasma
Substrate to undergo processing can be placed on the cathode or anode.
Substrate on cathode will be impacted by neutral particles (atoms, molecules) and positive ions.
Substrates on the anode will be impacted by neutral particles (atoms, molecules), negative ions, and electrons.
Set-up can be designed to have strong positive ion bombardment on the cathode. Material etched off cathode can then be deposited on a substrate placed on the anode. This deposition process is called DC sputtering. The material removal at the cathode is etching. A plasma processing tool can be designed to optimize deposition or etching.
Notes: <number>

## Slide 17: AC Capacitively Coupled
Cathode
Anode
Plasma
Vacuum Chamber Walls
Public Domain: Image Generated by CNEU Staff for free use
Notes: <number>

## Slide 18: AC Plasma: Capacitive Coupling
Energy is coupled into the plasma through time-changing electric field.
Usually driven at Radio Frequency 13.54 MHz.
Resulting plasma can be used for etching and deposition depending on the design of the processing chamber and the gases used.
Can be designed to have positive ions bombard the cathode.
Notes: <number>

## Slide 19: AC Plasma: Inductive Coupling
Energy is coupled into the plasmas through time-changing magnetic fields.
There are two common versions:
Inductively Coupled Plasma (ICP) and
Transformer Coupled Plasma (TCP).
Depending upon the system, they can be driven at RF or microwave energy.
Resulting plasmas can be used for etching and deposition, depending on the design of the processing chamber and the selected gas.
Notes: <number>

## Slide 20: Overview of Types of Plasma Processes
Additive processes---using plasmas for deposition
Subtractive processes---using plasmas for etching

## Slide 21: Plasma Processing Today

## Slide 22: Summary
Plasmas play a very big role in nanofabrication
Biggest role is in top down nanofabrication
They are important because they open paths to useful chemistry and this chemistry can be done at (relatively) low temperatures
This chemistry can be used for deposition (additive processes) or etching (subtractive processes)
Plasmas can be used to exploit chemical and physical phenomena
Notes: <number>