## Slide 1: Basic Nanotechnology Processes E SC 212
Notes: <number>

## Slide 2
Unit 2 An Introduction to Uses of Plasma in Processing
Lecture 2
Additive Processes and Sputtering

## Slide 3: Outline
Additive processes
Sputtering
Types of sputtering
Applications of sputtering
Notes: <number>

## Slide 4: Additive processes
These are what are termed deposition processes--- adding a thin film of a material
There are many types; e.g., evaporation, sputtering, chemical vapor deposition, plasma enhanced deposition, atomic layer deposition.

## Slide 5: Sputtering
In this example of sputtering, a film is being deposited
on the substrate by argon ions (green). These ions act as hammers
knocking film atoms (orange) off the target (orange too). A negative voltage
attracts the Ar ions to the target.
Public Domain: Image Generated by CNEU Staff for free use
Notes: <number>

## Slide 6: Sputtering
Plasma used for sputtering can be AC or DC Generated.
Which is better?
Public Domain: Image Generated by CNEU Staff for free use
Notes: <number>

## Slide 7: Sputtering
Deposition Process can be purely physical or it can be physical and
chemical.
Public Domain: Image Generated by CNEU Staff for free use
Notes: <number>

## Slide 8
Reactive Sputter Deposition
add reactive gas to chamber during deposition (evaporation or sputtering)
  oxygen, nitrogen
chemical reaction takes place on substrate and target
can poison target if chemical reactions are faster than sputter rate
adjust reactive gas flow to get good stoichiometry
without incorporating excess gas into film

## Slide 9: Sputtering
Target can be simple or compound (alloyed, mixed, multiple)
Public Domain: Image Generated by CNEU Staff for free use
Notes: <number>

## Slide 10: Some Sputtering Facts
Use of magnets can help
Threshold for sputtering is about 40eV

## Slide 11: Summary: Basic Sputtering Techniques
DC (diode)
RF (radio frequency)
magnetron

## Slide 12
DC sputtering
simplest - basically what we have talked about so far
Parameters:

## Slide 13
Parameters:
Pressure
Sputter voltage
  maximize sputter yield (S)
  typically -2 to -5 kV
Substrate Bias Voltage
  substrate is being bombarded by electrons and ions from target and plasma
    sputtering film while you deposit
  neutral atoms deposit independently
  put negative bias on the substrate to control this
  can significantly change film properties
Substrate temperature
  control with substrate heater
  heating from deposited material
    increases with increasing sputter voltage
    decreases with increasing substrate bias
Deposition rate
  changes with pressure
  increases with sputter yield
    usually increases with high voltage
Particle Energy
  increases with increasing sputter voltage
  decreases with increasing substrate bias
  decreases with increasing Ar pressure

## Slide 14
DC SPUTTERING RATES
Material | Atoms/ion Sputter Yield @ 400 Volts | Rate Relative to Cu | Static Rate (Angstroms/Minute) Measured @ 4” Source-to-Substrate Distance @ 70 watts/in2 DC @ 1 Millitor
Ag | 2.70 | 2.41 | 24,955
Al | 0.80 | 0.69 | 7,130
Au | 2.00 | 1.80 | 18,400
Cr | 1.10 | 0.70 | 7,250
Cu | 1.62 | 1.00 | 10,350
Mo | 0.70 | 0.57 | 5,870
Pd | 1.73 | 1.32 | 13,570
Pt | 1.20 | 0.88 | 8,980
Doped Si | 0.33 | 0.33 | 3,335
Ta | 0.28 | 0.26 | 2,650
Ti | 0.42 | 0.39 | 4,025
W | 0.28 | 0.23 | 2,300

## Slide 15
RF Sputter Deposition
Good for insulating materials

## Slide 16
Typical AC Sputtering Tool
Shutter
MFC
Target
Substrate
Throttle Valve
RF Power Supply
Ar2
Mechanical Pump
Turbo Pump
Ion Gauge
Blocking Capacitor
Impedance Match
TC1
TC2
Roughing Valve
Foreline Valve
N2
Vent/Purge
Public Domain: Image Generated by CNEU Staff for free use
Notes: <number>

## Slide 17
Magnetron Sputter Deposition
use with DC or RF
goal: increase ionization of Ar
Why? Higher sputter rates at lower Ar pressures (down to 0.5 mTorr)
  fewer gas collisions - more line of sight
How ? increase probability of electrons striking Ar
  increase electron path length
  use electric and magnetic fields
Most common configuration: crossed electric and magnetic fields
Put magnets (200 Gauss) behind target:
traps electrons near cathode
  more ionization near cathods (10x)
  fewer electrons reach substrate (less heating)

## Slide 18: Evaporation and Sputtering
What is the difference?

## Slide 19
Comparison of evaporation and sputtering
EVAPORATION | SPUTTERING
low energy atoms | higher energy atoms
high vacuum path few collisions line of sight deposition little gas in film | low vacuum, plasma path many collisions less line of sight deposition gas in film
larger grain size | smaller grain size
fewer grain orientations | many grain orientations
poorer adhesion | better adhesion

## Slide 20
Ion assisted deposition
Hybrid: evaporation and sputtering
bombard surface with ions
  not necessarily same type as in film
  ions typically NOT incorporated in film
relatively low voltages (50 - 300 eV)
l
  physical rearrangement
  local heating
can change film properties
  (for better or worse)

## Slide 21
SPUTTERING TARGETS
(Often 99.999% pure)

## Slide 22
COMMON SPUTTERING TARGETS MATERIALS |  | 
Boron Nitride | Boron Carbide | Silicon Carbide
Tungsten Carbide | Silicon Nitride | Aluminum Oxide
Hafnium Oxide | Calcium Floride | Zinc Oxide
Yttrium Oxide | Garnet | Spinel
ITO | Alloys | Cerments
Titanium Diboride | Hafnium Carbide | Titanium Carbide
Aluminum Nitride | Titanium Nitride | Cerium Oxide
Titanium Oxide | Zirconium Oxide | Titanium
Nickel | Intermetalics | Pure Metals
Siicides | Silicon | 

## Slide 23: Uses of Sputtering
Depositing thin films for many, many applications
Can deposit metals, semiconductors, and insulators
Large areas
High deposition rates

## Slide 24: Summary
Very versatile technique
Can be used to deposit many types of films
High deposition rate
Can cause damage