## Slide 1: Basic Nanotechnology Processes E SC 212
Notes: <number>

## Slide 2
Unit 2 An Introduction to Uses of Plasma in Processing
Lecture 4
Subtractive Processes and Etching

## Slide 3: Outline
Subtractive processes
Cleaning and etching
Dry cleaning
Dry etching
Notes: <number>

## Slide 4: Subtractive processes
There are two types: (1) those used for cleaning and (2) those used for etching.
The subtractive processes that are based on using plasmas are what is termed dry processes

## Slide 5: Cleaning and Etching---a question of degree

## Slide 6: Cleaning Processes
Cleaning (term used for wet and dry processes). Term used when removing very thin films (residues, “scum”) ---film may be as thin as a few monolayers.
De-scumming (term used for wet and dry processes)
Ashing (term used for dry cleaning based on oxygen plasmas)

## Slide 7: Etching Processes
Wet etching
Dry etching

## Slide 8: Dry Cleaning
Always uses a plasma*
Sputter cleaning (purely physical; e.g., Ar plasma bombardment)
De-scumming and ashing (can vary physical and chemical components; e.g., oxygen plasma)
*Can dry clean with “dry ice”; i.e., solid carbon dioxide pellets.

## Slide 9: Dry Etching
Always uses a plasma
Sputter etching (purely physical)
Reactive ion etching (can vary physical and chemical components)

## Slide 10: Some terminology
Reactive ion etching (RIE) is sometimes called plasma etching
RIE always places the substrate on the cathode
The term “Plasma etching” is always used if the substrate is placed on the anode
So---3 terms to keep straight: dry etching, RIE, and plasma etching

## Slide 11: Dry Etching
Want reproducibility
Want to remove material at rates of 1-1000nm/min.
Want selectivity (only etch what you want etched)
Want to control the etch profile

## Slide 12: Dry Cleaning Example: Barrel Reactor
Chemical removal (etching) dominant
Very useful for removing organic thin layers (residue, scum)
Usually uses oxygen plasma (i.e., ozone radicals) to remove film—this is called ashing

## Slide 13: Dry Cleaning Example: Barrel Reactor

## Slide 14: Dry Cleaning Example: Sputter Cleaning
Purely physical cleaning

## Slide 15
Dry Etching Example: Reactive Ion Etch System
N2
O2
CF4
MFC’s
RF Power Source
Vent/Purge
Cathode with backside cooling
Throttle Valve
Typical Gasses
Mechanical Pump
Turbo Pump
Ion Gauge
Blocking Capacitor
Impedance Match
TC1
TC2
Roughing Valve
Foreline Valve
Public Domain: Image Generated by CNEU Staff for free use
Notes: <number>

## Slide 16
Sputter etching (purely physical)
[Also called ion milling]
Gives anisotropic profile
Not selective
Used when want straight walled profile and selectivity
is not an issue
Used for ion milling in chemical analysis

## Slide 17
RIE:
Playing Physical Bombardment Off Against Chemical Attack
N2
O2
CF4
MFC’s
RF Power Source
Vent/Purge
Cathode with backside cooling
Throttle Valve
Typical Gasses
Mechanical Pump
Turbo Pump
Ion Gauge
Blocking Capacitor
Impedance Match
TC1
TC2
Roughing Valve
Foreline Valve
Public Domain: Image Generated by CNEU Staff for free use
Notes: <number>

## Slide 18: Summary
Plasma cleaning and etching processes produce less waste disposal problems
Effluent control
Widely used in cleaning applications
Widely used in etching applications
RIE gives great versatility in selectivity and etch profile control