## Slide 1
Basic Nanotechnology Processes E SC 212

## Slide 2
Unit 6 Physical Deposition
Lecture 1
Physical Vapor Deposition

## Slide 3: Outline
Introduction
Thermal and e-gun evaporation
Sputtering
Laser ablation

## Slide 4
Introduction
Physical Vapor Deposition (PVD) basically consist of vaporizing a source (target) in order for the transfer to and deposition on a substrate
The processes are preformed under vacuum to prevent contamination issues
PVD allows for very precise atomic layer film growth in thickness ranging from nanometers to millimeters
Normally there is no chemical reaction throughout the deposition process. However, in some methods (e.g. sputtering) new growth-species can be created chemically in the vapor phase and deposited on the substrate
There are many types of physical deposition methods and systems, three of which will be presented here
Notes: <number>

## Slide 5: Outline
Introduction
Thermal and e-gun evaporation
Sputtering
Laser ablation

## Slide 6
Thermal Evaporator
Thermal energy is used to atomize elemental metals. Alloys tend to separate due to melting temperature
Metal selection is based on temperature, with a nominal limit of Platinum
Vacuum level is important to minimize contamination. Generally a base vacuum of 10-5 Torr is desired to prevent water contamination
This originates 'shadowing' phenomena with 3D objects, especially in those regions not directly accessible from the evaporation source substrate surface is generally low (order of kT, i.e. tenths of eV). This affects seriously the morpholgy of the films, often resulting in a porous and little adherent material

## Slide 7
Thermal Evaporator
Vent Valve
Roughing Valve
TC1
TC2
Mechanical Pump
Hi-Vac Valve
Foreline Valve
Ion Gauge
Turbo Pump
DC Power Supply
Substrate
Shutter
Tungsten Filament
CTM
Public Domain: Image Generated by CNEU Staff for free use

## Slide 8
E-Gun Evaporator
E-beam source permits the use of metals that have a higher melting temperature than the evaporator.
Crucible materials are selected to prevent contamination
Crucible selection chart……………….

## Slide 9
Crucible Type | Source Material
Standard Graphite | Antimony
Glassy Coated Graphite | Aluminium, Chromium, Gold, Nickel, Silicon
Alumina (Aluminum Oxide) | Antimony, Copper, Gold, Iron, Nickel, Platinum, Silver
Boron Nitride | Antimony, Aluminium,
Molybdenum | Barium, Copper, Silver
Tantalum | Barium, Copper, Silicon, Titanium Dioxide
Tungsten | Alumina Al2O3, Barium, Gold, Zirconium Oxide
E-Gun Crucible Chart
Cu
Ga
Ag
Public Domain: Image Generated by CNEU Staff for free use

## Slide 10
E-Beam Evaporator
Vent Valve
Roughing Valve
TC1
TC2
Mechanical Pump
Hi-Vac Valve
Foreline Valve
Ion Gauge
Turbo Pump
DC Power Supply
Substrate
Shutter
Tungsten Filament
CTM
Vent Valve
Roughing Valve
TC1
TC2
Foreline Valve
Ion Gauge
Shutter
Substrate
CTM
Crucible
E-gun
Mechanical Pump
Turbo Pump
Hi-Vac Valve
Public Domain: Image Generated by CNEU Staff for free use

## Slide 11
E-Beam Evaporation
Target anode is bombarded with an electron beam given off by a charged tungsten filament under high vacuum
Vacuum level is important to minimize contamination. Generally a base vacuum of 10-5 Torr is desired to prevent water contamination

## Slide 12: Outline
Introduction
Thermal and e-gun evaporation
Sputtering
Laser ablation

## Slide 13
Sputtering
RF power is used to create ions that impinge on the target.
Ion bombardment “grinds down” the target, and the resulting material is deposited on the substrate
The product of ion impingement energy and substrate temperature create a unique morphology of the deposited material
Permits the use of many materials.
  Compounds
  Pure metals
  Mixtures
  Alloys
Notes: <number>

## Slide 14
Sputtering Advantages
Reproducibility
Thickness Control
Stronger Adhesion
Deposits More Materials
  Compounds
  Pure metals
  Mixtures
  Alloys

## Slide 15: Sputtering
Benefits
  Ability to deposit complex compounds while maintaining their stoichiometry
  Capability to deposit high-temperature and refractory metals
  Ability to deposit controlled, uniform films on large substrates and components
  Can be part of a multi-chamber cluster tool
  Can be used as a pre-process substrate cleaning tool

## Slide 16
Sputtering Disadvantage
Higher quality equipment
Higher costs
Lower deposition rates
Organic material integrity is easily degraded by ion bombardment

## Slide 17: Sputtering Diagram
Target
Film growth
Trapped electrons
Target atoms
Substrate
Argon atoms
Public Domain: Image Generated by CNEU Staff for free use
Material being gauged way from target by ions
Plasma

## Slide 18
Film Integrity (Thornton Structure)
Illustrates relationship between
  Coating morphology
  Deposition temperature
  Pressure
Lieberman, M.A., Lichtenberg, A.J. Principles of Plasma Discharges and materials Processing. Wiley. New York. 1994

## Slide 19
Sputtering Tool
Shutter
MFC
Target
Substrate
Throttle Valve
RF Power Supply
Ar2
Mechanical Pump
Turbo Pump
Ion Gauge
Blocking Capacitor
Impedance Match
TC1
TC2
Roughing Valve
Foreline Valve
N2
Vent/Purge
Public Domain: Image Generated by CNEU Staff for free use

## Slide 20: Outline
Introduction
Thermal and e-gun evaporation
Sputtering
Laser ablation

## Slide 21
Laser Ablation
The laser’s wavelength is chosen based on the source material’s absorption characteristics
At low laser flux, the material is heated by the absorbed laser energy and evaporates or sublimates
At high laser flux, the material is typically converted from the source into a plasma the components of a least some of which deposits on the substrate
Pulsed lasers are usually used but it is possible to ablate material with a continuous wave laser beam if the laser intensity is high enough

## Slide 22: Laser Ablation Advantages
Laser ablation can effectively deposit complex films
Laser ablation allows the control of the deposition material when solid and the vapor composition when depositing

## Slide 23: Laser Ablation Disadvantages
Laser ablation systems have a far more complex design, thus high cost associated with them
Finding the best wavelength for evaporation can be difficult
Laser ablation often has a low conversion efficiency