## Slide 1: Basic Nanotechnology Processes E SC 212
Notes: <number>

## Slide 2
Unit 7 Advanced Etch Systems
Lecture 1
The Tools for Plasma Removal Processes

## Slide 3: Outline
Introduction
Etch Systems
Cluster Tools

## Slide 4: Types of Etch Systems
Plasma etch reactors can be grouped into three broad groups:
  Sputter etch – physical process, etches by ion bombardment only, uses a non-reacting gas, it is anisotropic and non-selective
  Chemical etch – chemical process, specially selected gases to react with materials, ion bombardment is negligible, it is isotropic and selective
  Combined etch – ion bombardment complements chemical etch, varies from isotropic to anisotropic with fair selectivity

## Slide 5: Plasma Etch Systems
The term plasma etch systems can refer to any system that uses plasma generation in order to etch a sample
A sample can be biased to improve bombardment’s effect on the etching. This is call Reactive Ion Etching (RIE)
A sample can be left unbiased which takes way much of the effects of bombardment, leaving chemistry as the dominant etching force. This is known as Plasma Etch (PE)

## Slide 6: Etch Systems
Horizontal Plate RIE
Parallel Plate Etch
Microwave Etch
Electron Cyclotron Resonance (ECR) Etch
Hexode RIE
MERIE
Inductively Coupled Plasma (ICP) Etch
Ion Beam Etch
Advanced Strip and Passivation (ASP)

## Slide 7
This is the system that we have studied, and drew a detailed block diagram of an in-depth understanding of the system in E SC 212.
The substrate is placed on a powered cathode
The cathode is generally water-cooled to remove the heat generated by ion bombardment.
Chamber walls usually function as the anode, and may also be temperature controlled.
Horizontal Plate RIE

## Slide 8
Generic Parallel Plate
Plasma Model
Positive Ions
Electrons
Neutral Atoms and Molecules
Molecular Fragments
The majority of the plasma body consists of etch gas molecules, etch by-product molecules and radicals. A typically low density plasma consists of less than 1% charged species.
Public Domain: Image Generated by CNEU Staff for free use

## Slide 9
Simple Diagram of a Horizontal Plate RIE
~
50 Ω Impedance Match
-
Ion drawn to negatively
charged cathode
Public Domain: Image Generated by CNEU Staff for free use

## Slide 10
Typical Horizontal Plate
Reactive Ion Etch System
N2
O2
CF4
MFC’s
13.56 MHz RF Power Source
Vent/Purge
Cathode with backside cooling
Throttle Valve
Typical Gases
Mechanical Pump - C
Turbo Pump - C
Ion Gauge
Blocking Capacitor
Impedance Match
TC1
TC2
Roughing Valve
Foreline Valve
Capacitance Manometer for throttle valve control
Scrubber
Public Domain: Image Generated by CNEU Staff for free use
Notes: <number>

## Slide 11: Simple Diagram of a Parallel Plate (Planar)
~
50 Ω Impedance Match
-
Ion not directed
to substrate
Short around capacitor
Public Domain: Image Generated by CNEU Staff for free use

## Slide 12: Microwave Etch
Plasma is formed in a tuned microwave cavity remotely located from the etch chamber
A UV light source may be used to ignite the plasma
Active gas species flow through a showerhead into the etch chamber
Heaters are generally used to increase the rate for photoresist ashing
This system is often called a down stream asher

## Slide 13: Microwave Etch
N2
O2
He
MFC’s
Vent/Purge
Throttle Valve
Typical Gasses
Mechanical Pump - C
Turbo Pump - C
Ion Gauge
TC1
TC2
Foreline Valve
2.45 GHz Power supply
Tuning Stubs
IR Substrate Heating Lamp
Capacitance Manometer for throttle valve control
Plasma is Generated “Out of Sight” of the substrate.
Roughing Valve
Baffling: blocks line of sight
Public Domain: Image Generated by CNEU Staff for free use

## Slide 14: Electron Cyclotron Resonance Etch (ECR)
ECR uses lower pressures than a conventional parallel plate RIE to be able to achieve cyclotron resonance. Lower pressures offer these advantages:
  Reduced particles
  Reduced residues and contamination
  More inherent anisotropy
The disadvantages are:
  More damage due to increased MFP
  Less chemistry
  Difficult to achieve a uniform plasma greater than 6 inch diameter

## Slide 15: Electron Cyclotron Resonance Etch (ECR)
The design provides a high ion density at low pressure to more effectively transfer energy to the free electrons and at the same time keep them in the plasma region longer.

## Slide 16: Electron Cyclotron Resonance Etch (ECR)
A magnetic field parallel to the direction of the flow causes the free electrons to travel in a spiral path.
The frequency an electron travels around the spiral is determined by the magnetic flux density.
Maximum energy can be transferred when the frequency of electrons spiraling around magnetic flux line (electron cyclotron frequency) is equal to the frequency of applied electric field.

## Slide 17: Electron Cyclotron Resonance Etch (ECR)
Additional magnets may surround the substrate area to aid in plasma uniformity
Relatively high bombardment damage and inability to etch substrates larger than 150mm generally make this technically obsolete.

## Slide 18
Typical ECR Etch System
Vent/Purge
N2
O2
CF4
MFC’s
Cathode with backside cooling
Throttle Valve
Typical Gasses
Mechanical Pump - C
Turbo Pump - C
Ion Gauge
Blocking Capacitor
Impedance Match
TC1
TC2
Roughing Valve
Foreline Valve
2.45 GHz Power supply
Tuning Stubs
Capacitance Manometer for throttle valve control
Magnets
873 Gauss
Steering Magnets
Optional
13.56 MHz RF Power Source
Wave Guide
Wave Guide Window
Scrubber
Public Domain: Image Generated by CNEU Staff for free use
Notes: <number>

## Slide 19: Hexode RIE
This is a batch type RIE.
This system holds substrates vertically on the six-sided cathode.
The chamber walls are grounded to act as the anode.
Let’s discuss the design, and how this would impact the recipe, and material processing…..

## Slide 20: Hexode RIE
N2
O2
He
MFC’s
Vent/Purge
Throttle Valve
Typical Gases
Mechanical Pump - C
TC1
TC2
Roughing Valve
Foreline Valve
Throttle Valve
Turbo Pump - C
Capacitance Manometer for throttle valve control
Impedance Match
13.56 MHz RF Power Source
Substrates
Anode
Hexode (Cathode)
Blocking Capacitor
Public Domain: Image Generated by CNEU Staff for free use

## Slide 21: Hexode RIE
The hexode system is often used for isotropic processes.
Pressure is relatively high, in the 100’s mT range to provide high concentration of chemical reactants
DC bias is minimal due to the high pressure and large cathode

## Slide 22: Magnetically Enhanced RIE (MERIE)
Similar to a Horizontal Plate RIE with the addition of a magnetic field in the plasma chamber to confine the plasma away from the grounded chamber walls
Magnetic field also increases the electron and ion concentration
The magnetic field is produced by electromagnets surrounding the outside of the chamber. Nominal value of the magnet energy is 60 Gauss.
Three phase AC current powers the magnets and creates a rotating magnetic field. This field creates uniformity in the etch.

## Slide 23
Typical MERIE System
N2
O2
CF4
MFC’s
Vent/Purge
Cathode with backside cooling
Throttle Valve
Typical Gases
Mechanical Pump - C
Turbo Pump - C
Ion Gauge
Blocking Capacitor
Impedance Match
TC1
TC2
Roughing Valve
Foreline Valve
13.56 MHz RF Power Source
Capacitance Manometer for throttle valve control
Magnets
~0-75 Gauss
Scrubber
Public Domain: Image Generated by CNEU Staff for free use
Notes: <number>

## Slide 24: Magnetically Enhanced RIE (MERIE)
As in the ECR, the plasma is confined with a magnetic field and the electron and ion densities are increased
The magnetic field is about 1/10th of the power of the ECR (nominally 60 Gauss), so electron confinement is achieved without electron cyclotron resonance.

## Slide 25
Magnetically Enhanced RIE (MERIE)
13.56 MHz
Sample
E
B
Plasma Body
Magnet B
Magnet A
Blocking Capacitor
Impedance Match
E – Electric Field Vector
B – Magnetic Flux Vector
Rotation of these vectors occurs at low frequencies
Magnet A’
Magnet B’
Public Domain: Image Generated by CNEU Staff for free use

## Slide 26
The Effect of a Magnetic Field on the Plasma
The magnetic confinement makes plasma generation more efficient by preventing electron loss to the grounded chamber walls
Plasma is denser, more reactive species and charged particles, thus increasing etch rates
This configuration allows the DC bias to be reduced, leading to less energetic substrate bombardment (‘damage’)

## Slide 27
Electron Motion in a Magnetic Field
E
B
e-
Plasma
Sheath
Cathode
B – Static Field
E – Field Oscillation at 13.56 MHz
Public Domain: Image Generated by CNEU Staff for free use

## Slide 28: Effect of Magnetic Field on DC Bias
Public Domain: Image Generated by CNEU Staff for free use

## Slide 29: Effect of Magnetic Field on DC Bias
More collisions = more ions
Electrons are not lost to the walls, they are contained in the magnetic field.
Grand result is more ion population with less individual ion energy
Recall high individual ion energy leads to damage.
High etch rate leads to faster throughput, and reduced manufacturing cost!

## Slide 30: Inductively Coupled Plasma Etch (ICP)
Inductively Coupled Plasma (ICP) reactor utilizes the electrodes driven by separate power supplies
A sheet of dielectric material separates the electrode holding the substrate from the other electrode
The high density plasma is confined beneath the dielectric material

## Slide 31: Inductively Coupled Plasma Etch (ICP)
13.56 MHz RF or 100KHz Power Source
Blocking Capacitor
Impedance Match
CM for throttle valve control
Cathode
High Density Plasma
Dielectric Plate
Coil
N2
O2
CF4
MFC’s
Vent/Purge
Throttle Valve
Typical Gasses
Mechanical Pump - C
Turbo Pump - C
TC1
TC2
Roughing Valve
Foreline Valve
Impedance Match
13.56 MHz RF Power Source
Scrubber
Public Domain: Image Generated by CNEU Staff for free use

## Slide 32: Ion Beam Etchers (IBE)
Use grid electrodes to focus the electrons into a culminated beam directed toward the substrate
Substrate can be tilted with respect to the ion beam for greater control of the etch profile
Reactors are used most often to etch hard-to-etch materials like some metals and group III-IV compounds

## Slide 33: Ion Beam Etchers (IBE)
Cathode
Anode
Neutral Ar atom
Ionized Ar atom
Gas (Ar) Inlet
Ar Ions with momentum
Ar atoms with momentum
Substrate (Wafer)
Tilted rotating substrate holder
Highly collimated ion beam extraction grid
Neutralization filament
Solenoid Magnetic field which increases ionization
High energy electron stream
Public Domain: Image Generated by CNEU Staff for free use

## Slide 34: ASP Chamber Based on design, what material, what recipe parameters?
Gas Distribution Shield
Gas / RF
Blocking Plate
Vacuum
Channel
Isolation
Plate
Sample
Susceptor
Quartz Lamp
Window
Heating Lamps
Vacuum
Channel
Public Domain: Image Generated by CNEU Staff for free use

## Slide 35: ASP Strip & Passivation Recipe
Recipe Parameters | 200 mm Sample |  | 150 mm Sample | 
 | Step 1 | Step 2 | Step 1 | Step 2
O2 (sccm) |  | 3500 |  | 3000
N2 (sccm) |  | 200 |  | 200
H2O (sccm) | 500 | 300 | 500 | 300
Pressure (T) | 2 | 2 | 2 | 2
Power (W) | 800 | 1400 | 800 | 1400
Temperature (C) | 250 | 250 | 220 | 220
Time (sec) | 60 | 60 | 60 | 60

## Slide 36: Survey of Dry Etch Equipment
Type of Etch Tool | Typical Pressure Range | Descriptions
Reactive Ion Etch (RIE) | Low (10 mT – 150 mT) | Slow etch rate, batch loading required for throughput, less affected by high rate etching damage, asymmetric electrode configuration, negative DC Bias on the cathode, no sputtering of anode, samples are placed on the powered electrode (cathode).
Parallel Plate Etcher (Planar) | Medium (100 mT – 1 T) | Usually single wafer, symmetric configuration, No DC Bias, high rate required for adequate throughout, samples can be placed either on the grounded electrode (Plasma etch Mode) or the powered electrode (Reaction Ion Etch Mode), sputtering of both electrodes can occur, less sample – to – sample variability than in a typical batch system, good individual sample endpoint detection control possible.
Downstream Microwave Etch | High (0.5 – 2 T) | No high energy ion bombardment, reactive species created outside of the etching region, then transported to the etching chamber downstream of the plasma, etching is isotropic without application of bias to the sample, useful for photoresist stripping and other “non-critical” applications.

## Slide 37: Survey of Dry Etch Equipment
Type of Etch Tool | Typical Pressure Range | Descriptions
Hexode RIE | High 100’s mT | Batch process RIE tool. Wafers are mounted on a large six-sided cathode, etch chamber walls acting as the anode. The large cathode distributes the bias, and with the high pressure results in low bombardment. Use often as a photoresist striper.
Magnetically Enhanced Reactive Ion Etch (MERIE) | Low (10 mT – 250 mT) | Magnetic field is responsible for more efficient plasma generation at lower pressures, higher ion and reactant species production, denser plasma, high etch rates, lower bias for less bombardment “damage”, controlled anisotropy.
Electron Cyclotron Resonance (ECR Reactor) | Very Low (< 20 mT) | Magnetron microwave source, magnetic coils, high density plasma, low ion energy, complicated and expensive, technology continues to mature

## Slide 38: Survey of Dry Etch Equipment
Type of Etch Tool | Typical Pressure Range | Descriptions
Inductively Coupled Plasma (ICP) | Low (100’s mT) | ICP is a high density plasma system that uses a separate power supply outside of the etch chamber to control the plasma in the etch chamber. Separate power supplies for plasma generator and sample electrode allow for better control of ion generation.
Ion Beam Etch (IBE) | Low (< 100 mT) | Physical sputter mechanism, high excitation energy, strongly directional (anisotropic), ion density and acceleration voltage can be independently controlled, poor selectivity, low etch rates.
Advanced Strip & Passivation (ASP) Also known as Resist Strip & Passivation (RSP) | High (0.5 - 2 T) | Two stage process. The first step neutralizes caustic chemicals on the sample by flowing in stem. The second stage ashes of the PR with oxygen. High pressure results in shorted mean free path and reduced bombardment.

## Slide 39: Outline
Introduction
Etch Systems
Cluster Tools

## Slide 40: Cluster Tools
Overall trend toward cluster tools in the field
Once loaded into the machine, a substrate remains under vacuum until all the processes are completed
Cluster tools decrease contamination by reducing handling and limiting exposure to the environment
Multiple chambers performing the same etch can be used to increase production throughput. Chambers for non-etching process can also be combined with the etch process chambers.

## Slide 41
Cluster Tool Considerations
Decrease in cycle time (increased throughput)
Reduced handling and exposure to contamination
Cost reduction via sharing robotic handler, software/hardware control system, and vacuum system
Small footprint

## Slide 42: Generic Cluster Tool Configuration
Input
Loadlock
Output
Loadlock
A.S.P.
Etch
Si3N4
Etch
Metal
Etch
Central Robotic
Transfer
Arm
Public Domain: Image Generated by CNEU Staff for free use