## Slide 1
Basic Nanotechnology Processes E SC 212

## Slide 2
Unit 3 An Introduction to Wet Etching
Lecture 1
Wet Etching

## Slide 3: Outline
Introduction & Definitions
Isotropic vs. Anisotropic Etching
Wet Etch Parameters and Limitations
Examples of Etch Profiles
Wet Etch Recipes
Notes: <number>

## Slide 4: Introduction
Definition of etching: The process of selectively removing material by chemical, electrolytic, or physical means.
Chemical = a.k.a. “chemistry,” chemical reactions to convert solid material into soluble products.
Physical = bombardment, as in dry etching

## Slide 5: Introduction
Etching is used to remove material from selected regions:
The regions may be dictated by patterning, such as a photoresist pattern that was previously made with photolithography.
Or the region could be an entire wafer or substrate, as in the wet stripping of an entire blanket layer.
Substrate
Film
PR
Idealized
Case
Substrate
Film
Public Domain: Image Generated by CNEU Staff for free use
Notes: <number>

## Slide 6: Types of Etching
There are two types of etching:
  Wet etching
    Uses liquid chemicals to etch.
    Usually creates a unique isotropic profile.
    Uses only chemistry to etch.
  Dry etching
    Uses plasma to etch.
    Creates a more ideal etch (can create isotropic or anisotropic).
    Uses both chemistry and bombardment to etch.
Notes: <number>

## Slide 7: Introduction
Etch vs. Dissolve
(with respect to wet chemistry)
Etch: a chemical reaction takes place to convert the film into a soluble product.
Dissolve: no chemical reaction is necessary. A good solvent is used to bring the material into solution without undergoing a chemical reaction.
Note: these terms are sometimes used interchangeably in nanofab processes.

## Slide 8: Introduction
Substrate
+
Chemical Reaction
Substrate
Over Time
1
2
3
Soluble Product
Solvent
Polymer Film
Public Domain: Image Generated by CNEU Staff for free use

## Slide 9: Introduction
Cleaning may also be considered as wet a type of wet etching.
In this case, the materials being etched away include unwanted residues (organics, metals, etc.) and particulate matter.
Creates a controlled surface on which to build things (e.g., devices).
Before Cleaning:
Unknown Surface State
After Cleaning:
Controlled Surface

## Slide 10: Example Cleaning Steps
Name | Components | Removes…
Piranha Mixture | Sulfuric Acid, Hydrogen Peroxide | Organics and Metals
SC1 | Ammonium Hydroxide, Hydrogen Peroxide, Water | Particles and Organics
SC2 | Hydrochloric Acid, Hydrogen Peroxide, Water | Metallic Residues
HF or BOE | Hydrofluoric acid, Buffer, Water | Native Oxide (SiO2)
Proper cleaning generally involves many sequential steps and therefore can generate a significant volume of waste:
Piranha  Water  SC1  Water  SC2  Water  HF  Water  Drying

## Slide 11: Figure of Merit: Etch Rate
Etch Rate = thickness etched per time
Usually desired rates are in the 10’s to 100’s of nm/min
If rates are too high, may be difficult to control the process
Too low of rates = long etch times

## Slide 12: Figure of Merit: Selectivity
The ability of an etchant to attack one material and not another.
Wet chemical etching can be very selective, or not very selective depending upon the application.
Represented as a ratio:
Etch Rate of Material 1
Etch Rate of Material 2
Selectivity =
2
1
2
1
2
Layer 2 Protects Layer 1
Layer 2 is Adjacent to Layer 1
versus
Public Domain: Image Generated by CNEU Staff for free use
Notes: <number>

## Slide 13: Aspect Ratio
Public Domain: Image Generated by CNEU Staff for free use
Generally, high aspect ratios are harder to achieve than low ones.
High aspect ratio features are very desirable for many applications.
Due to its isotropic nature, it is difficult to obtain high aspect ratios with wet etching.
Dry etching is usually required to fabricate high aspect ratio features.
D
W
Aspect Ratio =
Notes: <number>

## Slide 14: Outline
Introduction & Definitions
Isotropic vs. Anisotropic Etching
Wet Etch Parameters and Limitations
Examples of Etch Profiles
Wet Etch Recipes
Notes: <number>

## Slide 15: Isotropic vs. Anisotropic
Isotropic: The same in all directions. Material is removed (etched) at the same rate in all directions (lateral and vertical).
Anisotropic: Directions are not equal. Etch rate in vertical direction is different from (greater than) etch rate in lateral direction.
Isotropic
Anisotropic

## Slide 16: Anisotropy
A = 1 -
RL
RV
RL = Lateral Etch Rate
RV = Vertical Etch Rate
RL
RV

## Slide 17: Isotropic
Isotropic = the same in all directions
  RL = RV
  Characteristic wet etch profile.
  Tends to undercut during etching.
  Strictly chemical etching.
  No physical energy component.
Notes: <number>

## Slide 18: Pure Isotropic Etching
Undercutting
A = 1 -
RL
RV
= 1 - 1 = 0
  RL = RV
Public Domain: Image Generated by CNEU Staff for free use
Notes: <number>

## Slide 19: Undercut
Substrate or Etch Stop Layer
(not susceptible to etchant)
Film to be Etched
Before
Etching
No
Undercut
Undercut
Masking Layer
(not susceptible
to etchant)
Public Domain: Image Generated by CNEU Staff for free use

## Slide 20: Undercut Example
10 um
4
3
3
Original Pattern Size = 10 um
Resulting Feature Size = 4 um
Undercut = 3 um each side
Undercut: Lateral etching that occurs under the masking (protecting) layer.
Expressed as a distance (length).
Public Domain: Image Generated by CNEU Staff for free use

## Slide 21: Anisotropic
Anisotropic: directions are not equal
RV  RL, usually RV > RL
  Commonly attained using dry etching.
  Characteristic dry (plasma) etch profile, a function of chemistry and bombardment.
    Chemistry – the chemical reactions that take place on the substrate.
    Bombardment – kinetic ion energy directed at the substrate.
Notes: <number>

## Slide 22: Anisotropic
Anisotropic: directions are not equal
  This type of profile can be achieved by some wet etches, in special cases.
  Wet etchants etch some single crystal materials faster in certain crystallographic directions, resulting in anisotropic etch profiles.
  Example: TMAH and KOH wet etching of silicon with certain crystal orientation.
Notes: <number>

## Slide 23: Pure Anisotropic Etching
A = 1 -
RL
RV
= 1 - 0 = 1
  RL = 0
Public Domain: Image Generated by CNEU Staff for free use

## Slide 24: Anisotropic Silicon Wet Etches
K. Sato et al.rSensors and Actuators 73(1999)131–137
Actual etch profiles of deep grooves etched into a (110) or (100) silicon substrate using TMAH and KOH: (a) 26% TMAH 86oC; (b) 40% KOH 70oC
Notes: <number>

## Slide 25: Anisotropic Etching of Single Crystals
Crystal: a solid material consisting of very well-ordered atoms or molecules with a repeating pattern that extends in all three dimensions.
Directions and faces are not necessarily the same. Crystals may be anisotropic due to the packing arrangement of their constituent atoms or molecules.
Weaker
Bonds
Stronger
Bonds
RL
RV
In this idealized case:
RV > RL
Public Domain: Image Generated by CNEU Staff for free use

## Slide 26: Wet vs. Dry Etching
Generally…
Wet Etching: higher selectivity but lower anisotropy
Dry Etching: lower selectivity but higher anisotropy
But…special conditions can exist which may give increased control over selectivity and/or anisotropy.

## Slide 27: Outline
Introduction & Definitions
Isotropic vs. Anisotropic Etching
Wet Etch Parameters and Limitations
Examples of Etch Profiles
Wet Etch Recipes
Notes: <number>

## Slide 28: 3 Steps of Wet Etching
Movement of etchant species to the surface of the sample
Chemical reaction with the exposed film (to form soluble products)
Movement of the reaction products away from the sample
+
2. Chemical Reaction
1
3
Public Domain: Image Generated by CNEU Staff for free use

## Slide 29: Rate Limiting Step
The slowest step determines (limits) the overall etch rate.
The slowest step in a process is called the rate limiting step.
Rate Limiting Step | Remedy
Transport of etchant to the surface of the film | Agitation, stirring, mixing, sonication
Chemical reaction between etchant and film | Heat
Transport of products away from the surface | Agitation, stirring, mixing, sonication

## Slide 30: Wet Etching Parameters
Parameter | Example | Comments
Concentration | Molarity of acid in etch solution or ratio of components (etchant to buffer) | Changes over time as etchant is depleted and etch products are released into solution
Etch Time | Time of immersion in etch solution | Easy to control with digital timers
Temperature | Temperature of etch bath | Easy to control with heaters and thermostat
Agitation | Stirring or sonication (ultra- vs. mega-sonics) | Can be complicated to control. Depends of geometry of vessel and sample holders
Number of Runs | How many samples are etched at once? After how many batches is the solution changed? | Easy to control but requires bath composition to be analyzed

## Slide 31: Common Problems in Wet Etching
Bubbles can form and prevent good transport to/from the surface.
  Sources of bubbles:
    If the etch products are gases
    Entrainment of bubbles due to vigorous agitation
Resist scumming: incomplete development leaves a thin layer of photoresist that prevents etching.

## Slide 32: Resist Scumming
Scum layer at
bottom of feature
No Scum
Desired Etching
No Etching
Note: the top layer is chosen to be very resistant to etching.
Public Domain: Image Generated by CNEU Staff for free use

## Slide 33: Wet Etching Limitations
Difficult to control
Isotropic in nature (except special cases)
High levels of defects (especially from particulates in the etch solution)
Cannot be used for small features
Practical limit = 2-3 um
Produces large volumes of liquid waste

## Slide 34: Other Etching Considerations
Safety of the operator
Damage to the sample or substrate
Proper disposal of waste
Environmental concerns

## Slide 35: Wet Benches
Wet benches are used to provide a safe and clean working environment.
Generally wet benches are connected to an exhaust fan to draw hazardous fumes away from the user. The clear sash aids in containing fumes and prevents splashing.
Typically the benches provide DI water, sinks, and storage for process chemicals.
Benches are often segregated to prevent unwanted reactions between incompatible materials.
Public Domain: Image Generated by CNEU Staff for free use
Notes: <number>

## Slide 36: Outline
Introduction & Definitions
Isotropic vs. Anisotropic Etching
Wet Etch Parameters and Limitations
Examples of Etch Profiles
Wet Etch Recipes
Notes: <number>

## Slide 37: Isotropic Etch Profiles
Si
SiO2
PR
Si
SiO2
PR
Si
SiO2
Si
SiO2
PR
PR
Si
PR
PR
Si
Public Domain: Image Generated by CNEU Staff for free use

## Slide 38: Sidewall Profiles
Types of etch | Sidewall Profile | Diagram
Wet Etch | Isotropic | 
Dry Etch | Isotropic | 
 | Anisotropic | 
 | Anisotropic—Taper | 
 | Silicon trench | 
Public Domain: Image Generated by CNEU Staff for free use

## Slide 39: Outline
Introduction & Definitions
Isotropic vs. Anisotropic Etching
Wet Etch Parameters and Limitations
Examples of Etch Profiles
Wet Etch Recipes
Notes: <number>

## Slide 40: Wet Etch Selection
Materials have varying etch rates in different etchants.
For a particular target material, some chemistries will etch more efficiently than others.
Increasing temperature will increase an etch rate for a specific chemistry.
Temperature and chemistry are used to control selectivity.
The following information provides general guidelines for etching various materials.
Notes: <number>

## Slide 41: SiO2
Wet Etchant
Hydrofluoric Acid
HF*
Etch Temp
Concentration
500 Å/min
20oC
2M
Buffered Oxide Etch
HF:NH4F:H2O*
1:1:6
20oC
2,000 Å/min
Acetic acid :
Ammonium Fluoride
C2H4O2 : NH4F*
1,000 Å/min
2:1
20oC
*Van Zant, Peter. Microchip Fabrication 4th ed. New York. 2000
+Runyan, W.R., Bean, K.E. Semiconductor Intergrated Circuit Processing Technology. New York. 1994
Relative Etch Rate
Notes: <number>

## Slide 42: Hydrofluoric Acid
HF is the preferred wet etch for SiO2. It can be used in several different forms:
  Undiluted HF (49% by wt)
  Buffered Oxide Etch (BOE): a diluted form of HF that uses ammonium fluoride to buffer the solution.
  NH4F  NH3 + HF
  The buffer maintains the supply of HF and provides control over pH (acidity or basicity)
  Common form: 6 parts buffer solution (40 wt% NH4F in H2O) to 1 part HF (49 wt% in H2O)
Notes: <number>

## Slide 43: Silicon
Wet Etchant
Relative Etch Rate
Etch Temp
Concentration
HF:H2O2:H2O*
1:1:6
20oC
Nitric Acid & HF
HNO3:HF:*
1,000 Å/min
*Van Zant, Peter. Microchip Fabrication 4th ed. New York. 2000
+Runyan, W.R., Bean, K.E. Semiconductor Intergrated Circuit Processing Technology. New York. 1994
5:1 HF
45 Å/min
20oC
Notes: <number>

## Slide 44: Si3N4
Wet Etchant
Relative Etch Rate
Etch Temp
Concentration
Phosphoric Acid
H3PO4
150-180oC
20oC
80 Å/min
80% solution in DI
6:1
*Van Zant, Peter. Microchip Fabrication 4th ed. New York. 2000
+Runyan, W.R., Bean, K.E. Semiconductor Intergrated Circuit Processing Technology. New York. 1994
600 Å/min
Buffered Oxide Etch
NH4F/H2O:HF/H2O*
Phosphoric Acid:
Nitric Acid: Acetic Acid: DI
H3PO4:
HNO3: C2H4O2:H2O*
16:1:1:2
40-50oC
1,000 Å/min
Notes: <number>

## Slide 45: Hot H3PO4 Etching
The bath is kept at 150 – 180oC.
A selective etch for SiNx vs SiO2 (10:1).
Difficult to control the bath, because of the high temperature of the chemicals.
During the removal, some oxynitride is formed. A short HF deglaze may be necessary to remove the oxynitride before further processing.
Notes: <number>

## Slide 46: Metal Etching
Often metals are deposited over SiO2 or Si3N4, since these common dielectrics provide electrical insulation.
When metal etching, it is important to choose a chemistry that will effectively etch the metal, without attacking the underlying material.
Notes: <number>

## Slide 47: Aluminum
Wet Etchant
Relative Etch Rate
Etch Temp
Concentration
Hydrochloric Acid:
Acetic Anhydride
HCl: (CH3CO)2O *
Phosphoric Acid:
Nitric Acid: Acetic Acid: DI
H3PO4:
HNO3: C2H4O2 :H2O *
16:1:1:2
40-50oC
*Kern, Werner. Chemical Etching. Princeton, NJ. 1978
350Å/min
1:1
3,000Å/min
20oC
Notes: <number>

## Slide 48: Aluminum Etch
Phosphoric acid, Nitric acid, Acetic acid
  The most commonly used etch for aluminum.
  Used because it can break through the Al2O3 layer to etch the Al beneath.
HF can also be used to etch Al.
Notes: <number>

## Slide 49: Platinum
Wet Etchant
Relative Etch Rate
Etch Temp
Concentration
Hydrochloric Acid:
Nitric Acid: DI
HCl: HNO3: H2O*
400-500Å/min
3M
Hydrochloric Acid+
HCl
1,000Å/min
20oC
*Kern, Werner. Chemical Etching. Princeton, NJ. 1978
+Runyan, W.R., Bean, K.E. Semiconductor Intergrated Circuit Processing Technology. New York. 1994
7:1:8
85oC
Notes: <number>

## Slide 50: Gold
Wet Etchant
Relative Etch Rate
Etch Temp
Concentration
*Kern, Werner. Chemical Etching. Princeton, NJ. 1978
Potassium Iodide: Iodine
KI: I2: H2O *
Hydrochloric Acid:
Nitric Acid
HCl:HNO3 *
Potassium Ferricyanide:
Potassium Cyanide:
Potassium Hydroxide
K3Fe(CN)6: KCN: KOH *
0.5 – 1 µm/min
25 – 30 µm/min
600 Å/min
20oC
30-40oC
20oC
4:1:10
3:1
4:2:1
Notes: <number>

## Slide 51: Gold Etch
Pre-mixed gold etch is used in our lab
  Gold Etch TFA made by Transene Inc.
  KI : I2 : H2O Solution
Solution is opaque, so removal from solution is required to observe endpoint.
Notes: <number>

## Slide 52: Chromium
Wet Etchant
Etch Rate
Etch Temp
Concentration
*Kern, Werner. Chemical Etching. Princeton, NJ. 1978
+ http://www.transene.com/cr.html#1020
Hydrochloric Acid
HCl *
Ceric Sulfate : Nitric Acid
Ce(SO4)2 : HNO3 *
1,500 Å/min
800 Å/min
Sodium Hydroxide:
Potassium Ferricynide
NaOH: K3Fe(CN)4 *
250-1,000Å/min
1:3
20-40oC
9:1
20oC
20oC
3M
40oC
2400Å/min
Ceric Ammonium Nitrate:
Nitric Acid
H8CeN8O18 : HNO3+
16:6
Notes: <number>

## Slide 53: Chromium Etch
Pre-mix used in lab
  Chromium Etch 1020 made by Transene Inc.
  H8CeN8O18: HNO3 Solution.
Used for etching Cr masks and vacuum-deposited Cr in general.
Photoresist mask can be used.
Doesn’t require depassivation.
Notes: <number>

## Slide 54: Vapor Etching
Uses chemical vapor chemistry to etch rather than liquid chemistry.
Requires heating of chemicals to produce the required vapor and prevent condensation.
Most commonly used vapor is HF.
Advantages:
    Continued vapor replenishment at chemical/material interface.
    More controllable than the standard dip etch procedure.
    Instant etch termination.
Disadvantages:
    Material dependant.
    Generally toxic vapors.
    Must be contained in a closed system.
Notes: <number>