## Slide 1: Basic Nanotechnology Processes E SC 212
Notes: <number>

## Slide 2
Unit 2 An Introduction to Uses of Plasma in Processing
Lecture 3
Plasmas and Deposition

## Slide 3: Outline
Some more additive processes
Plasma enhanced chemical vapor deposition (PECVD)
Plasma Enhanced atomic layer deposition (PEALD)
Applications of PECVD and PEALD.
Notes: <number>

## Slide 4: Additive processes
These are deposition processes--- adding a material
There are many types; e.g., evaporation, sputtering, chemical vapor deposition, plasma enhanced deposition, atomic layer deposition.

## Slide 5: The Additive Processes we will discuss in this lecture (plasma enhanced chemical vapor deposition and plasma enhanced atomic layer deposition) both employ plasmas in the additive chemical process

## Slide 6: Chemical Vapor Deposition (CVD)

## Slide 7: Plasma Enhanced Chemical Vapor Deposition (PECVD)

## Slide 8: Example: In CVD approach a-Si:H is deposited from silane by heat-driven decomposition at 580 C.

## Slide 9: Example: In PECVD approach a-Si:H is deposited from silane by plasma-driven decomposition at ~230C.

## Slide 10: Comparison
Big difference in processing temperatures
Difference in a-Si:H films produced
Difference in hydrogen content
Difference in structure

## Slide 11: PECVD
Ω
~
Impedance Match
AC Power Source
Throttle Valve
Silane
Plasma
Si
Amorphous silicon film growing
H
Gas Inlet #1
Gas Inlet #2
In PECVD, gas molecules (e.g., the precursor Silane) are broken
apart by a plasma. The radicals, ions, and electrons produced result in a chemical reaction on the substrate producing the creation of a film as shown . The substrate is not involved in the chemical reaction in PECVD.
Public Domain: Image Generated by CNEU Staff for free use

## Slide 12: Other PECVD Electrode Configurations are Possible; e.g., the Triode PECVD reactor

## Slide 13: Plasma Enhanced Chemical Vapor Deposition

## Slide 14
PECVD Summary
Lower temperature processes compared to conventional CVD
Film stress can be controlled by high/low frequency mixing techniques
Dry plasma cleaning process with end-point control can reduce need for physical/chemical chamber cleaning (use of load-locks)
Control over stoichiometry via process conditions
Offers a wide range of materials
Conformal step coverage or void-free good step coverage
~ 60nm/min for a-Si:H deposition rate

## Slide 15: Step Coverage

## Slide 16
AKT PECVD System for a-Si TFT-LCD
AKT PECVD System for a-Si TFT-LCD
AKT PECVD System for a-Si TFT-LCD
AKT PECVD System for a-Si TFT-LCD
AKT PECVD System for a-Si TFT-LCD
AKT PECVD System for a-Si TFT-LCD
AKT PECVD System for a-Si TFT-LCD
AKT PECVD System for a-Si TFT-LCD
PECVD tool used to fabricate a-Si:H TFTs for LCD Displays

## Slide 17: Some other Variations: Plasmas with Varying Degrees of Remoteness can be used in PECVD

## Slide 18: Atomic Layer Deposition (ALD) and Plasma Enhanced Atomic Layer Deposition (PEALD)

## Slide 19
The ALD Cycle: Thermal or PE
1. TMA Dose | 2. TMA Purge | 3. O2 Plasma | 4. Short post plasma purge
ALD cycle for Al2O3 deposited using TMA and O2 plasma6. Only step 3 varies between H2O for the thermal process or O2 plasma. Deposition rates vary from ~0.08-0.5nm/min (slow) |  |  | 

## Slide 20: Plasma Enhanced ALD
Some Benefits of Remote Plasma Atomic Layer Deposition
In addition to the benefits of thermal ALD, remote plasma allows for a wider choice of precursor chemistry with enhanced film quality:
Plasma enables low-temperature ALD processes and the remote source maintains low plasma damage
Effective metal chemistry through use of hydrogen plasma rather than complex thermal precursors
Eliminates the need for water as a precursor, reducing purge times between ALD cycles - especially for low temperatures.
Higher quality films through improved removal of impurities, leading to lower resistivity, higher density, etc.
Ability to control stoichiometry
Plasma surface treatment
Plasma cleaning of chamber is possible for some materials

## Slide 21: Applications of PECVD and PEALD.
PECVD—thin film deposition (semiconductors, insulators)
PECVD—nanoparticles (e.g., CNTs)
PEALD—thin film deposition (insulators, some metals)

## Slide 22: Summary
Plasma enhance deposition techniques are widely used and very powerful
Use of plasmas to enhance CVD lowers processing temperatures, gives different variations of a material (more knobs to tune for structure, stoichiometry)
Use of plasmas to enhance ALD expands variety of materials that can be deposited and can enhance through-put.