## Slide 1
Characterization, Testing of Nanotechnology Structures and Materials
E SC 216
Notes: <number>

## Slide 2
Unit 1
Basic Techniques
Lecture 1
Characterizing with Light or Physical Properties

## Slide 3: Outline
Introduction
Optical Microscopes
Profilometry
Ellipsometry
Reflective Spectroscopy
Contact Angle
Film Stress
Sheet Resistance

## Slide 4: Metrology
A group of processes used to determine physical and chemical properties of the nanoproduct during and / or after the fabrication process
Metrology tools are essential to determine the quality of fabrication processes and their resultant materials and devices.

## Slide 5: Yield
The percentage of quality goods produced out of the total group of goods started.
Yield is enhanced by the ability to measure specific characteristics of a substrate in production. It is used to improve upon manufacturing processes if necessary.

## Slide 6: In-situ Characterization
In-situ characterization is a key part of manufacturing today. It provides information about the quality of a device before it is completed.
Improves yield, minimizes waste, monitors processes, provides data for statistical process control.
This process is often non-invasive

## Slide 7: In-situ Characterization
The use of characterization tools in-line to gauge the progress of a manufacturing process.
What can be measured in-situ?
substrate temperature, substrate surface quality, film thickness, growth/etch rates, optical constants, residual gas, etc.

## Slide 8: Residual Gas Analyzer Graph

## Slide 9: Residual Helium at 1.5x10-4 T System Pressure

## Slide 10: Ex-situ Characterization
This is characterization that necessitates taking a product out of the production line for testing and characterization.
Reasons for performing certain characterization techniques ex-situ:
  May be invasive
  May require special sample preparation
  May be low throughput
Whether or not a characterization method is performed in-situ or ex-situ depends on the production process and may vary from process to process.

## Slide 11: Ex-situ Characterization
Some Common Examples:
Structural Characterization Techniques:
  X-ray Diffraction (XRD)
  X-ray Photoelectron Spectroscopy (XPS)
  Auger Electron Spectroscopy (AES)
  Secondary Ion Mass Spectroscopy (SIMS)

## Slide 12: Ex-situ Characterization
Some Common Examples:
Microscopy:
  Transmission Electron Microscopy (TEM)
  Scanning Probe Microscopy (SPM) – AFM and STM
  Scanning Electron Microscopy (SEM)

## Slide 13: Outline
Introduction
Optical Microscopes
Profilometry
Ellipsometry
Reflective Spectroscopy
Contact Angle
Film Stress
Sheet Resistance

## Slide 14: Optical Microscopy
This microscope is the oldest type of microscope and uses visible light and a system of lenses to magnify an image
Due to the size of the wavelength, only low-magnification views and pictures (~1000x) are possible
Some light microscopes can be connected to cameras and computers for simple and cost effective defect detection

## Slide 15: Optical Microscopy
Quirk, M., Serda, J. Semiconductor Manufacturing Technology. Prentice Hall, Upper Saddle River. 2001

## Slide 16: Optical Microscopy
The microscopes in our lab are Leitz Ergolux
Optical Microscopes with video and still camera CCD attachments
Quirk, M., Serda, J. Semiconductor Manufacturing Technlogy. Prentice Hall, Upper Saddle River. 2001

## Slide 17: Optical Microscopy
Specifications | (CNEU) Leitz Ergolux
Stand with coarse/fine adjustment | Bright field / dark field vertical illuminator
12v / 100w lamp housing with socket & bulb | Ergonomic tilting trinocular head
Pair of 10x oculars | 
Motorized 5-Place nosepiece | 5x, 10x, 20x, 50x, 100x BF/DF objectives
6" x 6" X-Y mechanical stage with glass plate | Variable 12v/20w power supply
CCD camera | Photoshop imaging software
Advantages | 
Able to view a variety of samples | Ease of use
Bright field/dark field modes | Ability to capture images with camera
Disadvantages | 
Limited magnification range (5 – 1000x) | Cannot measure feature depth on patterned substrates
Imaging software requires manual adjustment | 

## Slide 18: Outline
Introduction
Optical Microscopes
Profilometry
Ellipsometry
Reflective Spectroscopy
Contact Angle
Film Stress
Sheet Resistance

## Slide 19: Profilometry
Uses a sharp probe and physically contacts the surface to determine the topography of the substrate’s surface.
Used to measure:
  Film thickness
  Surface topography
  Step heights

## Slide 20: Typical Profilometry Scan

## Slide 21: Profilometry
A Tencor 500 Alpha Step Profilometer.

## Slide 22: Veeco Dektak 6

## Slide 23: Outline
Introduction
Optical Microscopes
Profilometry
Ellipsometry
Reflective Spectroscopy
Contact Angle
Film Stress
Sheet Resistance

## Slide 24: Ellipsometry
Ellipsometry is a measurement technique that uses the polarization of laser light to determine film thickness.
Non-destructive and non-contact technique
Very useful method of measuring thickness of materials that are transparent

## Slide 25: Ellipsometry
Use a linearly polarized laser light source that when reflected from the sample becomes elliptically polarized
Polarized light, is light that consists of only light rays traveling in one plane
The shape of the reflected ellipse is measured and film thickness is determined based on given information: angle of reflection, index of refraction, etc.

## Slide 26: Ellipsometry
The ellipsometer in the Nanofab is a variable
Angle Spectroscopic Ellipsometer
(Gaertner Scientific L116C Ellipsometer ).
This refers to the ability of the machine to
vary the angle of the incident light, optimizing
measurements.
Rensselaer Polytechnic Institute. Joel L. Plawsky
Professor of Chemical Engineering

## Slide 27: Ellipsometry
Specifications | Gaertner L115S-8
Laser Light Source | 632.8 nm Helium-Neon (Red)
Incidence Angles | 50º and 70º are used mostly
Beam Diameter | 1.0 x 1.6 mm at 50º and 1.0 x 3.0mm at 70º
Method of Measurement | Four detector-voltages are used to determine state-of-polarization of light of reflected beam. The surface parameters Psi and Delta, and hence film thickness and index of refraction, are calculated.
Film Thickness Range | 0 to 6000 nm
Accuracy | ± 3 Angstroms
Repeatability | ± 1 Angstrom
Refractive Index | ± 0.005
Scanning Modes | Operator selectable; 5 point, 9 point, XY grid or contour map
Scanning Stages | Rotation with translation stages with built in stepping motors
Stepping Motor Drive Source | Two axis, programmable controller; manually or computer controlled
Scanning Increments | 0.01º steps rotation ; 0.01 mm steps to translation

## Slide 28: Refractive Index
A property of transparent substance that addresses how much a light beam bends as it travels through the test media
By measuring two unique angles of incidence, the ellipsometer can determine index of refraction and thickness.
Changes in the index of refraction can represent changes in stoichiometry

## Slide 29: Refractive Index
SiO2
n=1.46
Air
n=1.0

Air
n=1.0
SiO2
n=1.46

Public Domain: Image generated by CNEU Staff for free use

## Slide 30: Outline
Introduction
Optical Microscopes
Profilometry
Ellipsometry
Reflective Spectroscopy
Contact Angle
Film Stress
Sheet Resistance

## Slide 31: Reflection Spectroscopy
Reflection spectroscopy is the analysis of light that has been reflected or scattered from a solid, liquid or gaseous medium.
Commonly used to determine film thickness and index of refraction.
Non-destructive and non-contact.
Simple and relative low cost

## Slide 32: Reflection Spectroscopy
A broadband light source is reflected off the sample at normal incidence.
The intensity of the reflected light is measured over the range of wavelengths.
Computer software utilizes the property of dispersion (the wavelength dependence of a medium’s index of refraction) to determine the film thickness
Light source
Detector

## Slide 33: Reflection Spectroscopy
The reflection spectroscopy equipment in the
Lab is a Nanometrics Nanospec AFT
model 010-180.
Nanometrics Inc

## Slide 34: Reflection Spectroscopy
Advantages and Disadvantages:
Able to analyze multilayer films.
Can measure organic films like photoresist.
Usually requires a reference sample of known composition and thickness

## Slide 35: Outline
Introduction
Optical Microscopes
Profilometry
Ellipsometry
Reflective Spectroscopy
Contact Angle
Film Stress
Sheet Resistance

## Slide 36: Contact Angle
Measures the adhesion of liquids to a surface can be used to calculate surface energies or adhesion tension
Characterizes surface parameters:
  wettability (hydrophobicity), cleanliness, finish, and adhesion
These parameters can be used predict things such as adhesion, corrosion, or biocompatibility

## Slide 37
Contact Angle
Instruments that analyze contact angles are either referred to as:
  Tensiometer
  Contact Angle Analyzer
  Geniometer

## Slide 38: Contact Angle
The tangent angle formed between a liquid drop and its supporting surface is relative to the forces at the liquid/solid or liquid/liquid interface.
This angle is representative of surface bonding energy.
Substrate
Droplet
Contact Angle

## Slide 39
Contact Angle Tools
Cahn Radian DCA Analyzer
Kruss DSA 10 Contact Angle Analyzer
SensaDyne Bubble Tensiometer
http://www.kruss.de/en/products/contact-angle/easydrop.html
http://www.qtech.com.pk/thermo.html
http://www.sensadyne.com/sts.html

## Slide 40
Contact Angle
Case Study: Biological Applications
C. Dahmen, et al. studied Surface functionalization of amorphous silicon and silicon suboxides for biological applications. There findings were published in Thin Solid Films Vol 427, Issues 1-2 , 3 March 2003, Pages 201-207

## Slide 41
Contact Angle
Wetting angle for four different silicon and suboxide
samples as a function of surface treatment with HF.
The longer these four samples were treated with HF the more the surface topography changed and the smaller the contact angle became.
C. Dahmen, et al. Surface functionalization of amorphous silicon and silicon suboxides for biological applications. Thin Solid Films Vol 427, Issues 1-2 , 3 March 2003, Pages 201-207

## Slide 42: Outline
Introduction
Optical Microscopes
Profilometry
Ellipsometry
Reflective Spectroscopy
Contact Angle
Film Stress
Sheet Resistance

## Slide 43: Film Stress
Stress in a layer that may deform the substrate and create uniformity, reliability, or reproducibility concerns
Mechanical stress from the deposited film is transmitted to the underlying substrate and to other layers
Film stress is an important concern of top down manufacturing

## Slide 44: Film Stress
Tools based on a scanning laser-beam or a split-beam laser are commonly used
Changes in the radius of curvature of the substrate resulting from a film’s deposition can be measured and analyzed
Applies to all types of standard thin films
Metals, dielectrics, semiconductors, and polymers

## Slide 45: Film Stress
Film Stress Map
Quirk, M., Serda, J. Semiconductor Manufacturing Technology. Prentice Hall, Upper Saddle River. 2001

## Slide 46: Outline
Introduction
Optical Microscopes
Profilometry
Ellipsometry
Reflective Spectroscopy
Contact Angle
Film Stress
Sheet Resistance

## Slide 47: Sheet Resistance
Resistance: a measure of how much a sample opposes the flow of electrical current
Resistivity: a material property that factors out the dimensions of the sample
Sheet resistance: a measure of resistance of uniform thin films

## Slide 48: Sheet Resistance
Sheet resistivity can be determined by running a current between two points on a square of the layer to be measured
Can be interpreted as the end-to-end resistance of a square sample of a thin film on a substrate
It depends on film resistivity and thickness, but is independent of the size of the square being measured

## Slide 49: Sheet Resistance
To determine resistivity and therefore resistance, the following equation can be used:
ρs = V x 2πs
I
This information can be determined using the 4-point probe. It is a tool that is makes contact
with the substrate. This contact is required to determine the resistivity, but is destructive to
the surface.
The 4-point probe has four equally spaced probes that are in a single line. A known current
(I) is passed between the probes and the potential difference (V) between the two inner
probes is measured. This method avoids contact resistance.
ρ - Sheet resistivity
V – DC voltage across probes
I – DC current through probes
s – spacing between the probes
V
I
R
Voltmeter
Constant Current
Quirk, M., Serda, J. Semiconductor Manufacturing Technology. Prentice Hall, Upper Saddle River. 2001