## Slide 1
Characterization, Testing of Nanotechnology Structures and Materials
E SC 216
Notes: <number>

## Slide 2
Unit 2 Common Spectroscopic Measurements
Lecture 1
Introduction to Photon-Based Spectroscopies

## Slide 3
Reflective Spectroscopy
FTIR
UV-vis Spectrophotometry
Outline

## Slide 4: Reflection Spectroscopy
Reflection spectroscopy is the analysis of light that has been reflected or scattered from a solid, liquid or gaseous medium.
Commonly used to determine film thickness and index of refraction.
Non-destructive and non-contact.
Simple and relative low cost

## Slide 5: Reflection Spectroscopy
A broadband light source is reflected off the sample at normal incidence.
The intensity of the reflected light is measured over the range of wavelengths.
Computer software utilizes the property of dispersion (the wavelength dependence of a medium’s index of refraction) to determine the film thickness
Light source
Detector

## Slide 6: Reflection Spectroscopy
The reflection spectroscopy equipment in the
Lab is a Nanometrics Nanospec AFT
model 010-180.
Nanometrics Inc

## Slide 7: Reflection Spectroscopy
Advantages and Disadvantages:
Able to analyze multilayer films.
Can measure organic films like photoresist.
Usually requires a reference sample of known composition and thickness

## Slide 8: Outline
Reflective Spectroscopy
FTIR
UV-vis Spectrophotometry

## Slide 9: FTIR Spectroscopy
FTIR spectroscopy stands for Fourier Transform Infra Red spectroscopy
This technique measures the infrared light absorbed by a sample.
Fourier math principle is used to correlate the absorbed band of light from the incident laser to a specific bond.
This technique is based on the principle that bonding between atoms is like a spring. The bonds vibrate at frequencies that match those of infrared light. Therefore, a specific portion of the infrared (IR) light spectrum can excite these unique bonds.
Simply stated, different bonds vibrate at different frequencies and will absorb only radiation that matches that frequency.

## Slide 10: FTIR Spectroscopy
This absorption can therefore be used to identify bonds using IR radiation.
Used to detect and identify molecules present on a surface or detect and identify the chemical bonding in a thin film in a non-destructive manner.
Basically, IR light is split into two beams. One of he beams interacts with the sample, and it is destructively added to the known beam. The resultant waveform show the amplitude and specific frequency absorbed. This is a popular testing algorithm.

## Slide 11: FTIR Uses
Confirm the identity of a pure compound by seeing bonding types present
Detect the presence of specific impurities by seeing bonding
Detection of biological entities by seeing bonding
Detection of bonding and therefore chemical composition of thin films.
Used as a non-destructive characterization tool

## Slide 12: FTIR Equipment
The beamsplitter transmits half the beam to the moving mirror and half
to the fixed mirror. They reflect and then recombine in the comparator.
The mirrors move to recombine the beams constructively or destructively.
The detector reads
the beam as a continuous
electrical signal called an
interferogram.
The computer converts
the interferogram into an
absorption graph.
D.J. Paul. University of Cambridge 2006

## Slide 13: Absorbance of IR light by Water
Infrared vibrational modes
D.J. Paul. University of Cambridge 2006

## Slide 14: FTIR Spectra of Isopropanol
Carey, F. Organic Chemistry Online. McGraw Hill 2000

## Slide 15: Absorbance and Transmittance
Transmittance (T) is the percentage of energy that a bond transmits with respect to the amount of energy that is being exposed to.
T = 1- (Fraction of Light Absorbed)
Every bond has its own absorbance and transmittance energy.

## Slide 16: Absorbance, Reflectance and Transmittance
Radiation causes excitation of bonds
Bonds between atoms start to vibrate and move towards and away from each other when excited by the appropriate IR frequency
When excitation occurs energy is taken out of the IR light (absorbed) and converted into a mechanical motion. The IR light that isn’t absorbed gets reflected or transmitted.

## Slide 17: Spectrophotometer
A spectrophotometer is used to measure reflectance and absorbance as a function of the wavelength
The system uses the UV-Visible range of E-M energy
Sample can be liquid, solid or gas
Can be used to measure plasmon frequencies in metal nanoparticles, and the bandgap of a semiconductor
It detects absorption caused by plasmons, electronic transitions, and by molecular excitations whereas FTIR, because of its wavelength range (IR), detects absorption by bond vibration

## Slide 18: Cary 300 UV-Vis Spectrophotometer
Modes | Single/double/dual single beam
UV light source | Deuterium arc lamp
Visible light source | Incandescent bulb
Accessories | Specular reflectance, Diffuse reflectance

## Slide 19: Interaction of Light with Matter
When light strikes a sample, many processes can occur:
Reflection
Scattering
Diffraction
Absorption
Transmission
The interaction depends both on the wavelength of the light and the properties of the sample.
Incident
Reflected
Transmitted
Scattered

## Slide 20: UV-vis Spectrophotometer
Measures difference in intensity between two beams of light:
  One is the reference (or initial) beam and has intensity = I0
  One beam passes through the sample and has intensity = I
  Note: I < I0
The measurements can be performed in at least two different ways:
  Single beam (sequential: ref then sample)
  Double beam (simultaneous: ref and sample)

## Slide 21: Single Beam Measurement
I0
I
Step 1: Measure blank sample and use this as the “baseline” which will be factored out of all future sample measurements. This corrects for absorption by the solvent and other uncontrolled variables.
Step 2: Measure actual sample in the exact same solvent that was used for the baseline.

## Slide 22: Double Beam Measurement
I0
I
Beam
Splitter
In this set-up, the sample and reference are measured simultaneously. This allows for a continuous comparison between the two samples.

## Slide 23: Measurement Considerations
What is measured by the spectrophotometer?
  The intensity of light striking the detector
When done correctly, the difference between the measured intensity and the reference intensity is due only to events occurring in the sample.
Most often, absorption by molecules in the sample reduces the light intensity as the beam passes through the sample.

## Slide 24: Measurement Considerations
However, other processes (in addition to absorption) can be happening during the measurement. For example:
Reflection
Scattering
Fluorescence
Phosphorescence
These decrease the amount of light reaching the detector
These increase the amount of light reaching the detector

## Slide 25: Measurement Considerations
The Cary 300 instrument measures transmitted light and can calculate the amount of light absorbed.
It can also compensate for reflection when proper references (baselines) are used.
Also, with the “integrating sphere” detector, our instrument can directly measure reflected light.
However, our set-up cannot account for scattering or light emission from the sample (e.g., fluorescence). Other instruments can be used to measure these quantities, if needed.

## Slide 26: Terminology
Consider the simple case of a well-behaved homogeneous solution (no scattering or emission processes).
When light passes through the sample it can be reflected (R), absorbed (A), or transmitted (T).
The sum of these 3 processes must account for all of the incident light. If the initial intensity was 100:
100 = R + A + T
With appropriate baseline measurements, reflection is factored out, so the only processes we need to consider are A and T:
100 = A + T

## Slide 27: Terminology
Quantity | Description | Range | Calculation
Transmittance (T) | Ratio of intensities between incident and transmitted light | 0 ≤ T ≤ 1 | 
% Transmittance (%T) | Transmittance expressed as a percentage | 0% ≤ %T ≤ 100% | 
% Absorbed (%A) | The percentage of light absorbed by the sample | 0% ≤ %A ≤ 100% | 
Absorbance (Abs) | A logarithmic quantity that is directly proportional to concentration | Abs ≥ 0 | 
I0
I
Note: I0 is usually baseline corrected to factor out absorption by the solvent and reflection caused by the sample holder

## Slide 28
%A
Abs
10% Transmitted = 90% Absorbed = 1.0 Abs
50 %T = 50 %A = 0.3 Abs

## Slide 29: Absorbance (Abs)
Q: Why use a logarithmic quantity instead of a simple linear one?
A: The absorbance is directly proportional to concentration.
The Beer-Lambert Law
The absorbance of a beam of collimated monochromatic radiation in a homogeneous isotropic medium is proportional to:
the absorption path length (l), which is commonly 1 cm (thickness of the cuvette)
the concentration (c).
The law can be expressed as: Abs = -log(I/I0) =  c l
where the proportionality constant () is called the molar absorption coefficient.
SI units:
Abs = dimensionless
l = cm
c = mol/L
 = L/mol·cm
http://goldbook.iupac.org
Abs
concentration (c)
Slope =  · l

## Slide 30: UV-vis Example
Absorbance = 0.80 at λmax
Abs = -log(T)
0.80 = -log(T)
T = 10-0.80 = 0.16
16% Transmitted
84% Absorbed
Dye solutions used in solar cell experiment