Synthesis of Colloidal Gold Nanoparticles in Solution

Objective:  To synthesize colloidal gold nanoparticles from solution-phase precursors. To use UV-vis spectrophotometry to measure changes in the color of the resulting colloidal suspension as an electrolyte is added.

Background:  In contrast to homogeneous solutions, a colloid is a mixture that contains two discrete phases of material: the dispersed phase and the continuous phase. Colloids can be just about any combination of the three states of matter. Common colloids include milk, inks, smoke, and toothpaste. For example, milk is a complex mixture of solids and lipids dispersed in a continuous water phase. Due to the very small size of suspended particles (about 1 to 200 nm), they are subjected to Brownian motion and do not settle out over time when properly stabilized. Another interesting property of colloidal mixtures is that they scatter light. Homogeneous solutions do not scatter light. This phenomenon can easily be observed by shining a laser (e.g., laser pointer) through a sample of the gold nanoparticles. If the beam path through the sample is visible, the sample is scattering light. If the beam is not visible, the sample is homogeneous insofar as it does not have small particles. In fact, the light scattering properties of colloidal particles can be put to good use in a technique called dynamic light scattering, which uses scattered light to measure the size distribution of colloidal particles in a sample.

A common way of preparing colloidal metal nanoparticles in solution is to reduce a water-soluble metal salt with a chemical reducing agent. In the case of gold nanoparticles, hydrogen tetrachloroaurate (HAuCl4) and sodium citrate serve as the gold source and reducing agent, respectively. Both materials are soluble in water. When combined and heated, reduction of the gold salt occurs and gold nanoparticles form over a period of minutes. As the reaction progresses, the mixture turns from clear to a deep red color which is indicative of colloidal gold nanoparticles.

The nanoparticle colloid appears red in color due to a unique interaction between light and the electrons of the gold nanoparticles. The interaction is called surface plasmon resonance (SPR) and can be envisioned as the collective oscillation of conduction band electrons in resonance with the electric field of the incident light. The wavelength (color) of the SPR depends on many factors, including: the size and shape of the nanoparticles, the solvent in which they are dispersed, and the presence of surface capping agents which were used in the synthesis reaction. The wavelengths of SPR can be measured with a UV-vis spectrophotometer. Your instructor will assist you with the operation of this instrument. Generally, larger particles absorb at slightly longer wavelengths than smaller particles. Also, the more uniform the nanoparticles are (i.e., the narrower the size distribution) the narrower the SPR absorption peak will be. Therefore, UV-vis gives useful information regarding gold nanoparticle samples.

The gold nanoparticles remain suspended in solution because of their small size and due to the citrate ions which coat their surfaces. Citrate ions are negatively charged. When two nanoparticles come close to each other, the negative charges repel each other and push the particles apart. This electrostatic repulsion between neighboring nanoparticles prevents them from aggregating together. However, the addition of ions (e.g., salts) to the nanoparticle suspension can screen the citrate surface charges. Screening has the effect of neutralizing repulsive forces between particles. So, in the presence of screening ions, nanoparticles can approach each other, stick together, and form larger aggregates. This type of behavior results in color changes because aggregates have different optical properties than the originally well-dispersed individual nanoparticles.

Experiment:

- Combine 5 mL of 1mM hydrogen tetrachloroaurate and 50 mL of deionized water in a 100 mL beaker.

- Stir the solution with a magnetic stir bar or glass stirring rod.

- Bring the solution to a gentle boil on a hot plate.

- Add 0.5 mL of 1% sodium citrate to the boiling solution.

- Continue boiling for 10 minutes and observe the color change of the solution.

- After the solution has turned a deep red color, cool it to room temperature. Add fresh DI water to bring the total volume back up to 50 mL.

- Find the peak absorbance of the colloidal suspension with the UV-vis spectrophotometer. Make a graph of absorbance vs. wavelength. Make appropriate dilutions with DI water to keep abs < 1.0.

- Add 2 mL of 1M sodium chloride solution to 10 mL of the colloidal mixture. Stir and allow the resulting mixture to rest for 5 minutes. Record your observations.

- Use the UV-vis spectrophotometer to record absorbance vs. wavelength for the salt-containing solution.

- Use a light source, such as a laser pointer, to observe whether the various solutions used and synthesized in this lab scatter light. Solutions to test: HAuCl4 solution, Au nanoparticle suspension, salt solution. Record your observations.

- If time permits, your instructor may ask you to characterize the nanoparticles via other methods: AFM or FESEM. Be sure to hand in all results and images along with your answers to the questions below.

Reference: A.D. McFarland, C.L. Haynes, C.A. Mirkin, R.P. Van Duyne, H.A. Godwin, J. Chem. Educ. 2004 81 544A.

Questions:

- Include and describe in detail all of your spectrophotometer graphs. What is the wavelength of maximum absorption for each measurement? If you determined the size of your nanoparticles, please report it. (5)

- Explain what happened to the colloid when sodium chloride was added to the solution. Would this happen if a sugar (sucrose) solution was added to the nanoparticles? Why? (5)

- Research and summarize in your own words one application for gold nanoparticles in the life sciences. Why are gold nanoparticles useful for this application? (5)

- Research and summarize in your own words one literature article regarding gold nanoparticles in solid state applications (e.g., solid state electronic devices). What is the advantage of using nanoparticles versus a larger particle or another compound that is not nanoscale? (5)

- Include any AFM or FESEM images obtained from this lab session along with a discussion of each result. (5)