Dye-Sensitized Nanocrystalline Solar Cell

Reference: This handout is designed to work with the “Titanium Dioxide Raspberry Solar Cell” lab which is available from the University of Wisconsin Madison MRSEC. The web address is http://mrsec.wisc.edu/Edetc/nanolab/ Materials for this lab are available from the Institute for Chemical Education: http://ice.chem.wisc.edu/

Objective: The objectives of this lab are: (a) to fabricate a photoelectrochemical cell, (b) to measure the UV-vis absorption spectra of the dyes used to construct the device; (c) to determine the current-voltage and power output characteristics the completed dye-sensitized solar cell.

Background

Fossil fuels are limited, non-renewable resources comprised of biomass that has been deposited over millions of years. Photosynthesis is the main process that creates biomass and its main inputs are water, carbon dioxide, and sunlight. From these ingredients, the cellular machinery of plants builds sugars and other carbohydrates. So, fossil fuels are essentially stored solar energy – energy stored in the form of chemical bonds created by plants that lived millions of years ago. Burning fossil fuels breaks those chemical bonds and releases the stored energy as large amounts of heat. The products of combustion are carbon dioxide and water. If carbon dioxide is released into the atmosphere at a faster rate than it is removed (e.g., by growing plants, by dissolving in sea water, or by other mechanisms), then the concentration of carbon dioxide in the atmosphere will increase over time. Measurements indicate that human activities, such as slash and burn farming and the burning of fossil fuels, have a large effect on the composition of the atmosphere. Rising carbon dioxide levels produce an increased greenhouse effect, which over time may alter the global climate.

Recently, as consumers and governments have become aware of the true costs of burning fossil fuels, there has been renewed interest in solar power generation. During the day, 800-1000 W/m2 of solar power reaches the surface of the earth. Converting even a fraction of this into usable power could dramatically decrease our dependence on non-renewable resources. Therefore, researchers are continuously looking for novel ways of harnessing solar radiation as a clean and abundant energy source. In addition to driving down the cost of making conventional silicon solar cells, scientists are developing new types of photovoltaic devices. These include ones made from polycrystalline and amorphous silicon, other inorganic semiconductors and nanoparticles (e.g., CdSe), and even organic polymers. While the newer constructions are generally less efficient than their silicon counterparts, they hold the promise of being much less expensive to manufacture.

Conventional silicon-based solar cells were developed over forty years ago by Bell Labs. Typically, they employ a p-n junction, as illustrated in Figure I. Absorbed light creates free electrons and holes in the silicon materials. These charge carriers are collected by electrodes attached to the top and bottom surfaces of the semiconductor. The resulting current flow can drive an external load or be stored in a battery for future use.

Conventional solar cells are widely used for electrical power generation. For example, they power satellites and provide electricity in remote locations that cannot be reached by the distribution grid. However, since they must be constructed from extremely pure silicon, conventional devices are often too expensive to be competitive with other forms of electricity generation.

Figure I. Typical silicon solar cell. Current is collected by leads attached to the electrodes.

On the other hand, the relatively low cost of generating electricity from fossil fuels does not reflect the true cost of such activities. The price of electricity generated in coal-fired power plants includes the costs associated with: (i) mining the coal; (ii) buying and operating the equipment needed to burn it to drive generators; and (iii) distributing the electricity over transmission lines to end users. But the price does not accurately reflect unknown costs which may be related to the build-up of carbon dioxide and other pollutants in the atmosphere.

In this experiment, you will construct a dye-sensitized solar cell (DSC), similar to those pioneered by Michael Grätzel at the Swiss Federal Institute of Technology in Lausanne, Switzerland. This particular type of device is actually a photoelectrochemical cell, which means that a photo-induced chemical reaction causes electrons to travel from one substance to another. The device construction and operation are illustrated schematically in the figure below.

Figure II. Structure and operation of a dye-sensitized solar cell.

DSCs consist of a nanostructured semiconductor film coated with organic dye molecules. The nanostructure intimately contacts an electrolyte solution that contains a iodide-triiodide mediator. The film and solution are sandwiched between two electrodes, which allow for electrical connections. Importantly, one electrode (the one coated with nanocrystals) must be transparent, while the other should be coated with a carbon catalyst to facilitate reduction of the iodide-triiodide mediator.

Titanium dioxide (TiO2) is a common white pigment that can be found in everything from paint to paper products. TiO2 exists in several crystal forms including rutile, anatase, and brookite structures. These forms differ in the spatial arrangement of titanium and oxygen atoms in the crystals. Since the anatase form of TiO2 is a semiconductor with a band gap of 3.2 eV, it primarily absorbs UV light rather than visible light. Anthocyanin dyes, on the other hand, are organic molecules that absorb visible light extremely well. This gives them a deep red-purple color. When certain anthocyanin dyes come in contact with TiO2, they can complex with the surface of the nanocrystals. This is depicted in the figure below. The dye molecule acts as a ligand and forms bonds with titanium atoms on the TiO2 surface. In this case, since two bonds are formed between the ligand and metal, the anthocyanin dye molecule is said to chelate the titanium atom. This is a particularly strong type of interaction and it makes the dye very difficult to remove from the surface of the semiconductor. Therefore, chelating anthocyanin molecules cannot be rinsed off by solvent or the electrolyte solution during operation of the solar cell. The close proximity of the dye molecules to the TiO2 surface allows the dye to sensitize the semiconductor: when the dye molecules absorb visible light, they can transfer photo-excited electrons to the TiO2. Hence the name of the device.

Figure III.  Structure of anthocyanin dye attached to TiO2 surface.

The operation of a dye-sensitized solar cell can be described as follows (refer to Figure II):

- Light enters through the transparent conductive electrode. Most of the visible light passes through the TiO2 and strikes the anthocyanin dye molecules which form a complex with the TiO2 surface.

- The dye molecules absorb the light. The energy from the absorbed photons effects electronic transitions in the dye, resulting in a photo-excited (high-energy) state.

- Photo-excited dye molecules inject electrons into the nanocrystalline TiO2. This leaves the dye molecules in a partially oxidized state.

- The iodide-triiodide mediator transfers electrons to oxidized dye molecules. The result is that the dye molecules are reduced back to their original state while the mediator becomes oxidized.

- Electrons that were injected into the TiO2 percolate through the nanocrystalline network and are collected by the top electrode.

- After passing through an external circuit, and possibly being used to drive an electrical load, the electrons reach the carbon coated counter electrode.

- The carbon acts a catalyst to transfer electrons back into the oxidized mediator, which has diffused from the dye-TiO2 surface through the electrolyte solution and to the back electrode. Thus, the mediator is reduced back to its original state and the electrical circuit is completed.

Characterization of Photovoltaic Devices

The following relationships and terminology relate to the characterization of solar cells:

Current density (J) is the current (I) divided by the area (A) of the device.

J(mAcm2)=I(mA)A(cm2)

The open circuit voltage (Voc) is the voltage produced under illumination when no current is flowing (i.e., leads disconnected or under infinite resistance).

The short circuit current (Isc) is the current that flows through an illuminated solar cell when there is no external resistance (i.e., when the electrodes are simply connected or short-circuited). The short-circuit current is the maximum current that a device is able to produce. Under external load, the current will always be less than Isc. Short circuit current can be converted to short circuit current density (Jsc) by dividing by the area of the device.

Power (P) is current multiplied by voltage (V) or power density is current density multiplied by voltage.

P(mW)=I(mA)×V(Volts) or P(mWcm2)=J(mAcm2)×V(Volts)

The maximum power point is the point (Vmpp, Impp) on the I-V curve where the maximum power is produced. This point can also be identified on J-V curves as (Vmpp, Jmpp).

The power conversion efficiency (PCE) is the ratio of power produced by the device (at its maximum power point) to the total amount of power available in the incident light. The PCE can be calculated from device parameters as follows, where Pin = 100 mW/cm2 at 1 sun illumination:

Efficiency=PoutPin=JmppVmppPin=JscVocFFPin

Here, the fill factor (FF) is the ratio of a photovoltaic cell's actual maximum power output to its theoretical power output if both current and voltage were at their maxima, Isc and Voc, respectively. This is a key quantity used to measure cell performance. It is a measure of the “squareness” of the I-V curve.

The figure below contains a typical current density-voltage curve. Terminology introduced above is illustrated.

Figure IV.  Example J-V curve for a solar cell. Current density (blue line) is graphed on the left axis. Power density (red line) is graphed on the right axis.

Note: Be prepared to answer questions about the material in this handout during your pre-lab quiz. (5 points)

Procedure

- Read through the entire procedure before beginning.

- Any down time can be spent obtaining UV-vis absorption spectra of the dye solutions (refer to the attached data sheet).

- Place a small amount of the anthocyanin dye solution in a petri dish and gently immerse the TiO2 coated substrate into the solution with the TiO2 film facing down.

- Soak the TiO2 film for 10 minutes in the dye solution. If white TiO2 can be seen upon viewing the stained film from either side of the glass, then the film should be soaked longer (in 5 minute increments until the TiO2 film is completely stained). When staining is complete, the TiO2 should appear dark purple.

- While the TiO2 film is soaking, prepare the carbon coated electrode according to your TA’s instructions. Use a multimeter (set to measure resistance) to determine which side of the bare glass slide is conductive. The carbon coating should be applied to the conductive side. Do not move on to the next step until the carbon coating has been prepared and you have all other materials ready to go and within easy reach.

- Do not remove the substrate from the staining solution until you are ready to completely finish the assembly process from start to finish. The stained TiO2 film should not be exposed to air for more than one minute. This minimizes degradation of the anthocyanin dye molecules.

- Once complete staining has been confirmed, remove the TiO2 coated substrate from the dye solution and wash the film by immersing it in a petri dish of DI water for several seconds. Remove substrate from the petri dish and carefully rinse it with the DI water gun.

- Immerse the stained substrate in a petri dish of isopropanol for several seconds. Remove it and place the substrate (TiO2 side up) on a tissue.

- Gently blot dry the stained film with a clean tissue.

- The alcohol rinse helps to remove water from the nanocrystalline film. All water must be removed prior to assembling the device and adding the electrolyte solution. Repeat the isopropanol rinse, if necessary, to ensure that the TiO2 film is dry.

- With the TiO2 side facing up, carefully place the carbon coated electrode on top of the TiO2 film so that the carbon side faces the TiO2. Do not slide or rub the films against each other.

- Using minimal force, position the two electrodes such that the carbon coating completely covers the stained TiO2 film. Proper positioning should leave 4-5 mm of each plate exposed on alternate ends of the assembly. The exposed areas will serve as contact points for the test leads (wires with alligator clips).

- Carefully pick up the assembly and place two binder clips on the flush edges to hold the plates together.

- Place one drop of electrolyte solution onto the overhanging surface of one of the plates such that the liquid drop can be drawn between the two plates via capillary action.

- Very gently open and close the binder clips to allow the electrolyte solution to work its way into the device. You should be able to see it wet the stained TiO2 film.

- Add another drop of electrolyte solution to the other end of the device, if needed, and repeat the gentle opening and closing of the binder clips. The entire stained area of the TiO2 film needs to contact the electrolyte solution for the device to function properly.

- Wipe off the exposed areas of the glass contacts with alcohol in order to remove excess electrolyte solution. It is very important that the contact areas be clean and free of electrolyte.

- Apply one small piece of copper foil tape to each of the exposed electrode surfaces. Wrap excess foil around to the back of each glass slide. This ensures good electrical contact between the alligator clips and the electrode surfaces.

- Fasten alligator clips and electrical test leads to the device. Attach the black (-) wire lead to the TiO2 coated glass. Attach the red (+) wire lead to the counter electrode (carbon coated glass).

Student ID#: ____________________

Data Collection and Analysis

Obtain UV-vis absorption spectra (400-800 nm) of the dye solutions used in this lab. Be sure to adjust the concentrations, by diluting with DI water, to keep the maximum absorbance < 1. Record the wavelength (λmax) where the maximum absorption occurs for each dye solution. Also, note down the color of each solution. Export your data to a spreadsheet or else do a “print screen” once you have collected the spectra. Include plots of absorbance vs. wavelength for each solution when you turn in your data sheet and answers to questions. (5 points for UV-vis measurements)

| Dye Solution | λmax (nm) | Color of Solution |
| --- | --- | --- |
| Blackberry Extract |  |  |
| Raspberry Extract |  |  |
| Fruit Juice |  |  |

Record data regarding your solar cell in the spaces provided below.

(5 points for data collection and analysis)

Which dye solution did you use to make your DSC?

Measure the active (stained) area of your device with a ruler: __________________ cm2

Place your solar cell under the light source and allow it to equilibrate for 5 minutes. All of the measurements below should be done while the cell is illuminated.

The maximum current (Isc) and voltage (Voc) outputs can easily be measured by connecting a multimeter to the DSC via wire leads and alligator clips.

The negative electrode is the TiO2 coated glass slide. Attach the black (-) wire lead to the TiO2 coated glass. Attach the red (+) wire lead to the counter electrode (carbon coated glass).

Connect the free ends of the leads to a multimeter set to Volts. This reading, under illumination, is the open circuit voltage and is the maximum voltage that can be produced by the DSC.

Record the Voc here: __________________ Volts

Disconnect the multimeter, set it to mA (current measurement), and reattach it to the DSC leads. Now the multimeter measures the short circuit current of the solar cell.

Record the Isc here: __________________ mA

Divide Isc by the cell area to obtain the short circuit current density (Jsc): __________ mA/cm2

Device I-V Measurements:

This can be done in two ways: (1) If an automated I-V characterization instrument is used, obtain a copy of the data file from the instructor to take with you. The file can be opened with Excel. You can skip to the next page and start analyzing your results. (2) If device data is collected manually, proceed according to the instructions below and record your data points in the table.

Point-by-Point Data Collection:

The instructor will demonstrate how to use a potentiometer and two multimeters to do point-by-point current-voltage measurements with your solar cell. The circuit diagram below illustrates the setup. Essentially, the potentiometer provides a variable resistance (load) to current flowing through the circuit. One multimeter measures the potential developed by the solar cell, while the other measures the amount of current flowing at that voltage. It is important to have the wire leads connected properly. Have your TA examine your setup before collecting data.

Gather point-by-point current and voltage data at various resistance values. Do not move the solar cell or the light source while you are collecting data. Record your data in the Voltage (V) and Raw Current (I) columns below. Record voltage in units of volts and current in units of mA. Note: 1 A = 1000 mA. Increments of 0.05 V will suffice for most of the data collection. However, once the line starts to curve (see example in your lab handout), smaller voltage steps will be required to obtain a smooth curve.

| Voltage (V) (Volts) | Raw Current (I) (mA) |  | Voltage (V) (Volts) | Raw Current (I) (mA) |
| --- | --- | --- | --- | --- |

Transfer the data to a spreadsheet program and make a graph of current density versus voltage. Include the Jsc and Voc data points as well. The Jsc was recorded at short circuit, so its voltage value is zero. Similarly, the Voc value was recorded with no current flowing. Its current density value is zero. Be sure to label all axes appropriately, including units.

Also include a plot of power density versus voltage. (5 points for J-V and P-V graphs)

Determine the maximum point on the J-V curve. If data points were not collected at fine enough intervals, you may have to interpolate between two recorded data points.

Maximum Power Point (mpp): __________________ mW/cm2 @ __________________ Volts

Label the important points on your J-V plot: Jsc, Voc, mpp

Calculate the fill factor (FF) of your DSC:

FF=JmppVmppJscVoc=

Calculate the power conversion efficiency of your solar cell. Unless otherwise noted by your TA, the incident light power density (Pin) can be assumed to be 100 mW/cm2. Be sure to multiply by 100 in order to report the value as a percentage.

Efficiency=PoutPin=JscVocFFPin=

Clean up all materials according to the TA’s instructions. The conductive glass electrodes may be cleaned and recycled for future work.

Requirements (What do I need to turn in?)

- UV-vis spectra of all dye solutions available to you. See sample below. Yours should look very similar to this sample.

- Summary of data collected during the experiment, including:

  - Table containing color and wavelength (nm) of maximum absorption of each dye solution

  - Which dye solution did you use to stain your TiO2 film?

  - Measured area (in cm2) of your device

  - Voc: the open circuit voltage of your device (Volts)

  - Isc: the short circuit current of your device (mA)

  - Jsc: the short circuit current density of your device (mA/cm2)

- Graphs of Jsc vs. Voltage and Power vs. Voltage. See samples below. Jsc should be in units of mA/cm2 and power density should be in units of mW/cm2. You may choose to put both plots on the same graph or on two separate graphs. Make sure all axes are labeled (including units) and that the axes are scaled so that the graphs appear readable. Identify the following important points on your graphs: Jsc, Voc, mpp.

- Calculated device characteristics:

  - mpp: the maximum power point of your device recorded as an (x,y) coordinate where x = voltage of the mpp (Vmpp) and y = the power density at the mpp (Jmpp)

  - FF: the fill factor calculated as shown above. This should be number between 0 and 1.

  - Efficiency: the power conversion efficiency of your device report as a percentage.

- Answers to the questions below.

Questions

- Predict how the voltage and current output would change if two identical solar cells were attached: (a) in parallel; (b) in series. (5 points)

- If solar illumination contains 1000 W/m2 of available power and a solar array is 12% efficient, what area of solar cells is needed to obtain enough electrical power for a typical home (1 kW)? (5 points)

- Suggest a way to increase the power conversion efficiency of dye-sensitized solar cells. (5 points)

Grading

This lab is worth 35 points, distributed as follows:

Pre-Lab Quiz = 5 Points

Lab Activities, Data Collection, and Analysis = 15 Points

Post-Lab Questions = 15 Points

Sample UV-vis Spectra: All solutions are included. Axes properly labeled. Scale is from 400 to 800 nm. Wavelengths of maximum Abs are identified.

Sample Device Plots: Current density is on left (primary) y-axis. Power density is on right (secondary) y-axis. Axes are labeled and scaled to view the area of interest. Important points are clearly identified.