Nickel Nano-wires: Electrodeposition from Solution into a Pre-formed Porous Template

Objectives: To assemble a simple apparatus capable of electrodeposition of nickel nano-wires. To use the apparatus to deposit nickel into a pre-formed porous template. To dissolve away the template and disperse the nano-wires in solution. To characterize the resulting structures with an SEM.

- Training Necessary:  Chemical wet benches and SEM training.

Background:  Electrodeposition is a bottom-up manufacturing technique in which positively charged metal ions in solution are reduced (electrons added) at a surface. Electrodeposition occurs onto an electrode (a conductive surface that can pass electrons into the solution). The metal atoms form a metal film that grows in thickness, as more ions from solution reach the electrode and are reduced. If a template, such as a pre-formed porous pattern covers the electrode, than the growing metal film will fill in the template structure and take on its shape. The growth of nano-wires into column-like pores is illustrated schematically below.

Procedure:  For this lab, you will replicate the procedure which is posted on the University of Wisconsin’s MRSEC website: http://mrsec.wisc.edu/Edetc/nanolab/index.html

Prior to lab, please visit the website and review the procedure that is titled: “Synthesis of Nickel Nanowires: Syringe.” This module is located under the heading of “Intermediate” and is currently the third one in the list. The website contains video clips which demonstrate each step.

Generally, this lab requires the following steps:

1) Coat a nano-porous template with a conductive material, which will serve as the electrode, by sputtering a silver film onto one side of the template.  Use 50mT of Ar for 7.5 min.  The resulting current on the target should be ~45-50 mA.

2) Assemble a water-tight container that holds the template electrode in contact with a nickel sulfate solution. Note, that the nickel atoms in solution are partially oxidized. They exist as Ni2+ ions that are soluble in water.

3) Use a battery to apply a voltage between the template electrode and the counter electrode, which is suspended inside the nickel solution. This causes ions near the electrode surface to be reduced from Ni2+ to Ni0. To accomplish this, electrons must be transferred from the electrode to the Ni2+. Two electrons are required for each atom of nickel that deposits into the template.

4) After 30 minutes of electroplating, the nickel film will have mostly filled the pores of the template. Stop the plating by removing the voltage.

5) Wash the template with concentrated nitric acid for 5 minutes to remove the silver from the template.  Use a pipette to agitate the solution and to dissolve the silver.

6) Rinse the template thoroughly with DI water and then use a 6M sodium hydroxide (NaOH) solution to dissolve the alumina template for 10 min using a stir plate. The NaOH dissolves the alumina template, but not the nickel wires.

7) Nickel is a magnetic material, so the behavior of the nano-wire suspension can be observed in the presence of a magnetic field.  Using a magnet, gather the Ni nanowires and decant the NaOH from the beaker into a waste bottle.

8) Thoroughly rinse the resulting cluster of nanowires with DI water, and then decant the water away.

9)  Suspend the Ni nanowires in isopropanol and transfer to a small container.  The isopropanol is a volatile compound that will evaporate quickly when the Ni nanowires are transferred to a substrate for characterization.  Use a minimal amount (~5mL) of solvent in this step.

10)  Pipette a small amount (~1mL) of the Ni nanowires/IPA solution to a substrate and image with the SEM.  Try to take images at the highest magnification you can.  Be sure to measure at least five wires, for both length and width values.

Questions:

1) How many electrons are required to completely reduce each metal atom in the following compounds: Al2O3, NiCl2, AlCl3, CoSO4, CuSO4, PtO2. (6 pts)

2) Without removing the sample from the electroplating apparatus, how could you monitor the thickness of the metal deposited as a function of time? (2 pts)

3) Read the MSDS sheet for nitric acid that is posted on Angel. (3 pts)

- Nitric acid is a strong oxidizer.  What six materials will nitric acid violently react with?

- Nitric acid is very hazardous.  What are the effects of inhalation?

- Nitric acid itself is not flammable.  What type of fire hazards exist with this chemical?

4) Read the MSDS sheet for sodium hydroxide that is posted on Angel.  (3 pts)

- Name 4 materials that are incompatible with sodium hydroxide?

- What hazardous decomposition products are known to be created by sodium hydroxide?

- What are the target organs effected by exposure to sodium hydroxide?

5) Include your SEM images with measurements. (5pts)

6) What is the function of the nickel wire counter electrode? (2 pts)

7) Does the concentration of nickel ions in solution change as electroplating takes place? Why or why not? (4 pts)

8) Research and summarize one peer reviewed paper on Ni nanowires. (5 pts)