| ESC 214: Patterning for Nanotechnology |  |  |  |
| --- | --- | --- | --- |
| Lab | Lab Title | Topics & Methods | Activity |
| Lab # 1 | Pattern Transfer: Photolithography Training | Training on the contact and proximity lithography tool and spin casting benches. | Students undergo training on spin casting benches and on the theory and operation of positive i-line contact and proximity photolithography. |
| Lab # 2 | Pattern Transfer: Photolithography Practice | Student operation of the photolithography equipment to practice and refine the photolithography process. | Students will practice the techniques learn in the Photolithography Training Lab. The use of reflective spectroscopy an profilometry as methods of characterizing the photolithography process will be explored. |
| Lab # 3 | Template and Mold Fabrication | Student operation of the photolithography equipment to create a template mold. | Students will create a template using negative photolithography on a silicon wafer. Students will then use the template to create a molded structure in PDMS. The mold and molded structure will be examined with profilometer and SEM to study pattern transfer fidelity from template to mold. |
| Lab # 4 | Pattern Transfer: Microcontact Printing | Student mediated pattern transfer using the PDMS stamping technique. | Students will use the PDMS molded structures from the Template and Mold Fabrication lab as a stamp to print a quantum dot functionalized alcanethiol self assembled monolayer (SAM) onto a deposited Au film. Fluorescence microscope will be used to verify pattern transfer. |
| Lab # 5 & #6 | Multiple Level Pattern Transfer: Photolithography | Students carry out of the photolithography equipment for multi level alignment. | Photolithography, microscopy, profilometry, wet, and dry etch skills will be practiced. A second lithography step will be introduced and feature alignment will be practiced by each student. |
| Lab # 7 | E-beam Lithography | Demonstration of the e-beam lithography tool. | Students will be shown e-beam lithography tool and its operation will be discussed. Students will be given e-beam lithography samples and will characterize them using AFM and SEM. FESEM images will also be used and compared to the student SEM images |
| Lab # 8 | Imprinting Lithography | Student operation of stamp embossing equipment for imprinting patterns. | Students will be given embossing stamps made from silicon. Stamps will be used to imprint a pattern into a photo resist. Pattern transfer will be completed using RIE. |