## Slide 1
Metal Nanoparticles

## Slide 2
Metal Nanoparticles: How are they manufactured, what useful properties do they have and what are some examples of products?
Dr. James Delattre NanoHorizons. LLC

## Slide 3: Lecture Outline
History of Synthetic Metal Nanoparticles
Contemporary Definitions
Methods of manufacture
Useful properties
Commercial examples available TODAY

## Slide 4
History of Synthetic
Metal Nanoparticles
“We have only recently come to learn that every structure assumes special properties and a special behavior when its particles are so small that they can no longer be recognized microscopically, while they are still too large to be called molecules.”
from
“World of Neglected Dimensions” 1922.
Carl Wilhelm Wolfgang Ostwald
a.k.a. The Father of Colloidal Chemistry
History of Synthetic
Metal Nanoparticles

## Slide 5: History of Synthetic Metal Nanoparticles
In his studies of the interactions of light and matter, Faraday prepared gold ‘sols’ that were “very minute in their dimensions” and stated that “known phenomena appeared to indicate that a mere variation in the size of its particles gave rise to a variety of resultant colours.”
http://www.goldbulletin.org/assets/file/goldbulletin/downloads/Faraday_4_40.pdf

## Slide 6: History of Synthetic Metal Nanoparticles
Nearly 100 years later Turkevich used electron microscopic investigations to reveal that the ruby-colored colloids made by Faraday’s preparative routes produce particles of gold with average sizes in the 6
± 2 nm range.
http://www.goldbulletin.org/assets/file/goldbulletin/downloads/Faraday_4_40.pdf

## Slide 7: History of Synthetic Metal Nanoparticles
6
Mathew Carey Lea of Philadephia first synthesized colloidal silver in 1880s1
Used widely in photographic film industry throughout 20th century2
Still used today in X-ray films3
1 MC. Lea, “On Allotropic Forms of Silver”, American Journal of Science, 37 (1889) 476
2 D.Whitcomb, "Mathew Carey Lea: Chemist, photographic scientist", Chemical Heritage Newsmagazine, 24(4) (2006/7).
3 DR.Whitcomb, “Nanosilver Particles in Medical X-ray Diagnostic Films”, Eastman Kodak Company (2005). www.particlesociety.org/Whitcomb.pdf

## Slide 8: History of Synthetic Metal Nanoparticles
1969: Carey Lea colloidal silver produced using same methodology as 1889 1
  Size determination and characterisation using electron microscopy (TEM) confirms the size from historical characterisation methods 2
  Confirmed as metallic silver by X-ray diffraction
  Carey Lea colloidal silver
average size 7 - 10 nm
  Confirmation that historical colloidal silver is composed of nanoscale silver particles
= 100 nm
Lea, MC. “Allotropic Forms of Silver.” American Journal of Science, 37 (1889), 476.
Frens, G. & Overbeek, J.Th.G."Carey Lea's colloidal silver", Kolloid-Zeitschrift und Zeitschrift für Polymere, 233(1-2) (1969) pp922-929.

## Slide 9: History of Synthetic Metal Nanoparticles
In 1902, Alfred C. Barnes developed a new antiseptic silver compound, Argyrol, and formed the firm of Barnes & Hille in Philadelphia. The success of this endeavor provided Dr. Barnes with a sizable fortune which was used to amass America’s largest private collection of modern art including works by Picasso, Monet, Matisse, Cezanne and Renoir.

## Slide 10
1942 Argyrol Ad
History of Synthetic Metal Nanoparticles

## Slide 11: Why Synthetic Metal Nanoparticles?
Because naturally occurring metal nanoparticles can form by reduction of terrestrial metal ions by organic acids
http://www.nist.go v/mml/mmsd/silver
-051011.cfm

## Slide 12
History of Synthetic
Metal Nanoparticles
“We have only recently come to learn that every structure assumes special properties and a special behavior when its particles are so small that they can no longer be recognized microscopically, while they are still too large to be called molecules.”
from
“World of Neglected Dimensions” 1922.
Carl Wilhelm Wolfgang Ostwald
a.k.a. The Father of Colloidal Chemistry
Contemporary Definitions of
Metal Nanoparticles

## Slide 13: Contemporary Definitions
Credit: Nanoparticle Synthesis, Prof. Jimmy C. Yu, Department of Chemistry, The Chinese University of Hong Kong

## Slide 14: Contemporary Definitions
More than 24 distinct nano-related definitions have been proposed mostly by standards organizations and government agencies
Report of the ICCR Joint Ad Hoc Working Group on Nanotechnology in Cosmetic Products: Criteria and Methods of Detection ICCR-4, 2010

## Slide 15: Contemporary Definitions:
Cautionary Note on Regulatory Definitions
“First, we have the problem of definitions…Unfortunately, the generally accepted definition of nanotechnology—“the understanding and control of matter at dimensions between approximately 1 and 100 nanometers, where unique phenomena enable novel applications” is what the US National Nanotechnology Initiative uses—is one of expedience, not of science. It serves the purpose of stimulating new research and technology innovation in an exciting new area brilliantly. But it doesn’t clearly define a set of products and processes that have common and specific safety issues; and it was never intended to.
As a result, attempts to apply the generally accepted definition of nanotechnology to material and product safety ends up in a messy mismatch. Materials that are probably benign come under suspicion, while others that we should be worried about potentially slip the net.”
- Prof. Andrew Maynard
Director, University of Michigan Risk Science Center
“Ten things everyone should know about nanotechnology safety” 2020 Science

## Slide 16
Metal Nanoparticles:
Methods of Manufacture

## Slide 17: Manufacturing Methods:
Two General Approaches to Nanoparticle Synthesis
Top ⇨ Down:
  Start with the bulk material and “cut away material” to make the what you want
Bottom ⇨ Up:
  Building what you want by assembling it from building blocks (such as atoms and molecules).
Atom-by-atom, molecule-by- molecule, or cluster-by-cluster
Credit: Nanoparticle Synthesis, Prof. Jimmy C. Yu, Department of Chemistry, The Chinese University of Hong Kong

## Slide 18: Top-Down Approaches
Milling (rarely achieves nanoscale)
Sputter/laser/e-beam deposition
(energy + metal target = NPs)
Pulsed Wire Evaporation
Nanolithography
Pros
  Can be inexpensive
  Scalable
  Pure target = pure NPs (in theory)
Cons
  10 ~ 1000 nm; broad distribution
  Highly varied particle shape or geometry
  Oxidation / impurities
http://www.smith-nephew.com/key-products/advanced-wound-management/acticoat/

## Slide 20: Bottom-Up Approach
Liquid Phase Synthesis from Chemical Precursors
  Chemical Reduction
  Electrochemical Reduction
Vapor Phase Synthesis from Chemical Precursors
  Chemical Vapor Deposition
  Flame Spray Pyrolysis
Self-Assembly of Clusters, Particles
Pros
Good control of size distribution
Shape control in some cases
Cons
  Impurities often intermixed in NPs
  Limits on scalability in some cases

## Slide 21: Manufacturing Methods: Bottom-Up Chemical Reduction
Source: Nanoscale manufacturing curriculum for ATE

## Slide 22: Manufacturing Methods: Bottom-Up Chemical Reduction
Metal Nanoparticle Properties Including:
Composition
Particle size
Crystal structure
Shape
Zeta Potential
Reactivity
Solubility
can be controlled (though not independently) by modifying metal precursors, solvents, reducing agents and polymer stabilizers
G. Z. Cao, Nanostructures & Nanomaterials, London: Imperial College Press,
2004.

## Slide 23: Bottom-Up Approach
Strategies for high dispersion
  thermodynamic equilibrium approach
    supersaturate
    nucleate
    controlled growth
  kinetic approach
    limiting the amount of precursors for the growth
    confining in a limited space
    diffusion limited growth

## Slide 24: Manufacturing Methods: Bottom-Up Flame Spray Pyrolysis
Aerosol-assisted synthesis and assembly of nanoscale building blocks, NE Motl, J. Mater. Chem. A, 2013,1, 5193-5202

## Slide 25: Manufacturing Methods: Bottom-Up Flame Spray Pyrolysis
Pd dispersion and corresponding Pd particle size of flame-made Pd/Al2O3 with different Pd contents and Al2O3surface area.
Flame Synthesis of Supported Platinum Group Metals for Catalysis and Sensors
Reto Strobel, ETH-Zurich, Platinum Metals Review, Jan 2009.

## Slide 26: Surface Functionalization & Self Assembly
Fundamental problem: The thermodynamically stable state of metals, semiconductors, and polymers is bulk material, not colloidal particles. Stable colloidal dispersions require an interfacial stabilizer, which is a chemical that reduces the interfacial free energy between the particle and the solvent and makes short range forces between the particles repulsive.
R. P. Andres, Science (1996)

## Slide 27: Useful properties of metal nanoparticles
and commercial products

## Slide 28: Useful Properties: Photocatalytic “self cleaning” cement
Photocatalytic and Self-Cleaning Properties of Ag-Doped TiO2, Open Materials Science Journal, B. Tryba, 2010.

## Slide 29: Useful Properties: Photocatalytic “self cleaning” cement

## Slide 30: Useful Properties:
Band gap obtained by extrapolating the linear portion of the (αhν)1/2 versus photon energy (eV) curve of (a)
TiO2 and (b) 3% and (c) 7% Ag-doped TiO2 nanoparticles.
Photocatalytic “self cleaning” cement
Silver nanoparticles precipiated on TiO2 will “plasmon sensitize” TiO2 photocatalyst …
lowering the band gap and increasing photocataytic oxidative ‘self cleaning’ efficiency.
K. Gupta, Beilstein J. Nanotechnol. 2013,

## Slide 31: Useful Properties:
Nano-flares: Probes for Transfection and mRNA Detection in Living Cells D.S. Seferos et al., JACS, Dec 2007.
Nanoparticle-based Fluorescent Biodetection
Millipore SmartFlare™ Detection Probes Live Cell RNA Detection

## Slide 32: Useful Properties: Enhanced reactivity – Zero Valent Iron
Zero Valent Iron Nanoparticles are highly reactive and chemically reduce halogenated hydrocarbons and heavy metals. Widely used to remediate contaminated land and ground water.
http://www.lawandenvironment.com/uploads/image/zero%20valent%20iron.jpg

## Slide 33: Useful Properties: Enhanced reactivity – Zero Valent Iron
http://www.regenesis.com/contaminated-site-remediation-products/chemical-oxidation/Regenox/

## Slide 34: Useful Properties:
Electrical Conductivity and Capacitance
Leather Touch Screen Gloves
Capacitive touchscreens work by sensing the conductive properties of your skin.
Revolutionary nanotechnology integrated into the leather of the gloves mimics the conductive properties of the human skin; this makes the gloves touchscreen compatible. The nanotechnology functions independent from the human skin, this enables us to fully insulate the gloves with a layer of soft 100% wool lining.
Leather is coated with a combination of carbon black, silver nanoparticles and a conductive polymer adhesive.
See for example, Conductive leather materials and methods for making the same.
US Patent App 8507102 B1
http://www.mujjo.com/blog/tag/leather-gloves-with-nano-technology/

## Slide 35: Useful Properties: Catalysis – Carbon Dioxide to Methanol Conversion
2 H2 + CO → CH3OH
CO2 + 3 H2 → CH3OH + H2O
CO + H2O → CO2 + H2
Biofuels LPMEOH™ Liquefaction
CO/CO2 to methanol conversion over nanoscale copper catalysts on a zinc oxide support
Nanocatalysis: Synthesis and Applications , ed. Vivek Polshettiwar, Wiley 2013.

## Slide 36: Useful Properties: Catalysis – Carbon Dioxide to Methanol Converstion
Schematic diagram showing how nanostructured copper catalysts can be incorporated into a carbon friendly CO2 to methanol reactor using solar energy to heat the catalyst bed. Electron microscopy (right) shows that the reactive copper catalysts used for this work consist of a variety of particle shapes, such as rods and spheres, dispersed on a zinc oxide support.
http://www.netl.doe.gov/research/coal/energy-systems/gasification/gasifipedia/methanol

## Slide 37: Useful Properties: Antimicrobial Silver for Textiles Applications
Founded by Prof. Fonash in 2002
Manufacturer of nanoscale silver antimicrobial additives and fibers
Surface functionalized particles encapsulated in proprietary polymer stabilizers
Available under the SmartSilver brand

## Slide 38: Useful Properties: Antimicrobial Silver for Textiles Applications
Oxygen in air & water reacts with metallic silver to produce silver ions (Ag+).
  Silver Ions = active antimicrobial agent for all silver based antimicrobial additives.
Silver ions bind to components within bacteria that contain negatively charged groups.
  Including proteins and enzymes necessary for a bacteria to live, grow, and replicate.
Silver ions binds to multiple bacterial components which significantly interferes with the normal functioning of the bacteria; bacteria die
Major Modes of Action for Silver Ions on Bacterial:
(1) Cellular Membrane 1, 2, 3
Causes structural and functional changes in the bacterial membranes leading to their inability to properly function.
(2) Replication 1, 2
Binds to bacterial DNA thus prevent them from multiplying.
(3) Metabolic Pathways 1, 2
Binds to and inactivates metabolic enzymes required by bacteria to live and grow.
Ribosomes
Cytoplasm
DNA
Plasma Membrane
Cell Wall
Enzymes
Bacterial Cell
(1)
(2)
(3)
Jung, Woo Kyung, et al. "Antibacterial Activity and Mechanism of Action of the Silver Ion in Staphylococcus aureus and Escherichia coli." Applied Environ Microbiology (2008): 2171-2178.
Rai, M. K., et al. "Silver nanoparticles: the powerful nanoweapon against multidrug-resistant bacteria." Journal of Applied Micorbiology (2012).
Feng, Q. L., et al. "A mechanistic study of the antibacterial effects of silver ions on Escherichia coli and Staphylococcus aureus." Journal of Biomedical Materials Research (2000): 662-668.

## Slide 39: Useful Properties:
Antimicrobial Silver for Textiles Applications
NanoHorizons’ SmartSilver® in Do No Harm™Medical Scrubs
SmartSilver® particles at 40,000 Magnification Covalently Bonded Within the Cotton Fiber of Medical Scrubs

## Slide 40: Useful Properties: Antimicrobial Silver for Textiles Applications
SmartSilver® additives are delivered as a ready-to-use masterbatch, textile finish or dispersible additive
SmartSilver® particles are nanoscale, so they can be integrated into fine-structured materials such as fibers and foams without impacting processing or mechanical properties
SmartSilver® nanoparticles are small enough to be electrospun into 300 nm fibers without negatively impacting physical properties
Courtesy: Kyoto Institute of Technology and NanoHorizons
500 nm

## Slide 41: Useful Properties:
Nanoscale Silver for Biofilm Resistant Polymers
Almost all current in vitro tests used for evaluating antimicrobial polymers focus exclusively on planktonic (“floating”) cells.
Antimicrobial medical devices are increasing being evaluated for their ability to resist the growth of biofilms
New biofilm resistance test methods developed for antimicrobial catheters allow quantification of both planktonic bacteria and biofilm formation

## Slide 42: Useful Properties: Nanoscale Silver for Biofilm Resistant Polymers
-
1.00
2.00
3.00
4.00
5.00
6.00
7.00
8.00
0
24
96
Log Population
48 72
Contact Time (Hours)
Biofilm Resistance Test – Planktonic
x Inoculum
Control Catheter
Nanoscale Silver Impregnated Catheter
-
1.00
2.00
3.00
4.00
5.00
6.00
7.00
8.00
0
24
96
Log Population
48 72
Contact Time (Hours)
Biofilm Resistance Test - Adhered

## Slide 43: Useful Properties:
http://www2.dupont.com/MCM/en_US/index.html
Conductive Inks for OLEDs and Micro-nanoelectronics
“Dupont nano-silver conductive materials for OLED lighting” March 29, 2014.
Dupont Microcircuit materials introduces a new nano silver conductor ink developments for OLED lighting. Combines high conductivity, and excellent adhesion, low print thickness and smooth sintered surface.
T. Dong, Phys. Chem. Chem. Phys. 11, 6269 (2009)

## Slide 44: Useful Properties: Conductive Inks for OLEDs and Micro-nanoelectronics
Reduced melting temperature of nanoparticles. (Right) Resistivity as a function of curing temperature from Cabot-PEDS.
http://mems.soe.ucsc.edu/printed_materials.html

## Slide 45: Lecture Goals
Introduction to metal nanoparticles
Gain historical perspective
Familiarity with definitions (complex)
Common methods of manufacture
Useful properties of metal nanoparticles
Real world commercial examples

## Slide 46: Thank You!