## Slide 1
Organic Solar Cells

## Slide 2: Outline
Introduction to solar energy conversion
Overview of technology and materials
Processing sequence
Characterization of devices
Trends for the future

## Slide 3
“To give all 10 billion people on the planet the level of energy prosperity we in the developed world are used to, a couple of kilowatt-hours per person, we would need to generate 60 terawatts around the planet – the equivalent of 900 million barrels of oil per day.”
“When we look at a prioritized list of the top 10 problems, with energy at the top, we can see how energy is the key to solving all of the rest of the problems – from water to population.”
Top 10 World Issues
1. Energy
Water
Food
Environment
Poverty
Terrorism and war
Disease
Education
Democracy
Population
-Richard E. Smalley
Nobel Laureate in Chemistry (1996, for the discovery of fullerenes)
MRS Bulletin 2005, 30(6), 412.

## Slide 4
How do we make TW of power?
Fossil Fuels
(non-renewable)
Oil Coal
Natural Gas
Nuclear
(non-renewable)
Solar Wind
Hydroelectric Sustainable Biomass
Renewables

## Slide 5
Solar Radiation
1366 W/m2: Power density of the sunlight striking the Earth’s outer atmosphere.
Known as the solar constant.
1000 W/m2: Power at Earth’s surface on a clear day with the sun directly overhead.
300 W/m2: Approximate amount available on Earth when averaged over 24 hours.
153,000 TW …way more than enough!
atmosphere
surface

## Slide 6
The Solar Spectrum
Infrared (IR) →
UV Visible
H2O
CO2
O3
O2
H2O
H2O
H2O
Source: NREL Renewable Resource Data Center
www.nrel.gov/rredc/
Power Density (W/m2) | 
Solar Constant | 1367
AM 0 | 1353
AM 1.5 D | 768.3
AM 1.5 G | 963.8
AM 1.5 G | 1000

## Slide 7: Using the Sun’s Energy
The basic processes in converting the sun’s
energy into usable electricity are:
Absorption of light
Creation of free charge carriers: e- and h+
Transport and collection of charge
Using the electrical energy
  To power a device (e.g., a calculator)
  To recharge a battery (energy storage)

## Slide 8
Power Conversion Efficiency
Abbreviated PCE
•
Ratio of power density obtained from solar cell to the incident solar power density
The incident light is often produced by a solar simulator and Pin is commonly fixed at 100 mW/cm2
out
Pin
P
PCE 
Solar Cell
P
out
Light
Pin

## Slide 9: Outline
Introduction to solar energy conversion
Overview of technology and materials
Processing sequence
Characterization of devices
Trends for the future

## Slide 10
Solar Cell Technologies
1st Generation: Crystalline silicon
2nd Generation: amorphous silicon, CdTe,
CIGS (thin film technologies)
3rd Generation: organic and dye sensitized
Photos: NREL PIX

## Slide 11
Source: NREL

## Slide 12: First Generation Solar Cell
One p-n junction
Made of very high purity silicon
Can be single crystal or multicrystalline
Principle of Operation
Light absorption creates free charge carriers (electrons and holes)
The p-n junction directs current to flow in only one direction
Charge carriers are collected at the electrodes, which allow current to flow through an external circuit

## Slide 13
First Generation Solar Cell
Top electrode grid
n-type Si
electrons
p-type Si
Metal back electrode
holes
Load
e
e

## Slide 14: First Generation Solar Cell
Advantages Disadvantages
High efficiency
Long lifetime
Expensive materials
Expensive production processes
Rigid structures
Fragile
The aim of organic solar cell research is to overcome the disadvantages by using less expensive materials and less expensive production processes.

## Slide 15
Organic Solar Cells
Light
Hole Transport Layer (40 nm)
Transparent Electrode - 200 nm
Electrode - 100 nm
Active Layer - 200 nm
(Donor/Acceptor Blend)
Load
Organic solar cells are sometimes called plastic solar cells
Each device contains many layers
Glass
The active layer usually contains a mixture of two components: electron donor and electron acceptor
They are made up of materials such as: conductive polymers, small molecule semiconductors

## Slide 16
Organic Solar Cells: Materials
Transparent Electrode Indium Tin Oxide (ITO)
Hole Transport Layer PEDOT:PSS
Active Layer Donor Poly(3-hexylthiophene) (P3HT)
Active Layer Acceptor Fullerene Derivative (PCBM)
Size: 1-2 nm
Self-assembles into nanowire-like domains
Aqueous colloidal suspension with 20-80 nm particles
nm-sized crystallites

## Slide 17
Active Layer Morphology
LD
Donor (White)
Acceptor (Gray)
Hole
Exciton
Electron
Light
Light absorption creates excited species called excitons
Excitons must dissociate at donor-acceptor interface in order to create free charge carriers
Excitons have a limited lifetime and a limited diffusion distance (LD)
LD is on the order of nanometers
Excitons are lost if they do not dissociate into free electrons and holes
Therefore, donor and acceptor materials must be organized into nanoscale domains

## Slide 18: Outline
Introduction to solar energy conversion
Overview of technology and materials
Processing sequence
Characterization of devices
Trends for the future

## Slide 19: Processing of Lab-Scale Devices
Typically, lab-scale organic solar cells are small
in area (< 1 cm2)
Example: If a device is 3 mm x 3 mm, the active area is 9 mm2 or 0.09 cm2
Small devices are easy to fabricate and handle
in the lab.
Many small devices can be made on one
substrate (for optimization experiments).
Active area is defined by where the anode and cathode overlap to make a complete sandwich structure.

## Slide 20
One Device (top view)
Active Area
Anode Contact Pad
Cathode Contact Pad
Example of Device Layout
Example: 4 independent solar
cells on one substrate
1
2
3
4

## Slide 21: Processing Steps
Step | Description
Pattern ITO | Photolithography and Wet Etch
Clean ITO | Oxygen Plasma or UV-Ozone
Cast PEDOT:PSS | Spin Coater
Cure PEDOT:PSS HTL | Oven or Hot Plate
Cast P3HT:PCBM Active Layer | Spin Coater
Thermal Annealing | On 150 C Hot Plate
Evaporate LiF/Al Cathode | Metal Evaporator
Clean Anode Contact | Q-tip and Toluene
I-V Characterization | Solar Simulator

## Slide 22: Processing Steps
Photolithography
Wet Etch (HCl)
Spin and Cure
PEDOT:PSS
Cast and Anneal
P3HT:PCBM
Evaporate
LiF/Al
Clean Anode
Characterize
Light
I-V

## Slide 23
Thermal Annealing P3HT:PCBM
Adv. Funct. Mater. 2005, 15, 1617.

## Slide 24: Outline
Introduction to solar energy conversion
Overview of technology and materials
Processing sequence
Characterization of devices
Trends for the future

## Slide 25
Power Conversion Efficiency
Abbreviated PCE
•
Ratio of power density obtained from solar cell to the incident solar power density
The incident light is often produced by a solar simulator and Pin is commonly fixed at 100 mW/cm2
out
Pin
P
PCE 
Solar Cell
P
out
Light
Pin

## Slide 26
0
1
2
3
4
5
6
-12
-10
-8
-6
-4
-2
0
0
0.1
0.2
0.3
Volts
0.4
0.5
0.6
Power Density (mW/cm2)
J (mA/cm2)
FF = 0.62
PCE = 3.62%
Dark J
2
4
A = 0.09 cm2
Pin = 100 mW/cm2 from solar simulator
Voc = 0.56 V
Jsc = 10.47 mA/cm2
Vmpp = 0.43
Jmpp = 8.41 mA/cm2
Light J
Power
Jsc
Voc
(Vmpp, Jmpp)

## Slide 27
Solar Simulators
• Xenon arc lamp with filters to approximate AM1.5
• Spectral mis-match factors
• Calibration of light intensity (Pin)
• Temperature control of the sample

## Slide 28: Outline
Introduction to solar energy conversion
Overview of technology and materials
Processing sequence
Characterization of devices
Trends for the future

## Slide 29: Alternative Processing Techniques
Roll-to-roll printing
Ink-jet printing
Screen printing
Doctor blading
Vacuum-based deposition

## Slide 30
Controlled Structuring of Small Molecules
Growth of [C60(3 nm)/CuPc(3 nm)]n nanocrystalline donor/acceptor (DA) networks. n = number of bilayers.
Advanced Materials 2007, 19, 4166.

## Slide 31: Organic Solar Cells
Advantages Disadvantages
Materials are amenable to low-cost processing
Polymeric materials can be tailored to meet specifications (e.g., band gap, solubility)
Less efficient (so far) than other technologies
Long term stability needs to be proven
Viewed as cutting edge, but risky, technology

## Slide 32: Conclusions
Solving issues related to energy production, storage, and distribution will take a concerted effort.
Plenty of challenges for all areas of science and technology.
Nanotechnology is poised to make major
contributions to the energy sector.
Organic solar cells show promise for low- cost production ($/Watt).