## Slide 1: Etch overview for microsystems
Etch for Microsystems Learning Module
MEMS Leaf Spring - expands and contracts above the substrate [Graphics courtesy of Khalil Najafi, University of Michigan]

## Slide 2: Unit Overview
This unit is an overview of the wet and dry etch processes, the various thin films that are etched in the construction of microsystems, and the etchants (chemicals) used.

## Slide 3: Objectives
  Match microsystems components to the type of etch required to fabricate each component.
  Identify the differences between wet and dry etch.

## Slide 4: Introduction
For microsystems fabrication, etch is a process that removes select materials from
  the wafer's surface,
  below the wafer's surface, or
  from within the substrate.
A combination of these processes allows for the construction of electronic (on-chip circuitry) and mechanical devices (diaphragm / beam) on the same microchip.
[Graphic courtesy of Khalil Najafi, University of Michigan]

## Slide 5: The Etch Process for Microsystems
Microsystems are 3-D devices consisting of several thin layers of materials.
A layer may be used as
  part of an electronic circuit (insulator or conductor),
  a structural device for a mechanical component,
  a transducer layer for sensors
  a sacrificial layer for devices such as cantilevers, diaphragms or beams.
Layers of Micromachined Scanning Thermal Profilometer [SEM courtesy of Khalil Najafi, University of Michigan]

## Slide 6: Surface Etch
Surface etch for microsystems is the same as for integrated circuits (ICs):
Remove selected regions on one layer (the surface layer) of the wafer to create either a structural pattern or to expose an underlying layer of a different material.
For integrated circuits the underlying layer is for conductive interconnects. For MEMS, the surface layer is patterned with specific shapes for structural components such as cantilevers, mirrors, or probes.
Notes: The etch process normally follows photolithography or deposition during which a protective masking layer is applied to the wafer's surface. The protective masking layer is used to identify the material to be etched and to protect material that is to remain. The figure labeled “Pattern Transfer,” illustrates a mask pattern transferred into a photosensitive layer, shown in red (masking layer), on the wafer's surface (Photolithography Process). During the Etch Process (right), that pattern is transferred into the surface layer, removing exposed areas of the surface layer and leaving areas in the underlying layer open to a subsequent process step.
When building the electronics for a microsystem and for outlining mechanical components, the goal of the etch process is the same as that for building integrated circuits:
Remove selected regions on one layer (the surface layer) of the wafer to create either a structural pattern or to expose an underlying layer of a different material.
For electronic circuits, the underlying layer is now available for conductive interconnects. Connections between different conductive layers can be completed. For mechanical components, the surface layer is now patterned with specific shapes for structural components such as cantilevers, mirrors, or probes. The exposed underlying layer can also allow one to anchor a mechanical structure to it. Mechanical elements can also be conductive as in the case of electrodes or cantilevers.

## Slide 7: Transistor Etching
Etched layers of a transistor
This graphic illustrates five etched layers:
  Silicon substrate
  Insulating oxide or first oxide layer (openings are etched for the doped regions)
  Polysilicon layer (etched to leave just a small portion for the transistor gate)
  Second oxide layer (etched to provide openings for metal contacts to the doped regions and gate)
  Metal layer (etched to form the surface contacts)

## Slide 8: Bulk Etch
Bulk Back-Etch - the silicon substrate has been selectively removed from the wafer's backside.
Bulk Front-Etch - the silicon substrate has been removed from underneath a film on the wafer's surface.
In microsystems fabrication, bulk etch is used to remove material from underneath the mask or from the backside of the wafer (as illustrated in these graphics).
[Graphic courtesy of Khalil Najafi, University of Michigan]

## Slide 9: Release Etch
To release mechanical components, etch is used to remove whatever material is necessary to allow the component to operate according to design.
The component may be required to move up/down or side-to-side, rotate, vibrate, bend or flex. It may need to be suspended over an open area or formed into a free standing component such as a rotating mirror, oscillating piston, or spring (Scanning Electron Microscope (SEM) to right).
Leaf Spring - expands and contracts above the substrate [SEM courtesy of Khalil Najafi, University of Michigan]
Notes: In the construction of a micromechanical part, different components of a structure, such as a rotating gear, are built up layer by layer. Space between parts and layers are created using sacrificial materials which are later removed. This is similar to building scaffolds to hold up a structure during the construction process. At the end of construction, the scaffolding is removed.
In order to release mechanical components, the goal of the etch process changes. The goal is now to remove whatever material is necessary to allow the component to operate according to design, to give it the ability to move freely. The component may be required to move up/down or side-to-side, rotate, vibrate, bend or flex. It may need to be suspended over an open area or formed into a free standing component such as a rotating mirror or oscillating piston.
In such cases, the material underneath the object is removed to "release" the object.

## Slide 10: Release Etch
The material underneath the object is removed to "release" the object.
Specific etch processes remove select material from underneath the structural layer without affecting the structural layer.
The etched material (or sacrificial layer) may be another surface layer (left graphic) or bulk material from within the silicon substrate (right graphic).
Part of a Gear Train built using Surface Micromachining Technology. Sacrificial layers were etched (removed) in order to create released or moveable devices.
[Image courtesy of Sandia National Laboratories, www.mems.sandia.gov]
A bulk etch was used to create an opening under a perforated membrane. This process is called Bulk Micromachining.
Notes: In order to do this, etch processes must be able to remove select material from underneath the structural layer without affecting the structural layer itself. This select material (or sacrificial layer) may be another surface layer (left image) or may be bulk material from within the substrate (right graphic). The left image shows the result of a release etch where a sacrificial layer was removed. The image on the right illustrates a bulk etch in which substrate material is removed to provide a void underneath a structural layer.

## Slide 11: Natural Bridges
Examples of bulk etching in nature include natural bridges and arches. These structures are formed when the material underneath is etched by wind, rain, water, and natural erosion.
What are some other examples of substrate etching (or bulk etching)?
Natural Arch - Coyote Canyon, Utah [Photo courtesy of Bob Willis]

## Slide 12: Another Example
Mt. Rushmore in South Dakota
Mt. Rushmore [Photo courtesy of the National Park Service]

## Slide 13: And Yet Another Example
Mesa Verde National Park in Colorado
Mesa Verde [Photo courtesy of the National Park Service]

## Slide 14: Etched Layers
Each layer of film to be etched for a microsystem has a definitive purpose.
The actual material used for a specific layer is dependent on several factors:
  application or component being constructed
  mechanical and electrical properties needed
  previous and subsequent layers
  etch process
  etchant chemicals

## Slide 15: Etched Layers
Sacrificial Layer - deposited between structural layers for mechanical separation and isolation. Removed during a "release etch" to free the structural layers and allow devices to move. (Silicon dioxide, photoresist, polycrystalline silicon)
Types of Etched Layers
[Graphic courtesy of Khalil Najafi, University of Michigan]
Conductive Layer – conductive paths, vias, and electrodes for electronic circuits / components. (Doped Poly-crystalline, metals and metal alloys)
Insulating Layer – high resistivity to insulate one layer from another. (Silicon nitride, silicon oxide)
Notes: Conductive Layer – A layer used to construct conductive paths, vias, and electrodes for electronic circuits and components. (Doped Poly-crystalline, metals and metal alloys)
Insulating Layer – A high resistivity layer used to insulate one layer from another. (Silicon nitride, silicon oxide)
Sacrificial Layer - A layer deposited between structural layers for mechanical separation and isolation. This layer is removed during a "release etch" to free the structural layers and to allow mechanical devices to move. (Silicon dioxide, photoresist, polycrystalline silicon)

## Slide 16: Etched Layers
Etch Stop Layer – stops the etch when this layer is reached. (Boron-doped silicon, silicon dioxide, silicon nitride)
Etch Mask Layer – defines the pattern to be etched. (photoresist, silicon dioxide, silicon nitride, some metals)
Structural Layer - having mechanical /electrical properties needed for microdevices. (doped polycrystalline silicon, silicon nitride, some metals)
Notes: Structural Layer - A layer having the mechanical and electrical properties needed for the component being constructed. (doped polycrystalline silicon, silicon nitride, some metals such as chrome, gold and aluminum-copper)
Etch Stop Layer – A layer used to define the microstructure thickness by stopping the etch when the etch stop layer is reached. (Boron-doped silicon, silicon dioxide, silicon nitride)
Etch Mask Layer – A layer used to define the pattern to be etched. The mask layer exposes areas to be etched and protects areas that are not to be etched. (photoresist, silicon dioxide, silicon nitride, some metals)

## Slide 17: Etchants
Just as different materials are selected for their functional properties in creating the various layers of a MEMS, different chemicals are selected to etch those materials.
Etchants are chemical compounds which chemically react with the layer to be removed, thereby removing the layer.

## Slide 18: Selecting Etchants
Factors to consider when selecting etchants:
  Capable of etching through the select layer at a rate fast enough to complete the etch in a desired amount of time.
  Etch rate must not be too fast such that it over etches into the next layer.
  Capable of corroding or etching the protective mask layer.
  Should not react with existing layers that are not to be etched.

## Slide 19: Etch Processes
Etching is accomplished with either a wet or dry technique.
Wet etch removes the material through a chemical reaction between a liquid etchant and the layer to be etched.
Dry etch removes the material through a chemical reaction and/or a physical interaction between etchant gasses and the exposed layer.

## Slide 20: Factors Affecting Etch Quality
Etch rate – The rate at which the material is removed from the wafer.
Directional control – Since etch can occur in all directions, it is important to be able to control the direction of the etch. Directional control results in achieving the desired "shape" or etch profile (isotropic, anisotropic or a combination of both)

## Slide 21: Selectivity
Selectivity – Property of the etchant which permits it to selectively etch a specific material at a faster etch rate than other materials on the wafer.
Selectivity is the ratio defined by the following:
Etch rate of material to be etched
Selectivity = ---------------------------------------------------
Etch rate of material NOT to be etched
Based on this formula, which is desired in most cases – a high selectivity or low selectivity?

## Slide 22: Wet Etch
Removes the surface layer or bulk material through a chemical reaction between the material to be removed and a liquid etchant.
Chemistry is designed to be highly selective.
Reliable process using low cost equipment. However, the liquid etchants are usually expensive and quite hazardous.
The Wet Etch Process

## Slide 23: Isotropic Wet Etch
In most wet etch processes, the etch is isotropic.
Isotropic etch is a chemical etch that etches the selected layer in all directions.
Graphic shows the silicon nitride layer being etched vertically as well as horizontally (undercutting the masking layer).
Isotropic Wet Etch

## Slide 24: Isotropic Wet Etch
This characteristic makes it very effective at removing a entire layer of material such as a sacrificial or masking layer.
Graphic shows how structural layers are "released" after the removal of the sacrificial silicon dioxide layers.
This requires a selective wet etch process.
Isotropic Wet Etch

## Slide 25: Anisotropic Etch
Specific wet etches such as silicon and potassium hydroxide (KOH) result in an anisotropic etch profile.
An anisotropic etch is a straight wall edge or an etch that edges along a crystalline plane of the substrate or materials to be etched. (See graphic)

## Slide 26: KOH Anisotropic Etch
In a bulk etch process, KOH is used to etch the silicon substrate along a specific crystalline plane.
In the graphic, notice the sharpness of the angled edge within the silicon substrate. This edge is the result of the high selectivity of KOH (a liquid etchant) and the crystalline structure of silicon.
Bulk Anisotropic Etch
Backside of MTTC Pressure Sensor illustrating anisotropic etch
Notes: Specific wet etches such as potassium hydroxide (KOH) used to etch crystalline silicone, result in an anisotropic etch profile. The KOH etches the silicon along a specific plane. In the figures (Anisotropic Wet Etch), notice the sharpness of the angled edges of the bulk etch. This is due to the high selectivity of KOH (a liquid etchant) and the crystalline structure of silicon. The (111) plane, etches about 400 times slower than the (100) plane. In the photograph of the backside of a pressure sensor, you can see how these planes have been etched forming a well to the silicon nitride membrane (etch stop).

## Slide 27: The Wet Etch Process
The wet etch process consists of three primary processing steps:
  Etch
  Rinse
  Dry

## Slide 28: Step 1: Etch
Wafers to be etched are placed in a wafer carrier or “boat”.
Carrier is lowered into a tank of the etchant solution.
Wafers are left in the solution for a calculated amount of time.
The concentration of the solution and its temperature are constantly monitored, because both directly affect the etch rate. An increase in either parameter increases the etch rate.
Wafer Carrier in Etchant Solution
[Photo courtesy of Bob Willis]

## Slide 29: Step 2: Rinse
Once the etch time expires, the wafer carrier is lifted out of the tank.
It is transferred to another tank, such as a QDR (quick-dump-rinse) where it is rinsed with deionized water.
The picture shows a QDR in the "rinse" cycle.
Quick-Dump-Rinse (QDR) Tank

## Slide 30: Step 3: Dry
After rinse, wafers must be thoroughly dried to prevent problems with future processing.
Typically, the wafers are placed in a Spin Rinse Dryer (SRD) (see photo) where they are rinsed and dried.
The SRD's operation is similar to a centrifuge:
  Carrier is placed in the machine and rotated while being rinsed with deionized (DI) water.
  Water is turned off but the carrier continues to spin at a higher rotational speed.
  Heated nitrogen is introduced, removing any remaining water on the wafer.
SRD [Photo courtesy of Bob Willis]

## Slide 31: Dry Etch Process
In dry etch the wafer is exposed to a gaseous etchant suspended in a RF (radio-frequency) energized plasma.
Collisions between the gas molecules and energized electrons create a "soup" (plasma) made up of electrons, ions and radicals.
Plasma soup consisting of electrons, ions and radicals

## Slide 32: Dry Etch
By design, dry etch methods provide more control over the factors which influence etched results:
  directional control of the etch,
  anisotropic profiles, and
  process parameters (pressure, temperature, gas flow, power).
This control allows for a very selective and specific etch.
Notes: Because gases are the primary etch medium, and are housed in a sealed chamber, human exposure to dangerous solvents and chemicals is limited. However, the equipment is expensive to purchase and maintain. The application of RF power to the process also poses potential health and safety risks and must be carefully controlled..

## Slide 33: Types of Dry Etch
Dry etch is normally used to remove selected areas from the surface layer rather than bulk material of a substrate or a sacrificial layer.
Dry etch can be a chemical etch, physical etch or combination of the two.
Reactive ion etchers (RIE) provide the parameters for both types of etching.

## Slide 34: Physical Etch
Physical etch is very similar to the sputtering deposition process. It is entirely physical. No chemical reaction occurs.
Physical etch is referred to as "ion beam etching", "sputtering" or "ion milling".
Ions bombard the surface of the wafer, causing molecules to sputter off the surface. (See graphic)
Physical Dry Etch
uses ions to sputter molecules from surface

## Slide 35: A Type of Physical Etch
Sand blasting is a type of physical etch process.
A design is placed on a sheet of glass using a strong protective material.
This material stands up to the bombardment of high velocity sand particles.
The unprotected areas of the glass are etched by the sand which removes particles of glass from the surface.
When the desired depth is reached, the blasting stops.
The mask is removed and the design exposed.

## Slide 36: Dry Physical Etch
Wafers are placed on a negatively grounded holder in a vacuum chamber.
  Gas is introduced, chamber pressure reduced (e.g., <50 mTorr) and RF turned on. A plasma is struck (ignited).
  Gas molecules collide with high energy electrons resulting in positive ions.
  Ions are attracted to the negatively-grounded wafer holder.
  Ions accelerate as they move toward the wafer holder.
  Ions hit the wafer, sputtering molecules from the surface.
  Process continues until pattern is etched exposing the underlying layer.
Ion Beam Milling Process (Physical Etch)
[Graphic courtesy of MATEC]

## Slide 37: Dry Chemical Etch
Chemical etching requires plasma energy and a selective gas (the chemical etchant) to etch the wafer's surface layer.
Process begins the same as the physical etch: a plasma is struck and collisions occur between high energy electrons and gas molecules.
However, in dry chemical etch, the radicals formed by the collisions perform the etch rather than the positive ions.
Plasma Collisions
Notes: Radicals are atoms, molecules or ions with unpaired electrons making them highly reactive.

## Slide 38: The Chemical Dry Etch Process
Because radicals generate faster and survive longer than ions, more radicals are available in the plasma.
Radicals travel towards the wafer and are adsorbed by the surface material that is to be etched.
A chemical reaction occurs between the atoms of the material and the radicals. By-products of this reaction desorb from the surface and diffuse into the gas present in the chamber.
The reaction / desorption is the chemical etch.
Chemical Dry Etch Process
Notes: Through the collisions that take place in a plasma, radicals and positive ions are formed. Because radicals generate faster and survive longer than ions, more radicals are available in the plasma. Once produced, the radicals travel towards the wafer where they are adsorbed by the material on the wafer surface. A chemical reaction occurs between the material to be etched and the radicals. By-products of the reaction desorb from the surface and diffuse into the gas present in the chamber. The reaction / desorption is the chemical etch.

## Slide 39: Dry Etch Process Parameters
The two critical parameters in the dry etch process are Pressure and RF power level.
Chemical etching requires high-range pressures and low-range RF power levels.
Physical etching requires low-range pressures and high-range RF power levels.

## Slide 40: Reactive Ion Etch (RIE)
Reactive ion etching (RIE) uses mid-level RF power and mid-range pressure to combine both physical and chemical etching in one process.
The positive ions from the plasma bombard the wafer's surface at the same time that the radicals adsorb to the surface.
RIE process uses both ions and radicals

## Slide 41: RIE
RIE process provides high selectivity ratios.
RIE produces anisotropic profiles on features less than 3 microns wide.
RIE’s ability to capitalize on the advantages of both physical and chemical etching makes it an invaluable tool in the manufacture of microsystems components.

## Slide 42: Deep RIE
A special subclass of RIE is Deep RIE (DRIE).
DRIE is used to etch deep cavities (or trenches) in substrates with relatively high aspect ratios, such as 50:1 (The aspect ratio is the ratio of a cavity's depth to its width).
These cavities can be hundreds of micrometers deep while only a few micrometers wide.

## Slide 43: Deep RIE (DRIE)
The SEM image to the right shows a series of cavities etched using a DRIE process.
Notice that the deeper cavities have the wider openings. This means that on the same wafer with a number of different etch openings, different widths will achieve different depths.
A SEM of cavities etched with DRIE. [SEM courtesy of Khalil Najafi, University of Michigan]

## Slide 44: Deep RIE – Bosch Process
Most systems use "Bosch process":
The Bosch process uses a fluor polymer to passivate the etching of the sidewalls. Passivation protects the sidewalls from being etched but not the horizontal surfaces.
During the entire etching process, the gas mixture switches back and forth between etchant gasses and passivation gasses. This results in a deep, but narrow etch.
DRIE Cavity or Trench [SEM courtesy of Khalil Najafi, University of Michigan]

## Slide 45: DRIE Structures
In addition to creating cavities, DRIE is used to create tall components for microsystems devices which can later be "released" through other etch methods.
SEM image on the right shows a leaf spring created using DRIE. Notice how the spring is attached to a block at one end (front) and to a slider at the opposite end. The entire spring has been released from the substrate allowing it to expand and contract.
Leaf Spring [SEM courtesy of Khalil Najafi, University of Michigan]

## Slide 46: Let’s Review
What types of etch processes were used to form the linkage system in the diagram?

## Slide 47: Summary
In microsystems fabrication etch processes are used to remove bulk material from within a substrate, select material from within thin film layers, and complete layers above and below other thin film layers.
Several different types of etch processes are required:
  Wet etch (isotropic and anisotropic)
  Dry etch (physical, chemical, and both)
  RIE and DRIE
Notes: RIE and DRIE are dry etch processes that use both chemical and physical etch to form the required interleaving shapes. DRIE provides the high aspect ratio cavities required for the advancing technologies of semiconductor, micro and nanosystems.

## Slide 48: Disclaimer
The information contained herein is considered to be true and accurate; however the Southwest Center for Microsystems Education (SCME) makes no guarantees concerning the authenticity of any statement. SCME accepts no liability for the content of this unit, or for the consequences of any actions taken on the basis of the information provided.

## Slide 49: Acknowledgements
Made possible through grants from the National Science Foundation Department of Undergraduate Education #0830384, 0902411, and 1205138.
Any opinions, findings and conclusions or recommendations expressed in this material are those of the authors and creators, and do not necessarily reflect the views of the National Science Foundation.
Southwest Center for Microsystems Education (SCME) NSF ATE Center
© 2012 Regents of the University of New Mexico
Content is protected by the CC Attribution Non-Commercial Share Alike license.
Website: www.scme-nm.org
Revised April 2017