## Slide 1: MTTC Pressure Sensor Process
Process Storyboard
(Process parameters may change due to process improvements.)

## Slide 3: Bare Silicon
Description and Parameters:
Standard 150mm monocrystalline silicon wafer having <100> crystal orientation
Thickness: 675+/- 25 µm
Dopant (An intentional impurity to alter the resistivity): Boron
Resistivity (The resistance to current flow and movement of electrons in the silicon): 20 -cm
Step 1

## Slide 4: Silicon Nitride Deposition
Description and Parameters:
LPCVD deposited
1 µm low stress silicon nitride on both sides of wafer
Step 2

## Slide 5: Photolithography - Coat
Coat Parameters:
Frontside coat - Carefully center wafer on vacuum chuck
Bake wafer for 2 minutes at 110ºC / Cool wafer on metal table to bring wafer back to room temp
Dispense HMDS w/pipette/Spin (HMDS is a primer to allow photoresist to stick to the wafer)
Dispense photoresist (AZ9260) w/pipette/Spin
Backside coat - Carefully align and center wafer on vacuum chuck
Dispense HMDS w/pipette/Spin
Dispense photoresist (AZ9260) w/pipette/Spin
Bake wafer for 2 minutes at 110ºC to cure and remove solvents / Cool wafer on metal table to bring wafer back to room temp
Process Description:
Pattern the backside of the wafer with a photoresist window to expose the silicon.
This step will coat the frontside of the wafer first for protection against scratches, then the backside of the wafer.
3,6
2,8
1,5
4,7
Step 3a

## Slide 6: Backside Photolithography - Expose
1
2
3
Expose Parameters:
Load Mask Into Holding Tray and slide the tray into the Karl Suss alignment system
Load Wafer Into Karl Suss Contact Aligner
Expose wafer to UV light for approximately 300 seconds
Process Description:
Pattern the backside of the wafer with a window to expose the silicon.
The photoresist will become soluble when exposed to the ultraviolet light. The mask contains the window pattern.
Step 3b
Mask Pattern

## Slide 7: Backside Photolithography - Develop
Develop Parameters: Performed at Caustic Wet Bench, USE ACID GEAR
Place exposed wafer in last slot of white Teflon boat (closest to H bar)
Pour develop solution into container and insert boat so entire wafer is submerged
Allow wafers to develop for 10 minutes
Remove boat from develop solution
Place in QDR (Quick Dump Rinse) and Rinse 5X
Place entire boat into SRD (Spin Rinse Dryer) (H-bar in first) until unit reaches 15MΩ
Do a microscopic inspection to check for defects
1
5
6
7
Process Description:
Develops the exposed photoresist to open the windows and expose the silicon for a subsequent etch.
The developer is AZ400K 1:4 potassium based solution
Step 3c

## Slide 8: Backside Etch – RIE
Process Description:
This step uses a plasma etcher to etch the backside silicon nitride layer through the open resist windows, exposing the
underlying monocrystalline silicon wafer. The March Reactive Ion Etcher (RIE) is used for a very highly selective
etch. The RIE uses13.56 MHz (RF) to energize the plasma. The positive ions bombard the wafer’s surface to create
openings in the silicon nitride layer using this dry etching technique.
RIE Parameters:
Place wafer in the RIE for 300 seconds
Turn wafer 180º and etch for another 300 seconds, this insures a uniform etch
Remove wafer
Step 4

## Slide 9: Backside Photoresist Strip
Process Description:
The wafers are placed in a Piranha bath. Piranha is a mixture of H2SO4/ H2O2. This chemical solution aggressively removes photoresist. Extreme care should be taken when using a Piranha solution. The acid will interact with skin very quickly. Be sure to use the appropriate personal protective equipment (PPE) when performing the photoresist strip.
Photoresist Strip Parameters: USE ACID GEAR
Piranha Clean Mixture (Heated to 100ºC)
  4.5 gallons of Sulfuric Acid
  200 mL Hydrogen Peroxide
Always add Peroxide to the Acid!!!!!
Chemicals Used: H2SO4/ H2O2
Process Time: 15 minutes
Step 5

## Slide 10: Frontside Photolithography - Coat
Frontside Coat Parameters:
Carefully align and center wafer on vacuum chuck
Dispense Lift off Resist (LOR) w/ pipette and spin
Bake wafer for 2 minutes at 190ºC.
Cool wafer on metal table to bring wafer back to room temp
Process Description:
The next step in the process is to pattern the frontside of the wafer with the Wheatstone Bridge pattern. In this step, a lift-off resist is applied to create a desired undercutting during the develop process.
5. Align and center wafer on vacuum chuck
6. Dispense photoresist w/pipette and spin
Bake wafer for 5 minutes @ 100° C
Cool wafer on metal table
Chemicals Used: LOR, Photoresist
Step 6a

## Slide 11: Frontside Photolithography - Expose
Mask Pattern
Frontside Expose Description & Parameters:
Load Mask Into Holding Tray and slide the tray into the Karl Suss alignment system
Load Wafer Into Karl Suss Contact Aligner
Align wafer using alignment system
Expose wafer to UV light for 40 seconds
Process Description:
Exposes the Wheatstone Bridge circuit pattern.
3
Step 6b

## Slide 12: Frontside Photolithography - Develop
Process Description: Develops the photoresist & creates the resist undercut.
Frontside Develop Parameters: Performed at Caustic Wet Bench, USE ACID GEAR PPE
Place exposed wafer Teflon boat
Pour develop solution. Insert boat so entire wafer is submerged
Allow wafers to develop for 60 seconds
Remove boat from develop solution and place in QDR (Quick Dump Rinse) and Rinse, repeat this 5 times
Remove and place entire boat into SRD (Spin Rinse Dryer) until unit indicates 15MΩ rinse water resistivity
Perform a microscopic inspection to check for defects
Step 6c

## Slide 13: Metal Deposition
Wheatstone Bridge pattern after metal deposition
Deposition Parameters:
Mount wafers in the vacuum evaporator
Deposit 100 Angstroms of chrome onto the wafer – Process Time: 90 seconds
Deposit 4000 Angstroms of gold over the chrome – Process Time: 5 minutes
Process Description:
A vacuum evaporator deposits chrome and then gold onto the wafer. Chrome is used because it
adheres well to the silicon nitride and the gold adheres well to the chrome. The gold acts as the conductive layer and strain gauge for the resistor bridges in the Wheatstone Bridge.
Step 7

## Slide 14: Metal Liftoff
Process Description:
The wafer is soaked in acetone to dissolve the photoresist causing chrome/gold leads to lift off. The wafer must stay wet or the metal may stick randomly to the wafer surface. LOR will remain.
Liftoff Parameters:
Chemicals Used: Acetone
Process Time: Approximately 30 minutes
Stage 1: Chrome/Gold beginning to liftoff
Stage 2: Wheatstone bridge structures beginning to be revealed
Stage 3: Chrome/Gold liftoff complete
Microscope photo of Wheatstone bridge after liftoff
Step 8

## Slide 15: LOR Strip
Process Description and Parameters
Wafers are now submerged in develop solution to strip the LOR.
Chemicals Used: Develop solution at room temperature
Process Time: Approximately 2 minutes
Step 9

## Slide 16: KOH Etch
1
Good KOH Etch
Bad KOH Etch
Silicon Nitride Membrane
Blown Silicon Nitride Membrane due to over etch
cavity pattern before KOH
cavity during KOH shows silicon nitride pattern
KOH Etch Parameters :
Place wafers in a Teflon boat and place very gently into a 105ºC KOH bath, process for 2 hours
Reduce the temperature to 95ºC and leave for 90 minutes
Reduce the temperature to 80ºC for approximately 45 minutes, or until etch is complete
Place wafers in QDR then blow dry with nitrogen
Chemicals Used: KOH, IPA, nitrogen
Step 10
Process Description and Parameters : Performed at a Wet Bench, USE ACID GEAR PPE
Wafers are now submerged in a heated Potassium Hydroxide (KOH) bath. The silicon nitride acts as a hard mask and the exposed silicon etches anisotropically following the crystal planes. At the end of the etch, the wafers will be fragile since the bulk of the Si is removed.

## Slide 17: Testing and Probing
Process Description and Parameters
Wafers are now placed on a probing station. A power supply is used to apply a voltage, causing the membrane
to deflect.
Pressure Sensor wafer on probing station
Probe on the Wheatstone Bridge
Probing station and power supply
Final Product

## Slide 18: Acknowledgements
Copyright © by the Southwest Center for Microsystems Education and The Regents of the University of New Mexico.
Southwest Center for Microsystems Education (SCME)
800 Bradbury SE, Suite 235
Albuquerque, NM 87106-4346
Phone: 505-272-7150
Website: www.scme-nm.org
The work presented was funded in part by the National Science Foundation Advanced Technology Education program, Department of Undergraduate Education grants: 0830384, 0402651, 1205138.