## Slide 1: MEMS Micromachining overview
MEMS Micromachining Overview Learning Module
Surface
LIGA
Bulk
Microcantilever Chemical Sensor Array
[Image courtesy of Dr. Christoph Gerber, Institute of Physics, University of Basel]
Microgears
[Image Courtesy of Sandia National Laboratories, SUMMiT V process]
Graphic of High Aspect Ratio Rods
Notes: Welcome to MEMS Micromachining Overview presented by the Southwest Center for Microsystems Education. This presentation is a brief overview of three widely used MEMS Micromachining Processes: Bulk Micromachining, Surface Micromachining and LIGA. As a reminder, MEMS means microelectromechanical systems. These three micromachining processes enable the fabrication of micro-size components such as gears and geartrains, cantilevers, probes, needles, accelerometers, micro-sized rods and springs.

## Slide 2: Surface Micromachining
Microgears
[Image Courtesy of Sandia National Laboratories, SUMMiT V process]
Notes: Let’s start with surface micromachining. Surface micromachining uses thin film layers deposited on the surface of a substrate to construct structural components for MEMS. This scanning electron microscope image, also called a SEM, shows microgears that were fabricated using surface micromachining.
These gears are very thin, approximately 2-3 micrometers in thickness, but can be hundreds of micrometers (or microns) across. To give you a sense of scale, the gear teeth in this image are each smaller than the diameter of a human red blood cell which is 8-10 microns in diameter.

## Slide 3: Surface Micromachining
Structural and sacrificial layers are deposited, patterned and etched on top of a substrate.
Structures have low aspect ratios (short and wide)
Based on CMOS manufacturing. (CMOS – complementary metal oxide semiconductor)
[Image courtesy of Sandia National Laboratories]
Notes: Surface Micromachining builds components and structures using processes called deposition, photolithography and etch. These are the same processes and techniques used to make computer chips.
However, in surface micromachining, the fabricated structures move matter using devices such as gears and cantilevers rather than move electrons through electronic circuitry.
In order to move matter and to create moveable structures, spaces must be incorporated between moving components during the fabrication process. This is done with what is called, sacrificial layers. A sacrificial layer is placed between two structural layers to provide the spacer. Once the device is completed, the sacrificial layer is removed, releasing the part so it can move.

## Slide 4: Surface Micromachining
  A micromechanical part is formed out of deposited thin films
  At least one structural and at least one sacrificial layer.
Microcantilever Fabrication
A sacrificial layer is deposited, patterned and etched
A structural layer which is deposited, patterned, and etched
Sacrificial layer is removed.
[Image courtesy of Southwest Research Institute. Copyright SwRI]
Notes: Surface micromachining is based on the deposition and etching of alternating structural and sacrificial layers on top of a substrate. This graphic illustrate the fabrication of a single microcantilever. A sacrificial layer is deposited on the substrate followed by a photoresist layer. A pattern is transferred into the photoresist layer, then this pattern is etched into the sacrificial layer. The remaining resist is removed and a structural layer is deposited on top of the etch sacrificial layer. The cycle of photolithography and etch is repeated after which, the sacrificial layer is removed, leaving a suspended cantilever beam that is free to move.
Depending on the device being fabricated, several cycles of deposition, photolithography and etch may be required.

## Slide 5: Surface Micromachining
What is a sacrificial layer?
  Needed when building complicated components, such as moveable parts.
  Used to separate layers as the structure is being constructed
  Dissolved away at the end to free the structural layers.
[Image Courtesy of Sandia National Laboratories]
Notes: Complicated components, such as a movable gear transmission with chain drives, are possible because of the use of sacrificial layers. A sacrificial layer in surface micromachining is analogous to scaffolding used for bridge construction.
The lower image shows a cross-sectional view of a keystone bridge. This type of bridge is built by first constructing a scaffold made of wood. Pre-Cut stones are then placed on top of the scaffold. The final stone at the apex, called the keystone, is placed. Once this the keystone is in place, the scaffold is removed and the bridge doesn’t fall down (hopefully). The scaffold is temporary; its only purpose is to provide support during the construction process, then removed or sacrificed. This is the same principle used in building micro-size structures using sacrificial layers.

## Slide 6: Deposition
First layer could be an insulator, isolator or sacrificial layer.
First layer is “usually” a thermally grown silicon dioxide layer (SiO2 or oxide).
Other thin films and subsequent layers of oxide and other thin films use a type of Chemical Vapor Deposition (CVD).
Notes: Looking at the process steps in more detail…starting at the substrate, a thin film is deposited or, in the case of silicon dioxide, is grown on the surface of the substrate. This first layer can be an isolator, insulator, hard mask, or sacrificial layer. For many surface micromachined components, this first layer is silicon dioxide which is used for insulators and sacrificial layers.
Silicon dioxide or oxide is grown in a thermal oxidation furnace using heat and either oxygen gas or water vapor. Growing silicon dioxide on a silicon substrate is analogous to rust growing on iron forming iron oxide. Heat and humidity results in a faster growing iron oxide and more rust. The same goes for silicon dioxide. The rate of oxide growth and the thickness of the oxide can be controlled with temperature and humidity levels.
Subsequent layers of oxide as well as other thin films such as silicon nitride or polysilicon are deposited using a process called chemical vapor deposition. Metals and metal allows are deposited using a physical deposition process such as sputtering or evaporation.

## Slide 7: Photolithography
Pattern (Photolithography)
  Coat wafer with photoresist
  Align and expose resist to a pattern
  Develop resist
  Bake to harden resist
[Image Courtesy of MATEC]
Notes: After a thin film is deposited, photolithography is used to transfer a pattern from a reticle or mask to the thin film layer. Photolithography uses a thin coat of light sensitive material called “photoresist or resist”. The resist is exposed using ultraviolet or UV light by shining the UV through the mask to the resist. The graphic illustrates this process. Once the resist is exposed, it is developed then baked to harden the remaining resist.

## Slide 8: Photolithography and Etch
Pattern from mask is transferred into photoresist.
Photoresist pattern is transferred into underlying layer using an etch process.
After etch, the photoresist is removed.
Notes: After the photolithography process we move to etch. In the etch process the pattern in the resist is transferred to the underlying layer using either a wet etch or dry etch process. After etch, the resist is removed or stripped leaving the patterned material layer.
At this point another layer is deposited on top and the photolithography process is repeated with a different pattern or mask.
As previously mentioned, this cycle of deposition, photolithography and etch may occur many times during the construction of the micro-sized components and their related electronics.

## Slide 9: Surface Micromachining - CMP
CMP or Chemical Mechanical Polishing is used after one or two structural layers to flatten the bumpiness in the topography of the wafer’s surface.
Without CMP
With CMP
[Scanning Electron Microscope (SEM) images courtesy of Sandia National Laboratories]
Notes: After one to two layers have been deposited, patterned and etched, the top most layer starts getting bumpier and bumpier. In other words, the topography gets worse after each layer is processed.
We can mitigate this topography problem by using a process called chemical mechanical polishing or CMP. One type of CMP process, is to deposited a thick layer of sacrificial oxide followed with a polish (CMP). The polish removes the topography making the top of the sacrificial layer very smooth. The next structural layer is then deposited. This structural layer will now be flat on the bottom allowing the structure to move freely once the sacrificial layer is removed.
The image in the left shows the severe topography resulting if no CMP is done. Compare this to the image on the right. In this case a polish is done between the sacrificial and structural layer depositions. You can see that the components made using CMP will move more freely and easily than those fabricated without CMP.

## Slide 10: Surface Micromachining – Components
Comb Drive
Sandia National Labs
RF Switch
SCME
Chain
Paul Tafoya
SAW Sensors
Actuators
RF Switches
Inertial Sensors
Cantilevers
TRA’s
Notes: Surface micromachining is used to build a variety of devices and many of the devices are already found in consumer and commercial products such as cars, computers, phones, and medical devices.
Components built using surface micromachining include the combdrives, RF switches, and gear and chain systems such as those seen in these images. Other components built using surface micromachining include surface acoustical wave sensors, inertial sensors, cantilevers, and digital mirrors.

## Slide 11: Bulk Micromachining
Microcantilever Chemical Sensor Array
[Image courtesy of Dr. Christoph Gerber, Institute of Physics, University of Basel]
Notes: Bulk micromachining is a process that defines structures by selectively removing or etching into a substrate. Bulk Micromachining makes structures such as this Micro Cantilever Array possible. These cantilevers were fabricated by removing the bulk of the silicon substrate from under the structures.
Such cantilever arrays are being developed for “applications in chemistry, physics, biochemistry and medicine”.

## Slide 12: Bulk Micromachining
Removes the “bulk” of a material
Subtractive process
Cliff dwellings at Mesa Verde – an example of bulk etching
Micro-machined structures formed into the wafer substrate
[Image printed with permission from Barb Lopez]
Notes: Bulk Micromachining is a selective subtractive process which usually removes the bulk of a material. A couple of bulk etched products that you may be familiar with are Mt. Rushmore in which a bulk of a mountain was removed and ancient Indian cliff dwellings such as the ones shown in the picture of Mesa Verde in Colorado. For cliff dwellings the side of a cliff was removed and sculptured to create homes or dwellings.

## Slide 13: Bulk Micromachining
Three-dimensional MEMS device within substrate
Selective anisotropic etch
High volume manufacturing such as sensors
Bulk micromachined devices typically have high aspect ratios.
Backside of MTTC Pressure Sensor
(100)
(111)
Silicon nitride
Microfluidic channels with high aspect ratio fluidic chambers [C. Ionescu-Zanetti, R.M. Shar, J. Seo, Y.Jan, and L.P.Lee (PNAS, 2005). Printed with permission by Luke Lee, Dept. of Bioengineering, UC-Berkeley)]
Notes: Bulk Micromachining is a process in which monocrystalline silicon wafers are selectively etched to form three-dimensional MEMS devices. As I mentioned before, this is a subtractive process in which a bulk of the substrate is selectively removed.
Bulk micromachining takes advantage of the crystalline structure of the substrate by using anisotropic etch processes. The upper photo was taken from the backside of a MEMS pressure sensor fabrication wafer. This hole is the pressure reference chamber for a MEMS pressure sensor.
The bottom image shows a series of fluidic chambers and channels that have been bulk etched into a substrate. In both of these examples, you can see that the height of these chambers and holes are higher than the devices we saw in surface micromachining. This illustrates how the aspect ratio, which is the ratio of the height to the width, is higher in bulk than in surface. In fact, bulk micromachining can produce aspect ratios as high as 100 to 1 whereas components constructed using surface have an aspect ratio of 10:1 or less.
Omit the following from the script.
Credit for microfluidic chambers/channels: Microfluidic channels with high aspect ratio fluidic chambers [Image courtesy of Berkeley. Ref: C. Ionescu-Zanetti, R. M. Shaw, J. Seo, Y. Jan, L. Y. Jan, and L. P. Lee (PNAS, 2005)]

## Slide 14: Bulk Micromachining Processing
Deposition
Photolithography
Etch
  structural layers
  sacrificial layers
Bulk dry or wet etching of relatively large amounts of silicon substrate
[Image courtesy of Khalil Najafi, University of Michigan]
MEMS pressure sensor (frontside/backside) [Images courtesy of MTTC/UNM]
Notes: Bulk Micromachining involves some elements of surface micromachining and uses many of the same processes. In addition, Bulk micromachined structures can be coupled with surface micromachined components such as thin membranes, valves, thin piezoresistors and cantilevers.
Here we see two types of structures: The top images show the electronic sensing circuit of a MEMS pressure sensor on the left and the backside reference chamber on the right. The sensing circuit has been patterned into a metal layer using surface micromachining. The image on the right is the backside of the pressure sensor that consists of a bulk etched chamber. You can see the sensing elements of the sensing circuit at the top of the chamber.
The bottom image is a microfluidic membrane valve with a bulk etched inlet and surface micromachined valve plate on top. The proof mass in the center connected to the substrate via springs has been bulk etched from within the substrate.

## Slide 15: Bulk Micromachining – Etch Profiles
Isotropic Etch
Anisotropic Etch
Wet Etch vs. Dry Etch patterns
Anisotropic
Isotropic
Slow etching
crystal plane
Etch Mask
Notes: To produce a bulk etched component, the process requires a single crystal substrate on which a thin film of material is deposited. This film acts as an insulator, isolator or mask during the etch process. Eventually, this film may be patterned and etched, or completely removed.
Depending on the process and material used, various etch profiles can be obtained. The etch process can result in either isotropic or anisotropic structures depending upon the etchant and the material being etched. The type of substrate and the etchant can control the shape of the final etch.
A myriad of wet and dry etching techniques have been developed to achieve almost any desired structural shape. Some typical structures include grooves and slots that aide in assembly, nozzles that are used in inkjet print heads, cavities that create open volumes beneath membranes for pump and sensor applications, and holes and grooves that allow fluids to pass through.

## Slide 16: Bulk Micromachining – Components
  Cantilever Arrays
  Nozzles
  Microfluidic channels
  Needle arrays
  AFM Probes
  Membranes
  Chambers
  Through Wafer connections
Cantilever array
[Image courtesy of Seyet, Inc.]
[Image courtesy of Khalil Najafi, University of Michigan]
Notes: Here are some of the components possible using bulk micromachining. The top graphic illustrates a cantilever array that can be etched out of the substrate. The lower graphic is typical of the 3 axes accelerometer used in airbag deployment sensor. The proof mass that moves due to the acceleration is etched from the substrate.

## Slide 17: LIGA
[Graphic representing angled structures possible through LIGA processing]
Lithographie (Lithography), Galvanoformung (electroforming), and Abformung (molding)
Notes: Now let’s take a look at a third micromachining process called LIGA. LIGA was developed in the early 1980’s in Germany and is a German acronym that basically stands for lithography, electroforming, and molding. LIGA allows for the fabrication of unique devices not easily possible with surface or bulk micromachining. One such device is illustrated here. This image illustrates a mesh of angled structures that can be created by using LIGA.

## Slide 18: LIGA
  Additive process
  HARMST – High Aspect Ratio Microstructure Technology
  Structures have precise dimensions and good surface roughness
  Output - Finished parts, molds, or stamps
LIGA-micromachined gear for a mini electromagnetic motor
[Courtesy of Sandia National Laboratories]
Notes: LIGA is an additive, lithographic process which allows for the fabrication of complex, three dimensional structures with aspect ratios greater than bulk’s 100:1. LIGA is a type of HARMST process – High Aspect Ratio Micro-Structure Technology. Devices can be several millimeters tall and only a few microns wide. LIGA can also produce high aspect ratio molds allow for mass-production of micro-sized components mad of polymers, metals, or other molded materials.

## Slide 19: LIGA Process
[Image courtesy of HT MicroAnalytical, Inc.]
Deposit
Expose
Develop
Electroform
Planarize
Strip
Release
Notes: Let’s look at an overview of the LIGA process. The process is very similar to surface and bulk, but different materials and equipment are used. Plus there are a couple of steps unique to LIGA.
The first step is to apply a thick x-ray sensitive material such as PMMA, also known as Plexiglas to a conductive substrate. The next step is expose, followed by develop. After develop an electroplating or electroforming process fills the cavities formed during develop. Electroforming is following by CMP, then a PMMA strip and component release.

## Slide 20: LIGA Lithography
[Image courtesy of HT MicroAnalytical, Inc.]
Photosensitive Material: PMMA (polymethyl methacrylate) or Plexiglass
Light Source: Colimated Synchrotron radiation (x-ray)
Notes: Looking at these steps in more detail…The substrate for the LIGA process is a conductive material such as silicon or titanium. A layer of PMMA is either spun on the substrate or bonded to the substrate surface.
The masks used for LIGA are constructed with a substrate that allows X-rays to pass through such as beryllium or silicon, and then patterned with an X-ray absorbing layer such as gold or copepr. The graphic illustrates a patterned gold layer on top of a beryllium mask. The beryllium is transparent to x-rays.
For the expose step collimated x-rays from a synchrotron radiation source is directed toward the mask. The gold absorbs the x-rays while the openings in the gold layer allow the x-rays to penetrate the mask’s substrate and expose the PMMA layer underneath.
Like photoresist, the radiation modifies the PMMA so that the exposed material can be removed with a suitable or selective developer solution.

## Slide 21: The LIGA Process
[Images courtesy of HT MicroAnalytical, Inc.]
Notes: After expose is develop. In develop, the exposed PMMA is removed leaving a mold with high aspect ratio cavities, holes, or trenches. These cavities are filled with metal using an electroforming or electroplating process. Each of these process is explained in more detail in the micromachining lesson.

## Slide 22: The LIGA Post Process
Planarize, Strip PMMA, Release
Stamping or molding
Component level OR wafer scale assembly
Wafer scale bonding
  Multi-layer structures
  Packaging
Requires extensive, unique metrology
[Images courtesy of HT MicroAnalytical, Inc.]
To view this animated process, go here: https://youtu.be/CbN7h3o51Zo
Notes: The electroformed metal is planarized to flatten the top or surface. The PMMA is then removed and when applicable, the part is released. Depending on the component, the remaining structure could be used as a stamp, to make molds or be the end product.

## Slide 23: LIGA Structures
Molded fiber Optic Cable holders
PMMA 30m posts, 3m spacing, 300m tall
Precision miniature spring
Notes: This slide illustrates some examples of LIGA parts. Note the very high aspect ratios. LIGA can be used to build structures millimeters tall and a few micrometers wide, like the posts in the upper graphic, or a few microns tall and a few nanometers wide, like the coils of the spring.

## Slide 24: LIGA – Components
  HARMST
    Turbines
    Gears
    Springs
    Clips
    Needle Arrays
    Shutters
    Gratings
    Packaging
Ant with a LIGA micro-gear.
Image courtesy of Rorschungzentrum Karlsruhe, Germany
Notes: This is probably the most famous LIGA SEM in the world – it has been attributed to the folks at ANKA in Germany. This SEM shows a LIGA made gear on being held up by an ant’s foot.
LIGA Micromachining provides an extensive set of unique components for microstructure fabrications such as turbines, gears, springs, probes, and gratings. LIGA components extend the additive approach to accommodate interfaces and packaging issues.

## Slide 25: Summary
MEMS fabrication (also called micromachining) has allowed for the manufacturing of micro-sized devices that can be fabricated on top of substrates, within substrates, or molded and bonded.
Three widely used micromachining processes are
surface micromachining
bulk micromachining, and
LIGA (Lithography, Galvanoformung, and Abformung).
Notes: Surface, bulk and LIGA fabrication or micromachining processes have allowed for the construction of unique microsystems, devices and components. The number of devices that could be fabricated using these processes is limitless.
At this point, it is recommended that you read the MEMS Micromachining unit for more detailed information about these processes and complete the activities associate with this learning module.

## Slide 26: Acknowledgements
Made possible through grants from the National Science Foundation Department of Undergraduate Education #0830384, 0902411, and 1205138.
Any opinions, findings and conclusions or recommendations expressed in this material are those of the authors and creators, and do not necessarily reflect the views of the National Science Foundation.
Southwest Center for Microsystems Education (SCME) NSF ATE Center
© 2010 Regents of the University of New Mexico
Content is protected by the CC Attribution Non-Commercial Share Alike license.
Website: www.scme-nm.org
Rev June 2017
Notes: You can download the supporting MEMS Micromachining Learning module and activities from the SCME website.
Thank you for viewing this presentation produced by the Southwest Center for Microsystems Education.